## Slide 1: Summary, WPTE and WPPWIE plans for W dust studies in 2024-2025
Antti Hakola
On behalf of the WPTE and WPPWIE teams
Joint WP TE and WP PWIE Technical Meeting on Plasma Wall Interactions in full W devices

## Slide 2: Summary of the dust session
Dust studies on WPTE devices: lots of data and samples available from several campaigns – where to put the focus?
  AUG – dust collectors and dust particles analysed extensively and lab investigations made  Open questions: Do we catch all the underlying physics? Can all the estimated mass be collected? Extrapolation to ITER? Is arcing the most important mechanism for dust production also in ITER?
  WEST – extensive dust collection and microscopy studies performed but quantitative analyses largely pending  Open questions: link to WEST operations (origin of dust)? Testing ITER electrostatic collector for B dust in WEST?
  JET – dust collected over the years but little produced during ILW campaigns  Open questions: relation of W dust production to flaking and thermal cycling? Is 2-4 % conversion factor of deposits into dust JET specific?
Dust remobilization is quite well understood based on >10 years of work (MAGNUM-PSI, AUG,… + modelling)
  BUT: Impact of irregular W particles on adhesion/remobilization? Treatment of big flakes ejected from PFCs?
  BUT: B dust is a completely new field – main complexities material properties and irregular shape  carefully designed experiments in LPDs or tokamaks (using B dropper)? How relevant is B dust for ITER?
Proportion of various sources in dust production for ITER, generalization of results, integral number for dust formation, dependence on parameters other than mass
Dust formation addressed experimentally and via modelling – several pathways identified to form nanoscale dust
  Can we generalize the results to microscale dust observed in tokamaks?
  Applicability to B dust?
We have several labs available for analysing dust particles – MPG, CEA, IPPLM, RBI, VR,…
  Microscopy is/has been the key tool, fuel retention much less understood (machine specific – role of C)  IBA analyses to be strengthened

## Slide 3: Ongoing dust activities – a small community recently increased in volume
Deliverable ID: | Deliverable Title: | Volume (PM)
D001 | Database of the characteristics of produced W dust particles and comparison with data from tokamaks (IAP)  laboratory studies | 1,5
D002 | Database of the characteristics of produced B dust particles and comparison with data from tokamaks (IAP)  laboratory studies | 1,5
D003 | Document on the characteristics and amount of dust generated on ASDEX Upgrade during past experimental campaigns and on the connection of arcing on dust production (MPG)  dust analyses | 2,0
D004 | Document on the physical and remobilization characteristics of dust produced on ASDEX Upgrade and MAGNUM-PSI (VR)  review of dust properties | 2,0
D009 | Fracture and strentgh properties of B and W reference layers on W (UKAEA)  laboratory studies | 2,0
D010 | Ion-beam analyses of dust samples originating from ASDEX Upgrade, WEST, and W7-X (RBI)  dust analyses | 4,0
D011 | Report on the properties, composition, and amounts of dust produced on WEST during the Phase 1 operations (CEA)  dust analyses | 3,0
D012 | Microscopy and LIBS analyses of dust samples originating from ASDEX Upgrade, WEST, and W7-X (FZJ)  dust analyses | 2,0
D013 | Ion-beam analyses of dust samples originating from ASDEX Upgrade, WEST, and W7-X (VR)  dust analyses | 3,0
+ Additional activities foreseen in 2025 for VR and IPPLM

## Slide 4: Plans for 2024-2025
So far very few experimental proposals on WPTE devices – let’s see if many more will come up during the presently ongoing Call for Proposals
  Pre-plasma mobilization of magnetic dust PB (AUG) – presently considered as a candidate in 2025
  Call for proposals open until 11 October
Within WPPWIE, we have just got additional resources for dust analyses
  More emphasis on samples coming from tokamaks (AUG, WEST) and stellarators (W7-X)
  Better understanding of the underlying physics to make extrapolations to ITER
Other WPPWIE dust activities expected to continue also in 2025
  Production of W and B dust particles – finding out parametric dependencies of the underlying mechanisms  how many more experiments are required or should we concentrate on analysing the database?
  Remobilization characteristics of dust particles – do we need more experiments or just more modelling?
  Fracturing of B/W deposits to generate dust particles – should we have more focus put on off-normal event than normal operations in tokamaks?