## Slide 1: Sp B.1 Exposure of W samples to PSI-2 plasmas
O. Marchuk, M. Sackers, M. Rasinski, S. Brezinsek, A. Houben and A. Kreter
Forschungszentrum Jülich GmbH – Institute of Fusion Energy and Nuclear Waste Management - Plasmaphysik,
Partner of the Trilateral Euregio Cluster (TEC), 52425 Jülich, Germany

## Slide 2: Plans for 2024
High resolution (HRS) and imaging spectroscopy (IS) of bulk and redeposited W and B layers in PSI-2
Study of sputtering rates of W+B layers in PSI-2
B I lines in visible range only at different flux of D
Erosion rates of W in linear cross machine comparison study
VUV Spectroscopy for W and D atomic and molecular lines

## Slide 3: Setup of Psi-2

## Slide 4: Spectroscopic studies on W in PSI-2
Study of erosion and redeposition of W atoms/ ions using spectroscopy
W targets: poly W, W (111), W (110), W (100)
Plasma pressure : 0.01…0.1 Pa
Electron temperature: 1..20 eV
Electron density: 1010…1012 cm-3
Magnetic field: 0.025…0.1 T
Ionization degree: 1-5%
Targets: 13x13mm2
5
(1-5 are the line-of-sights)

## Slide 5: High resolution spectroscopy
S. Ertmer , PhD thesis, High-resolution spectroscopy studies on sputtered atoms in the linear plasma device PSI-2
RUB Bochum, https://doi.org/10.13154/294-8580
PSI-2
Spectral dispersion ~ 0.7 … 1.0 pm/ch
FWHM (Full Width Half Maximum) ~ 5-7 ch
Energy distribution
of sputtered atoms :
Kinetic energy , DE ~ 10 eV
Doppler Effect Dl/l0 = v/c
l0 - is the wavelength of transition,
v - is the velocity of W atoms
c – is the speed of light.
l0 @ 500 nm : DlW/l0 = 10-5
DlFWHM/l0 = 7*10-6
a
b
spectrometer
photons
Measurements
of energy distribution

## Slide 6
Calibration/Measurements/Modelling of the W spectra
Sackers M et al, Phys. Plasma (submitted)
498 nm
M. Sackers et al, Phys. Scripta (2023) 98 115603
Effect of finite –size target
Zeeman Effect
Instrumental Broadening
Hyperfine structure splitting
Finite lifetime of excited levels
Energy and angular distribution

## Slide 7: Different W ORIENTATION
Different line shapes for
different orientation [1]
Comparison with
PARCAS MD simulations [2]
Information on energy
and angular distribution of W atoms for the ion energy close to threshold
Control of surface roughness is required
[1] Sackers M et al, Phys. Plasma (submitted)
[2] Nordlund K, Comput. Mat. Science 3, 448-456 (1995)

## Slide 8: Application of HRR Spectroscopy for Layers
W target with fuzz
W target
Intensity and line shape stays constant for W target
Intensity and reflectivity increase for W fuzz target
within of 15-20 min (removal of fuzz)
Monitoring the processes on the surface

## Slide 9: Spectroscopy of B I @ 250 nm on W at PSI-2
W-target /100 nm B layer
Mo mask
W dummy
To PSI-2 using line of sight (#4)
(Backillumination)
(Calibration HCL)
PSI-2 (D2)
Dt=10s
B I @ 250 nm
(see talk A. Houben SP B.4 @ 14:35)
los

## Slide 10: Problem with Erosion rate of W @ Psi-2
Presence of Ar ++ in the plasma of PSI-2 [1] (spectroscopically not detected)
Sputtering by heavy Z elements (Mo and W from the manipulator)
Incorrect estimation of ion flux to the target
Measurements using two different manipulators were performed
at the same position.
Line shape at 90°
[1] Sorokin et al, Nuclear Materials and Energy 12 (2017) 1243–1247

## Slide 11: Comparison in EROSIOn Rate
Plasma parameters:
Plasma current 150 A
Exposure time – 20 min
Bias -60 V
Pressure 0.04 Pa
1. Small manipulator. Erosion length is about 2.5 m.
2. Large manipulator. Erosion length is about 3 m.
Sputtering by Mo or W ions could be excluded at our conditions
Ion flux data and presence of Ar++ must be still investigated ( fast reflected Ar)
Experiments with Ne gas are foreseen (higher ionization potential)

## Slide 12: CONCLUSIon
High resolution (HRS) and imaging spectroscopy (IS) of bulk and redeposited W and B layers in PSI-2 (partially done)
Study of sputtering rates of W+B layers in PSI-2 (done)
B I lines in visible range only at different flux of D (done)
Erosion rates of W in linear cross machine comparison study (partially done)
VUV Spectroscopy for W and D atomic and molecular lines (to be installed within 1 Month)