## Slide 1
Temperature (K)
t0 = 10 ns
Electron density (m-3)
t0 = 10 ns
On Eurofer97 containing
Fe, Cr, Cu, W, Na, Mn, V measured by XRF
Plasma thickness (mm)
t0 = 10 ns
Saha-Boltzmann plot
A. Bultel, A. Favre – Validation of the MERLIN code (spectra calculations)
Spectral radiance
relative difference
Spectral radiance
A. Favre, A. Bultel et al. JQSRT 330 (2025) 109222
https://doi.org/10.1016/j.jqsrt.2024.109222
At time t = 950 ns:
experimental spectrum
reconstruction by MERLIN
blackbody radiation

## Slide 2
FLATEN
DENSE + ReLU x5
Multi-layer perceptrons: decision
DENSE + ReLU + Softmax
DENSE + ReLU + DENSE
DENSE + ReLU + DENSE
105 spectra calculated by MERLIN with 12 parameters:
mole fraction in Ag, Ar, B, C, Cu, H, Mo, Ni, W
around the wavelength
at
related to LIBS measurements performed in WEST
A. Bultel, A. Favre – Coupling between Machine Learning and MERLIN for real time CF-LIBS
A. Favre… A. Bultel accepted in Spectrochim. Acta Part B
x 6
CONVOLUTION
RESIDUAL BLOC x4
MAX POOL
NORMALISATION
ReLU
CONVOLUTION
STACK
Convolutional Neural Network: information extraction
Input
MERLIN
(wavelength, spectral radiance)
A. Favre, A. Bultel et al. Phys. Scr. 99 (2024) 035609
https://doi.org/10.1088/1402-4896/ad2826
Learning  Loss function:
where is the prediction, the target and the prediction confidence on the parameter
Best prediction!
Tests for the quantification:
Outputs:
9 mole fractions
12 x
Lowest predicted value for H:
Real time test of the whole procedure (1000 times):
Writing-reading of a spectrum
Calibration
Image treatment
Network response
At 10 Hz: analysis at each laser shot