## Slide 1: PWIE SPX meeting
Indrek Jõgi
University of Tartu

## Slide 2: Analysis of B containing coatings and/or W coatings with LIBS
Chart: S-coordinate (mm)
| 507 | 452.5 | 415.5 | 358 | 352.5
 | 0.0010122 | 0.0092176 | 0.023011 | 0.0023743 | 0.013567
 | 0.0023999 | 0.0018044 | 0.26706 | 0.014473 | 0.010057 | 0.0090606
 | 0.3674 | 0.50294 | 0.46054 | 0.97285 | 1.4281 | 0.34708
 | 0.085 | 0.081 | 0.249 | 0.314 | 0.895
s (mm)
GDOES
LIBS
SIMS
GDOES
GDOES
GDOES
GDOES
LIBS
SIMS
SIMS
SIMS
SIMS
LIBS
LIBS
LIBS
LIBS
546
376
293
237
142
14
32
507
565
489
356
341
311
274
254
104
89
199
415
453
SIMS
SIMS
SIMS
SIMS
Chart: Wavelength (nm)
B I lines
C I line
LIBS spectrum
shot nr
Comparison of B depth profiles and total B determined by LIBS, SIMS and GDOES on WEST 32i/20o tiles
0.26
C
Mo – 3 μm
W – 12 μm
W – 0.9 to 2 μm
Mo marker – 100 nm
LIBS
SIMS
B depth distribution in C4-32i erosion region
GDOES

## Slide 3: LIBS results on He loaded samples and surface modifications
Chart: Crater nr
 | 671.3972 | 1585.0546 | 2556.7799 | 2452.3041 | 1703.6581 | 444.7446 | 345.2258
1 μm c-W
ToF-ERDA He retention (150 nm)
Edge 16·1015 at/cm2
Center 247·1015 at/cm2
LIBS He intensity
LIBS Depth profiles
Formation of Ta/Mo rich surface layer in the Center (up to 4 shots)
Chart: Wavelength (nm)
He spatial distribution
Chart: LIBS shot nr.
 | 67.6755 | 329.042 | 401.3176 | 501.2802 | 490.6637 | 459.203 | 438.2998 | 401.6839 | 370.4051 | 353.0672 | 259.8541 | 257.7327 | 247.0347 | 220.4804 | 203.9593 | 194.9484 | 152.6099 | 160.5425 | 132.7596 | 145.6177 | 129.0606 | 117.1456 | 130.1997 | 100.3319 | 112.2176 | 106.379 | 97.5245 | 93.3688 | 87.3022 | 75.6907 | 80.2949 | 81.087 | 70.4702 | 67.6873 | 72.6601 | 54.713 | 59.2419 | 55.3177 | 65.5774 | 58.1888 | 36.4135 | 42.9985 | 45.9356 | 42.4343 | 30.3575 | 35.1261 | 30.0992 | 25.0778 | 24.5113 | 28.1455
 | 721.7777 | 1469.7383 | 1029.6933 | 540.8832 | 293.7084 | 202.261 | 150.8726 | 165.7178 | 156.1019 | 203.5801 | 195.7376 | 271.7038 | 303.0879 | 309.7959 | 346.2441 | 385.9736 | 357.8411 | 412.6928 | 367.2521 | 450.4576 | 478.7066 | 462.5188 | 514.6989 | 510.059 | 475.5026 | 499.222 | 516.5494 | 481.8633 | 494.9026 | 467.852 | 543.4415 | 495.4895 | 539.2139 | 614.2153 | 577.4436 | 595.0146 | 574.3208 | 573.2951 | 636.7548 | 576.741 | 616.0297 | 597.8618 | 610.5617 | 630.5763 | 660.1141 | 602.7432 | 612.7718 | 715.7609 | 641.4421 | 651.0426
 | 515.9235 | 1250.7914 | 659.279 | 311.864 | 137.2234 | 71.4157 | 54.6616 | 57.7135 | 40.6214 | 34.9987 | 26.7925 | 18.1379 | 11.2439 | 12.2468 | 8.0076 | 3.0375 | 6.0603 | 0.095428 | 0.85736 | -3.5539 | -0.66744 | -3.0953 | -4.4701 | -6.7843
 | 817.3333 | 84.6667 | 31.6667 | 0
Chart: LIBS shot nr.
 | 518.8342 | 664.9329 | 619.0527 | 513.8857 | 412.2777 | 296.1433 | 179.4034 | 144.5021 | 111.9691 | 103.0739 | 77.314 | 80.1035 | 68.226 | 77.703 | 75.4093 | 70.5941 | 77.8917 | 68.6027 | 59.699 | 58.8008 | 59.9987 | 62.8534 | 46.7727 | 60.6612 | 51.2629 | 44.0785 | 39.0649 | 39.0246 | 34.6278 | 32.9057 | 38.9514 | 29.5052 | 29.486 | 22.217 | 27.034 | 19.6045 | 24.0195 | 19.8212 | 17.7902 | 8.431 | 16.3718 | 9.0164 | 11.9384 | 10.1346 | 2.1144 | 7.2403 | -0.12185 | 5.3552 | 0.31077 | 4.0247
 | -2.876 | 0.084893 | 32.5249 | 68.5497 | 174.8832 | 403.0686 | 540.432 | 633.1791 | 669.7341 | 693.1371 | 572.9666 | 628.3176 | 567.3107 | 611.3033 | 590.5046 | 612.4124 | 608.7432 | 623.5932 | 571.8473 | 572.7764 | 654.8334 | 610.4142 | 626.0515 | 664.1881 | 704.2545 | 674.9074 | 639.7289 | 672.9841 | 718.9476 | 704.3569 | 728.0786 | 644.8561 | 701.5299 | 673.8097 | 720.6874 | 710.7565 | 688.9195 | 720.5324 | 729.9191 | 676.1736 | 701.7455 | 667.906 | 702.4268 | 691.732 | 726.5931 | 714.2481 | 699.8983 | 678.7302 | 712.0476 | 641.0851
 | 12.5787 | 12.9311 | -6.1759 | 1.2391 | -12.2011 | -7.39 | -9.8065 | -11.5194 | -12.8748 | -12.0329 | -9.6302 | -18.3559 | -13.4301
 | 115 | 21.6667 | 0 | 0
He detectable during first LIBS shot
Magnum-PSI He plasma exposure 2700 s

## Slide 4: Outgassing, recycling and retention after D plasma loading
Chart: Crater nr
 | 54 | 45 | 43 | 48 | 56 | 63 | 60
 | 40 | 23 | 29 | 27 | 34 | 35 | 42
Chart: Crater nr
 | 104.4852 | 112.6958 | 77.5983 | 86.9675 | 113.3177 | 120.9156 | 123.0837
 | 90.424 | 90.5436 | 75.7615 | 44.7817
Magnum-PSI D2-N2 or D2-Ne plasma exposure 2700 s, example for 5 μm c-W
Chart: LIBS shot nr.
 | 104.4852 | 23.8388 | 14.9633 | 15.3167 | 9.9214 | 8.0213 | 15.5574 | 15.2181 | 14.0811 | 15.3998 | 15.0222 | 13.5362 | 14.5728 | 14.6159 | 13.7418
 | 112.6958 | 20.2631 | 18.5045 | 14.3558 | 10.7118 | 16.4814 | 16.5501 | 16.3281 | 15.6468 | 14.3163 | 15.8791 | 12.9255 | 17.3988 | 13.0679 | 12.9765
 | 77.5983 | 17.8712 | 16.5126 | 10.2904 | 12.3993 | 12.314 | 12.7368 | 16.6352 | 15.9356 | 15.75 | 15.9931 | 15.5547 | 15.5209 | 15.0352 | 15.3996
 | 86.9675 | 20.5954 | 20.0853 | 13.7884 | 13.8654 | 17.3857 | 16.4107 | 17.8613 | 17.0466 | 16.4707 | 15.7131 | 13.0679 | 14.9826 | 15.0142 | 14.1082
 | 113.3177 | 23.6484 | 18.0032 | 11.6135 | 12.2152 | 15.1628 | 15.3064 | 14.5145 | 17.0836 | 17.9994 | 14.925 | 19.0104 | 18.5325 | 16.5213 | 16.7876
 | 120.9156 | 29.9219 | 17.5971 | 10.8012 | 7.2253 | 12.7131 | 15.991 | 23.557 | 20.1696 | 18.6484 | 17.784 | 18.4106 | 16.1102 | 18.3064 | 14.6352
 | 123.0837 | 32.7437 | 20.7672 | 13.0175 | 12.6625 | 15.3846 | 19.6065 | 19.532 | 15.841 | 18.2976 | 20.1541 | 17.3838 | 17.712 | 15.3106 | 16.8209
Depth (nm)
0
317
633
950
1266
1583
1899
2216
101
100
10-1
10-2
0
2000
4000
6000
8000
10000
12000
14000
Depth (1e15 D/cm2)
D concentration (at. %)
NRA
Spatial distribution
Depth profiles
D2-N2 plasma
Depth profiles comparable
Spatial distribution for D2-N2 and D2-Ne plasma exposure somewhat conflicting

## Slide 5: LIBS on Be containing coatings with diferent type of fuel content
Chart: Wavelength (nm)
Cut-off by long fiber
Limitations for remote handling application
B and C are not detectable because strong lines near 250 nm absorb in long fiber and lines between 300-500 nm are too weak due to low LIBS plume temperature
Ghost lines present due to Echelle type spectrometer
H/D/T line intensities were near the detection limit and overlapping
Cut-off by mirror
Be I 332.1 nm
Be ghost lines
Chart: LIBS shot nr
Chart: SIMS depth (μm)
LIBS spectrum (2ONG7A-7)
W I lines
LIBS and SIMS depth profiles of 14IWG1A 11a
Samples were from different positions on limiters (2XR11, 4D15) and divertor (HFGC, 14IWG1A, 2IWG3A, b12_167, 2ONG7A, 2ONG8B).
Deposit layers distinguishable in LIBS depth profiles and confirmed by SIMS
Be, W, Mo, Fe, Ni, Cu, Cr, Ar, H, D were present in the spectra
Experiments in VTT for the preparation of JET remote handling operation
LIBS in atm. pressure Ar, 20 m fiber for signal collection and Echelle type Aryelle spectrometer for wide spectral range
LIBS
SIMS