## Slide 1: The diffusion of helium in tungsten-based refractory alloys by molecular dynamics
HeRHEA meeting
Guanying Wei
14 November

## Slide 2: Outline
Potential for He-refractory alloys
Binding energy(He-He, He-Vacancy)
Migration energy
Diffusion of He

## Slide 3: Potential He-refractory alloys

## Slide 4: Potential He-refractory alloys
Fitted property for metal – He and comparison with DFT as well as existing data.

## Slide 5: Check the stable configuration for 2 He atoms (From Toni Sutinen)
Put the first He at a Tetrahedron site, then the second He is put at another Tetrahedron which is far away from the first one 0.5 -5.0 Å with 0.5 as interval. Do the minimization and check the final distances between 2 He atoms.

## Slide 6: Binding energy between He clusters​
Pure metals
V-free materials: increase
V-containing materials:decrease

## Slide 7: Binding energy between He and Vacancy​

## Slide 8: Migration energy of a He atom​
He position​ | WTa​ | WMo​ | WTaMo ​ | WV​ | WTaV​ | WTaVMo​ | WTaVMoNb​
(0,0.5,0.25)*a ​ (0,0.5,0.75)*a | 0.2002+- 0.0041​ | 0.1319+- 0.0027​ ​ | 0.1961+- 0.008​ ​ | 0.4310+- 0.0074​ ​ | 0.3422+- 0.0053​ ​ | 0.3244+-0.0053​ ​ | 0.2887+- 0.004​ ​

## Slide 9: Migration energy of a He atom​
WMo
WTaVMoNb
The effect of entropy on the He migration

## Slide 10: Migration energy of a He atom​
Effect of Helium Atom Coordination Environment on its Migration

## Slide 11: Diffusion of He (MD simulation)
Box size: 20*20*20 = 16000 atoms + 0.1% Vacancies(16) +1% He (160 atoms)​
Potential: tabGAP potential + He-He pair potential​
Minimize first​
NPT relax 5 ns at 300 K, 900 K and 1500 K

## Slide 12: Cluster fraction
Growth with the temperature, He atom prefers to be individual in V-containing materials.

## Slide 13: Distribution of cluster size(V-free)​

## Slide 14: Distribution of cluster size​(V-containing)

## Slide 15: Evolution of He​

## Slide 16: Thank you for your attention!
Notes: Thanks