## Slide 1: 2025 Annual Work Plan => ITER support Work Package WP05-PWIE Plasma Wall Interaction and Exhaust
WP Project Leader
Sebastijan Brezinsek

## Slide 2: 2025 Objectives: Focus ITER support (I)
Impact of the tungsten first wall on tungsten source strength: simulation of first wall W erosion, deposition, and screening in limited, start-up, and diverted plasmas in ITER
=> first wall erosion, profiles to the wall, CXN and seed species (EAST neutral particle data as benchmark)
=> partially with IO plasma background / Thrust 2 activities TSVV-5,6,7 / SP D activities
=> PWIE code benchmark experiments in TE experiments
=> Atomic and molecular data of W (revised W line selection for ITER)
Understanding layer formation in WEST high fluence experiment: mimic WEST divertor conditions in MAGNUM-PSI, layer stability in laboratory experiments, HHF experiments and incorporate in migration simulations
=> Characterisation of layers under WEST-like flux , impact energies and material temperature conditions in lab experiments
=> Full analysis of post-mortem samples (… dust conversion factor)
=> Simulation of experiments with ERO2.0
W first wall PFCs damage predictions: Impact of VDEs and REs on ITER PFCs (transfer from Be PFCs)
=> Post-mortem analysis at JET: Be First wall and W divertor (ramp down RE at end of JET lifetime)
=> Simulations of REs and transfer from JET to ITER (partially in TSVV-7)
=> Operation beyond PFC specification and damage evolution of W PFCs
Temporary W first wall components testing: HHF and steady-state plasma exposure
Facilities available and discussion with IO about coatings (discussions on existing techniques / WP DIV)

## Slide 3: 2025 Objectives: Focus ITER support (II)
Characterisation of boron layers and impact on wall conditions: B layer properties, oxygen gettering, homogeneity, benchmark experiments for ERO2.0 modelling (incl. boronization experiments) *
Advanced simulation of physical and chemical erosion of boron: MD simulation data, benchmark experiments in linear plasma devices, and their simulations
Initial simulation of Boron migration and lifetime assessment: B first wall, mixed surface, thin B layer
ITER first mirror performance in the presence of boron: boronization / boronization + plasma / deposition*
Impact of boron on tritium retention in ITER: Start of T retention matrix (scaling law), T removal techniques (ICWC, ECWC, GDC), in-situ and ex-situ T quantification techniques (laser-techniques, NRA, TDS)
Active removal of fuel-containing boron layers: erosion, dust formation, and dust properties (i.e. TOMAS)
Wall conditioning optimisation: ECWC, ICWC, GDC and combinations to be tested in TOMAS
Laser-based technique development for thin B layers and partially eroded layers (in-situ/ex-situ)
Transfer of in-operando laser-based technique from JET and linear plasmas to ITER
Experiments coordinated with WPTE and WPW7X : linked by pre/post-mortem analysis and modelling

## Slide 4: 2025 Description of Work: Focus ITER support (I)
Meeting EUROfusion - the European Commission
February 2025
Understanding layer formation in
WEST high fluence experiment
Mimic W flux, divertor plasma,
and PFC temperature conditions
in MAGNUM-PSI
Impact of thermal stresses
on W layer stability during
W migration
Characterisation of boron layers
and impact on wall conditions
Impact of boron on
tritium retention in ITER
In operando studies of boron layers
and fuel retention in PSI-2 via LIBS
and post-mortem analysis
Mimic ITER B erosion, SOL-plasma,
and PFC temperature conditions
in D plasmas in PSI-2
Laboratory, tokamak and linear plasma studies to assess fuel content in co-deposited and implanted D in boron layers
Mimic ITER conditions during deposition of B (scaling law)
=> Be, W and C matrix exist!

## Slide 5: 2025 Description of Work: Focus ITER support (II)
Meeting EUROfusion - the European Commission
February 2025
W erosion, prompt re-deposition,
and first wall fluxes W sources
Operational space of linear machines
regarding impact energy and D ion flux
covering ITER conditions
Predictive simulation of W erosion, influx and migration in ITER. Experiments to address
e.g. code assumptions on erosion at wall
Analysis of JET-LIBS data (RH arm) and start of post-DT tile analysis
Interpretation of LIBS data and provision
of spatial and depth-resolved layer composition and fuel retention in JET post DT.
LID-QMS and LIBS applied in-vessel.
Comparison of in-vessel and post-mortem analysis for selected PFCs foreseen
Simulation of W sources and re-deposition in ITER
ITER-start up conditions coupled with ERO
ITER input
Scan of conditions and role of impurities
In W prompt redeposition at first wall
and divertor

## Slide 6
Substantial part of activities and linear, HHF and analysis machine time for ITER activities
HR and MR accountancy is complicated as part is also DEMO-relevant at the same time
TSVV-5 (EIRENE/NGM), -6 (SOLEDGE3X-/EMC3-EIRENE) and -7 (ERO/MIGRAINE)
are all supporting ITER simulations (partial change of scope in 2024)
Note: main PWIE laboratories have also ITER-contracts/partnerships
for some specific studies: CEA, FZJ, DIFFER, ERM-KMS, IPP?
=> No overlap, but complementary and extended work (ITPA as coordination)