## Slide 1: Update on Wf/W composites within SPA 3 – FZJ
Jan W.Coenen1,2 & Yiran Mao1 for the Wf/W Team
1: Forschungszentrum Jülich GmbH, Institut für Energie- und Klimaforschung 52425 Jülich, Germany,; 2: Department of Engineering Physics, University of Wisconsin Madison, WI 53706 Madison, USA
PWIE Meeting March 2025

## Slide 2: Crack formation for tungsten armor
Intrinsic brittleness of tungsten material
Thermal heat load at the divertor: thermal stress and thermal fatigue
G. Pintsuk et al. / Fusion Engineering and Design 88 (2013) 1858– 1861 1861
Neutron embrittlement
A damage resilient material is required
Accumulated equivalent plastic strain field in the tungsten armor block after the 5th HHF load cycle at 20 MW/m2.
-M.Li 2015.

## Slide 3: Long fiber tungsten fiber reinforced tungsten
Tungsten fiber-reinforced tungsten (Wf/W)
J. Riesch, Y. Han, J. Almanstotter, J.W. Coenen, T. Hoschen, B. Jasper, P. Zhao, C. Linsmeier, R. Neu, Development of tungsten fibre-reinforced tungsten composites towards their use in DEMO-potassium doped tungsten wire

## Slide 4: Flat tile mock-ups made of long fibre PM Wf/W
Flat tile mock-ups similar to DEMO standard design*
  Long fibre-reinforced PM-Wf/W
    fibre orientation 0/90°
    Yttria interface, thickness: L1  5 µm, L2  1.5 µm
  Brazing to CuCrZr cooling structure
  *) Area plasma facing surface 12 mm x 23 mm
top view L1
side view L2
L1
L2

## Slide 5: Production of Mockup based on longfibre Wf/W and High Heat Flux Tests
Strong surface temperature increase at the edges of tile 3 and 4 during 15 MW/m² cyclic loading
Optical microscopic analysis indicates that defects developed as well in the bonding zone between the tiles and the cooling structure, as in the Wf/W materials itself
CCD images during cyclic loading.
IR images during cyclic loading.
Chart: WfW flat tile mock-up-L1, cycling 15 MW/m², 10 sec.
shielding of damaged tile
scrapper

## Slide 6: Microstructure after HHF
after GLADIS L1
WfW L1 tile 4, bottom side, after GLADIS loading
WfW L1 tile 3, top side, after GLADIS loading
Joining with the heatsink could be the bottle neck of the component, but cracking and decomposition of the yttria is also observed

## Slide 7: Wf/W mock-up - monoblock chain
top view
side view

## Slide 8: High heat flux tests on monoblock mock-up
Hydrogen neutral beam HHF in IPP Garching
Screening to 12/15/20 MW/m2 followed by 100 cycles at 10/15/20 MW/m2
  Beam time 10s
  cold water cooling
Step | screening | cyclic loading | 
 |  | Load | Pulses
1 | up to 12 MW/m² | 10 MW/m² | 100
2 | up to 15 MW/m² | 15 MW/m² | 100
3 | up to 20 MW/m² | 20 MW/m² | 100
Chart: WfW (N2) monoblock mock-up, screening up to 15 MW/m²
| 6 | 6 | 8 | 8 | 6 | 6 | 8 | 8 | 10 | 10 | 12 | 12
T-QKTRD[C] | 699.5 | 698.9 | 884.5 | 882.2 | 690.2 | 691.1 | 873.5 | 872.5 | 1110 | 1108 | 1296 | 1306
T-QKTRD[C] before 20 MW/m² | 1111 | 1106 | 1632 | 1626

## Slide 9: HHF on monoblock mock-up
Chart: WfW monoblock mock-up, cycling 15 MW/m²
The surface temperature distribution is nearly stable during 10 MW/m² and 15 MW/m2 cyclic loading.
Wf/W blocks show higher surface temperature than pure W
Material is capable of surviving up to 100 cycles up to 20 MW/m2

## Slide 10: Plasma erosion
Neon plasma, 98-117 eV, flux: 1x ×1021 Ne+ m-2s-1, total fluence of 3 ×1024 Ne+ m-2, ~90⁰C in PSI-2
Before erosion
After erosion

## Slide 11: Plasma erosion
 | Mass loss | Depth loss
Reference W | ~2.85mg | ~2.4 µm
L-Wf/W | ~3.06mg | ~2.2 µm
Both samples match within the experimental uncertainty compared to the theoretical value.
The results show that the mass loss and erosion depth are comparable for both types of samples. Although L-Wf/W composites contain yttria at the fiber-matrix interface, which has a higher sputtering yield compared to tungsten, the volume fraction of yttria is so small that, it had minimal influence on the overall erosion properties.
the theoretical mass loss of pure W during the Neon plasma exposure is calculated as 3.3 mg based on:

## Slide 12: Laser shock
In PSI-2 1.6GW/m2 2ms
Lower crack density and length for Wf/W
Crack bridged by the fibers

## Slide 13: Hydrogen retention
D plasma exposure was applied. Bias ~95V, Flux:~2.45x1021 m-2s-1; the total fluence ~5x1025D+ m-2. During the exposure, the temperature was ~275 °C.
NRA experiments on different regions
Two points are tested, one on the region without fibers, and the other at the region with fiber/interfaces
Later, together with TDS results, these results will be helpful to understand whether we have different retention behavior for Wf/W compared to pure W
1000µm
Region with fibers
Matrix region

## Slide 14: Hydrogen retention
Lateral scan with 2.4 MeV with 1 mm step width (information depth < 3.3 µm)
Depth profiling with six different 3He energies between 690 keV and 4.5 MeV to probe the deuterium within the first 7.5 micrometer
D concentration larger in the matrix than in the fibers
Both fibers region and matrix region show higher D retention than for ITG-W maybe due to lower density and higher defect density
TDS will be done for D retention of the whole sample

## Slide 15: Thermal properties of L-Wf/W
Mainly due to different sintering density, different Wf/W show different thermal conductivity
For long fiber Wf/W, different thermal conductivity has been measured in different fiber arrangement
Sample type | Relative density
Wf/W short fiber | ~91%
Porous matrix Wf/W | ~78%
Long fiber Wf/W | ~91%

## Slide 16: Summary
The newly developed powder-metallurgical L-Wf/W has been characterized, including mechanical behavior, thermal physical behavior, erosion, retention, high heat flux tests.
the Wf/W composites could improve significantly the damage resilience compared to pure W without losing much of other properties.
HHF tests show that for the original status of Wf/W components, 15MW/m2 for flat tiles and 20MW/m2 for monoblocks could be handled
Outlook
Neutron irradiation
Fiber reinforced joining
Improving the sintering density