## Slide 1
SP F - IAP experiments. Boron plasma coatings and boronization studies.
Plama coatings – plasma parameters vs. film properties
C. Porosnicu, P. Dinca, B. Butoi, O. G. Pompilian, C. Staicu, B. Solomonea, C. P. Lungu
Approaches for surface coating with Boron by PECVD at low and high deposition rates using diborane as precursor
S. Vizireanu, G. Dinescu, D. Stoica, T. Acsente, V. Satulu, G. Dinescu, F. Dumitrache, Marius Dumitru, G. Morjan

## Slide 2
C. Porosnicu, P. Dinca, B. Butoi, O. G. Pompilian, C. Staicu, B. Solomonea, C. P. Lungu
IAP-Romania
Plama coatings – plasma parameters vs. film properties

## Slide 3: Outline
Boron coatings capabilities
Coating setups: TVA, HiPIMS, RF MS
Results form the B layers production task in 2025 under SBP4
Plasma characterisation - ion energy measurements
Prospects for studying B layers under SPF. Proposal of an experimental plan

## Slide 4
Deposition system used for obtaining B (-W)-D/H/etc. layers
Schematic description of the coating system used for B-D (Ne, N, He) layer deposition
From Be/D to B/D coating process – setups available
All the setups and experience used for Be was redirected to B
TVA Deposition system used for obtaining B (/W). layers
2024 was dedicated in setup and coating recipe development and plasma charactherisation methods

## Slide 5: Results form the B layers production taskin 2025 under SBP4
Pre-deposition. Calibration
Coating parameters
4x Si substrates
2 RF sources opperated at 100W each
Working pressure: 1x10-2mbar
Ar flow= 20sccm
D2 flow= 20 sccm
Measurements
SEM cross-section
TDS
In situ photo of the deposition
Cross-section-SEM results
TDS results (D concentration and quantity)

## Slide 6: Results form the B layers production taskin 2025 under SBP4
Thermal Treatment- 50oC- 500oC_Ramp 5oC/min
Deuterium quantity as a function of the thermal treatment
TDS result on B+D2_1050oC
Temperature (oC) | D released (at/cm2) | D released during the TT (%)
50 | 7.45E+14 | 0.01
100 | 8.25E+15 | 0.08
150 | 2.21E+16 | 0.22
200 | 2.98E+16 | 0.29
250 | 2.82E+17 | 2.76
300 | 1.06E+18 | 10.39
350 | 2.22E+18 | 21.76
400 | 3.24E+18 | 31.76
450 | 4.95E+18 | 48.53
500 | 6.45E+18 | 63.24
1050 | 1.02E+19 | 100.00
TDS measurement during Thermal Treatment
60 tungsten substrates 5x5 mm
2 RF sources opperated at 100W each
Working pressure: 1x10-2mbar
Ar flow= 20sccm
D2 flow= 20 sccm
Boron+D2(10%) 5μm
Preparation of 5x5 mm2 W samples coated with B+D2(10%)
Subject to thermal treatment post-coating
Sample holder
In situ photo of the deposition

## Slide 7: Results form the B layers production taskin 2025 under SBP4
12 tungsten substrates 10x10 mm
2 RF sources opperated at 100W each
Working pressure: 1x10-2mbar
Ar flow= 20sccm
D2 flow= 20 sccm
Sample holder
In situ photo of the deposition
Boron deposition (5μm) with and witout D
Boron deposition (100nm)
8 tungsten substrates
Eurofer φ 40 mm
2 RF sources opperated at 100W each
Working pressure: 1x10-2mbar
Ar flow= 20sccm
D2 flow= 20 sccm
Sample holder
In situ photo of the deposition
All samples were stable after the deposition (kept in vacuum).
Analisys (TDS, XRD,SEM, etc.) will be performed in April at IAP.
Samples to be sent this week (24-28 March) to the laboratories - sealed bags in vacuum, according to the matrix.

## Slide 8: XPS on tungsten-boride formation
Si2-6_340 nm | B1s | C1s | O1s | W4f | B/W
0.0 min sputtering | 15.1 | 45.3 | 32.9 | 6.7 | 2.3
0.5 min sputtering | 45.9 | - | 38.8 | 15.3 | 3.0
1.0 min sputtering | 58.3 | - | 15.8 | 25.9 | 2.3
5.0 min sputtering | 63.0 | - | 13.5 | 23.5 | 2.7
10.0 min sputtering | 63.3 | - | 13.1 | 23.6 | 2.7
Elemental relative concentrations (at. %)
Request for tungsten boride layers from Penn State University (A. Marin) under a PSU - WEST collaboration.
Samples coated by TVA – task performed.
TVA parameters variation- W/B coatings with and without boride formation
C. Porosnicu, S. Vizireanu | PWIE meeting | Prague | 24-27 March 2025 | Page 8

## Slide 9: Plasma characterisation - Ion energy measurements
RF plasma, P= 100W
BIAS voltage influence – several pressures

## Slide 10: Plasma characterisation - Ion energy measurements
RF plasma, P= 1e-02 mbar
BIAS voltage influence – several RF Powers

## Slide 11: Plasma characterisation - Ion energy measurements
RF plasma, Ion energy overview
BIAS, pressure and D/Ar ratio

## Slide 12: Plasma characterisation - Ion energy measurements
RF plasma, Ion energy overview
RF power, pressure and D/Ar ratio

## Slide 13: Plasma characterisation - Ion energy measurements
HiPIMS MP
B+Ar+D, Ar/D: 1/1
Frequency
Voltage
Pulse duration

## Slide 14: Plasma characterisation - Ion energy measurements
B+Ar+D, Ar/D: 1/1,
Bipolar HiPIMS,
Positive pulse duration varried
Positive pulse voltage varried

## Slide 15
  Different aproach than under SPB: Focus on plasma parameters instead of coating properties.
  For each set of parameters, very well defined plasma characterization
  Ionisation degree (Langmuir probe), Ion energy (IEDF), species identification (MS, OES), etc.
  Sistematic study
  Fixed plasma parameters – well characterized plasma => what will we obtain??
  stability, morphology, composition, adhesion, hardness, fuel retention
  Work plan has to be established by SP Leaders under SPB, SPC, SP D, SPX and SPF since the need of a “database of artificial B layers for physics studies: stability, fuel content, and release”
Prospects for studying B layers under SPF
Proposal of an experimental plan - Example and ideas:
Parameters to be varied: |  | 
RF-MS parameters (Input power) |  | Pressure (1e-03 – 1e-01 mbar)
HiPIMS MP and BP plasma parameters (Pulse duration and frequency, voltage for negative and positive pulse) |  | Acceleration voltage (0 to-200V for MS;-700V for TVA),
TVA parameters (voltage and current) |  | D/Ar ratio (1/20 – 1/1)

## Slide 16
S. Vizireanu, D. Stoica, T. Acsente, V. Satulu, G. Dinescu, F. Dumitrache, Marius Dumitru, G. Morjan
IAP-Romania
Approaches for surface coating with Boron by PECVD at low and high deposition rates using diborane as precursor

## Slide 17: Outline
Experimental capabilities at INFLPR for plasma and laser CVD in diborane;
    PECVD configurations used for boron deposition;
    Laser pyrolysis configuration used for preparation of B based nanoparticles;
Experimental parameters and sample labelling;
Results on Glow discharge (GD-) samples: Surface morphology;
Results on Plasma jet (J-) samples: Surface morphology;
Time stability of boron samples on Si substrates;
Boron samples deposited on W substrates;
Boron samples deposited for various temperatures;
Boron samples composition- XPS investigation;
Conclusions and future plans.

## Slide 18
Experimental capability at INFLPR
for a boronization in diborane
One essential component of the deposition system is the container in which we burn the flammable gas. At INFLPR this container was used before for burning silane SiH4 and lately for B2H6 for boron doping by laser pyrolysis [1].
Advantages: PECVD boron samples can be similar to those used in tokamak walls after boronization
Drawback: difficulties in diborane manipulation
Caution!!!
Details for handling diborane B2H6
We used a mixture of B2H6/H2 at ratio 1/10 in vacuum;
Non-used B2H6 is burning before exhausting;
Dedicated mass-flow controllers;
Diborane detection sensors.
More safety measure must be implemented
High toxicity: needs special health and safety equipment.
- TLV (Threshold Limit Values) =0.1 ppm;
immediately dangerous at 40 ppm.
Flammable gas: auto ignition in air at temperature ~ 40°C.
Special procedures must be followed to prevent hazard.
[1]. Balas M.; Dumitrache F. et al, Nanomaterials 2018, 8, 495 https://doi.org/10.3390/nano8070495
Container for
diborane burning
Air inlet
Residual gases exhausts
Vacuum pumps exhausts
Discharge chamber
Ar/B2H6 in

## Slide 19: Two PECVD configurations used for boron deposition
Set-up glass tube+ 2 parallel plate electrodes (50 mm and distance in between electrode 60 mm
Glow discharge (GD) configuration
RF plasma jet (J) configuration
Carrier gas: Ar and Precursor: H2/B2H6
Variable parameters: RF power, Flow rates, pressure, deposition time, Substrate: Si, W
Variable Working parameters:
RF power, Nozzle substrate distance, flow rates , Pressure, Deposition time, Temperature, Substrate: Si, W
Images of the plasma jet in Ar / B2H6
Gas ratio: Ar/Diborane
1000/5 (sccm)
300/5 (sccm)
Set-up steel vessel +Jet plasma source used before for PECVD of nanostructure carbon
[1]. S. Vizireanu et al, Plasma Sources Science & Technology 19, 034016, 2010.
[1]
B2H6
Ar
substrate
Carrier gas: Ar and Precursor: H2/B2H6
Ar/B2H6
injection
grounded holder and chamber
substrate

## Slide 20: Laser pyrolysis used for Boron based nanoparticles
Advantages:
pure and reproducible nano-products extremely fine and monodisperse powders (d < 30 nm);
continuous synthesis with high rate~1-10 g/h;
 B doped materials, B carbide and nitride: (Fe,Ti, Si) borides.
Specific synthesis of Boron rich NPs: B-C (O) NPs
XRD diffractogram of B4+xC-O NPs NPs /Laser pyrolysis
Reactive mixture: B2H6 / C2H2/ C2H4: 8/1/3 (sccm), Tflame=780 oC
[1]. Balas M.; Dumitrache F. et al, Nanomaterials 2018, 8, 495 https://doi.org/10.3390/nano8070495
Laser produced flame
[1]
C. Porosnicu, S. Vizireanu | PWIE meeting | Prague | 24-27 March 2025 | Page 20
Experimental method: laser pyrolysis
B2H6 was used as B precursors

## Slide 21
Preliminary Ar/B2H6 plasma jet investigation
OES investigations show the presence the Argon lines, and BH bands, Ha and Hb lines in plasma jet after introduction of 5 sccm of diborane.
Further investigations: Detailed studies follow after
I will mount a quartz window.
-OES study of He or D2/diborane plasma in various condition.
-OES study of boron films in interaction with plasma.
-Mass spectrometry study of boron films in interaction with plasma. Study of species during sputtering of boron layers in D2/H2 plasma
Plasma jet Ar/ B2H6 at 1000/5
Plasma +Optical fiber+ Optical multichannel analyzer+ acquisition
OES in plasma jet of Ar/diborane mixture

## Slide 22
a)
Pictures of samples a) GD-H and
b) GD-L on Si and W substrates
Pictures of samples a) J-H; b) J-L and c) to an intermediate Ar flow (500 sccm)
Labelling of samples:
H-samples at High Ar flow (1000 sccm)+5sccm B2H6
L-samples at Low Ar flow (300 sccm) +5sccm B2H6
Experimental parameters and samples labels
There are fixed parameters like RF power 100W, precursors kept always at the same flow values diborane: H2/B2H6 = 5 sccm
a)
a)
a)
b)
c)
Samples label | Ar [sccm] | B2H6 [sccm] | Deposition press. [mbar] | Time [min.] | Temper. Degree C
1. Set I- Samples deposits by Glow Discharge (GD-samples) |  |  |  |  | 
GD-H | 1000 | 5 | 0.7 | 10 | 
GD-L | 300 | 5 | 0.4 | 10 | 
2 Set II Samples deposits by plasma Jet (J-samples) |  |  |  |  | 
J-H | 1000 | 5 | 0.7 | 10 | 
J-L | 300 | 5 | 0.4 | 10 | 
J-H-RT | 1000 | 5 | 0.73 | 10 | 47 OC
J-H-400C | 1000 | 5 | 0.72 | 10 | 400 OC
J-H-600C | 1000 | 5 | 0.71 | 10 | 600 OC
J-H-700C | 1000 | 5 | 0.71 | 10 | 700 OC

## Slide 23: Glow discharge GD-samples: Surface morphology
GD-L, on Si from Ar/B2H6 ratio 300/5 sccm- Thickness: 40 nm
GD-H on Si in Ar/B2H6 ratio 1000/5 sccm top and cross section
SEM investigation results: top view and cross sections
Smooth films
Deposit. rate: 4 nm/min
Smooth films
Deposit. rate: 8.4 nm/min
Time:10 minutes, thickness ~84 nm

## Slide 24: Plasma jet (J) samples: Surface morphology
J-L samples are smooth and small deposition rate ~24 nm/min
SEM images of J-L samples 300/5 sccm
SEM images of J-H 1000/5 sccm top and cross section. J-H samples are rough.
Time: 30 minutes, thick 8.5 mm
Time:10 minutes, thick 4.1 mm
thick 0.24 mm
Deposition rate of J-H samples
at about 400 nm/min

## Slide 25: J-H samples. Details on morphology
Thick layer present many cracks and sponge-like morphology
At the film edges, a whitish color is observed, the film are oxidized and nanoparticles appear
case of J-H: for high Ar flows, the sample are very rough and irregular

## Slide 26
Initial SEM
SEM images of J-H sample
after 6 month.
Boron films are delaminated Exfoliation of thick layer can be observed after 6 months
Time stability: J-H sample on substrates Si
Adhesion behaviour in time (after 6 months)
of thick film deposited at (Ar/B2H6 1000/10 sccm)

## Slide 27: Boron-GD samples on W substrates
GD-L on W in Ar/B2H6 at 200/5 (layers of about 40 nm onto Si)
SEM image GD boron films onto W substrate- measured after 6 month
GD-H on W in Ar/B2H6 at 1000/5 layers (about 84 nm onto Si) :
Conformal film
No delamination
are observed
SEM image of the polished W substrate

## Slide 28: Boron-J samples on W substrates
Delamination or flakes deposition?
We have SEM only after 6 month for J-L on W
J-H pe W 1000/5: layer thickness 4 mm
cracks in the film are observed , however the layer does not completely delaminate
J-L on W 300/5: layer thickness 240 nm
SEM image Jet boron films onto W substrate- measured after 6 months

## Slide 29: Boron-J-H samples obtain for various temperatures
SEM images of J-H (Ar/B2H6 at ratio 1000/5 sccm, 100 W for 10 minutes at various temperatures.
The boron films are nanostructured at high temperatures. Nano-flakes and nanotubes are observed after 400 C and sponge like nano-structures are visible at 600 and 700 C.
Room Temp.
400 C
700 C
600 C
Room Temp.
400 C
700 C
600 C

## Slide 30: XPS investigation- survey spectra and elemental composition
Table with relative atomic concentration of elements in the samples
 | GD-H | GD-L | J-H | J-L
B 1s | 34.1 | 39.8 | 31.4 | 46.6
C 1s | 20.1 | 19.5 | 8.2 | 18.3
N 1s | 17.6 | 25.4 | 2.6 | 6.7
O 1s | 28.2 | 15.2 | 57.8 | 28.5
Boron, carbon, nitrogen and oxygen elements;
Boron is dominant element;
High Ar flow rate led to a smaller B content and samples oxidation compared to L-rate;
Lower Nitrogen and Carbon content in Jets sample;
Oxides and nitride from air leaks and exposure.

## Slide 31: XPS investigation- High resolution in C1s and B1s regions and bonding types
High resolution XPS spectra in the C1s and B1s region.
After calibration to C1s peak we observed various bond type of Carbon and Born atoms in the PECVD sample.

## Slide 32: Boron bonds type - B1s region deconvolution
Bond type | Binding en.[eV]
(B-B), | 187.2 ±0.1
(B-C); | 188.5±0.1
(B-N), | 190.8±0.1
(B-O subox.) | 192.4±0.1
B2O3 | 193.5±0.1
Deconvolution of high resolution XPS spectra in B1s region (binding energies found in the literature)

## Slide 33: XPS investigation- High resolution in B1s regions and bonding types and their percentage
Diagram with percentages of B1s components
High resolution XPS spectra in the B1s region
J-L contain metallic boron and J-H shows the most oxidized boron.
GD samples presents boron nitride bond type because of poor vacuum - mechanical pumps.

## Slide 34: Composition of boron PECVD samples for various temperatures
 | RT | 400C | 600C | 700C
B 1s | 34.9 | 34.9 | 32.6 | 34.0
C 1s | 6.1 | 13.1 | 16.7 | 14.9
N 1s | 2.7 | 6.3 | 8.2 | 13.0
O 1s | 56.4 | 45.7 | 42.5 | 38.1
Table with elemental composition from survey spectra for boron at various temperature
High resolution XPS spectra in the B1s region of samples deposited at various temperature.
Samples present oxidized boron.

## Slide 35
Time stability of composition in time
(after 6 months, substrates Si)
 | GD-H | +6 m | GD-L | +6 m | J-H | +6 m | J-L | +6 m
B 1s | 34.1 | 34.0 | 39.8 | 31.8 | 31.4 | 31.1 | 46.6 | 39.8
C 1s | 20.1 | 27.2 | 19.5 | 28.6 | 8.2 | 26.4 | 18.3 | 30.9
N 1s | 17.6 | 19.7 | 25.4 | 18.7 | 2.6 | 7.4 | 6.7 | 6.3
O 1s | 28.2 | 19.1 | 15.2 | 21.0 | 57.8 | 35.1 | 28.5 | 23.0
High resolution XPS spectra in the B1s region of boron PECVD samples measure after days and 6 months.
Table with elemental composition of initial and after 6 months of boron samples obtained by GD and plasma Jet
We can observed variation in B, C, N and O concentration.
The GD samples that presents boron nitride bonds are quite stable because are difficult to oxidize over time.
In the J-L samples that contain B-B and B-C remains almost the same shape.

## Slide 36: Conclusions
We demonstrated that we can obtain boron layers by PECVD in Ar/B2H6 mixture;
High deposition rate for jet (~400 nm/min) and low rate for glow discharge (4-8 nm/min);
Good adhesion of the thin B layers on W surface, and low adhesion on Si wafers;
For thin boron film the morphology remains stable in time (both GD-L and J-L at Low Ar);
The boron films are nanostructured at high temperatures;
The composition of boron layers deposited by PECVD from diborane contains in various concentrations B, C, N and O elements.
In the Jets samples we have metallic boron and oxide bonds type, while in the GD samples we found mostly boron nitride bonds type. The boron bonds type seems to be preserved after 6 months, except J-H samples which are quite spongy (not compact);
Modification of the composition of boron layers are observed in time.

## Slide 37: Future plans
Infrastructure:
Improving the work safety by inserting higher sensitivity diborane detectors, new system for burning the pumps exhaust;
Optimization of the deposition setups ( high vacuum pumping systems, mass flow controllers, diborane bottles – also with He, or D2, quartz windows for OES);
Development of new diborane discharge configurations relevant for fusion (we have know-how in designing of new plasma sources with injection for PECVD).
Research
Study of the boronization process (efficiency, species formed, influence of impurities) using diborane or other boron containing precursors by PECVD. Use diagnostics and characterization techniques for:
-Species formed during sputtering of boron layers in D2/H2 plasma (Optical emission spectroscopy and mass spectrometry available);
-Properties of Boron films deposited by PECVD using diborane (morphology, composition, adhesion, hardness, resilience to sputtering etc).
Identification of the critical issues in boronization, of interest for fusion technology: process, adhesion, time stability, behaviour in respect to sputtering;
Identification of the needs for PECVD preparation of thick/thin Boron layers for materials study (substrate types, pre-treatment, thickness, etc ).