## Slide 1: Update on the of 2025 tasks within SP-C
K. Schmid
E. Bernard, T. Morgan, A. Houben , A. Manhard, S. Markelj, T. Schwarz-Selinger, L. Ciupinski, M. Fellinger, D. Primezhofer, Y. Ferro, M. Lavrentiev, R. Bisson, J. Zavaznik, A. Kärcher, V. Nemanic, E. Pitthan, A. Teimane
Reporting Meeting PWIE 2024

## Slide 2: Tasks in 2025
Association | SPCToppic | Title
ISSP-UL | SP-C-1 | T-permeation experiments in 316L into gas and water
CEA | SP-C-1 | Permeation (D,T) through liquid/solid interfaces with interface characterization
CEA | SP-C-1 | Start developing W/Cu interatomic ML potentials for H transport studdies
JSI | SP-C-1 | Study of D location in tungsten single crystal containing single vacancy defects by NRA-C
MPG | SP-C-1 | Study importance of grain boundary diffusion
CEA | SP-C-1 | Test VnHk cluster binding energies from OKMC on experimental TDS and NRA spectra
JSI | SP-C-1 | D retention in displacement damaged Cu and CuCrZr
IPP_LM | SP-C-1 | TEM analysis of annealed, He implanted W. In cooperation with MPG
ÖAW | SP-C-1 | Systematic investigation of thickness dependence of re-deposited W layers on retention
VR | SP-C-1 | Systematic investigation of thickness dependence of re-deposited W layers on retention
CEA | SP-C-2 | Fluence dependence of D retention in B layers: Damage/Production vs Annealing
DIFFER | SP-C-2 | Evaluation of D/B ratio in co-deposited boron
FZJ | SP-C-2 | Formation of a-BH layers by co-depositon
FZJ | SP-C-2 | Permeation through B:D and B:W mixed layers on steel
JSI | SP-C-2 | Influence of B layer on permeation
JSI | SP-C-3 | Influence of surface He pre-implantation in EUROFER
MPG | SP-C-3 | Influence of surface He pre-implantation in EUROFER
JSI | SP-C-3 | Influence of rhenium presence on radiation damage and deuterium retention in tungsten
MPG | SP-C-3 | Influence of rhenium presence on radiation damage and deuterium retention in tungsten
FZJ | SP-C-4 | H-retention in CuCrZr and Cu
MPG | SP-C-4 | D retention in displacement damaged Cu and CuCrZr
JSI | SP-C-4 | H plasma exposure of deuterium loaded high-temperature self-ion irradiated W to study the retention in cavities in W
MPG | SP-C-4 | H plasma exposure of deuterium loaded high-temperature self-ion irradiated W to study the retention in cavities in W
23 Tasks for 108 PM

## Slide 3: Outline
Overview of topics covered in 2025
Plans for 2026/27

## Slide 4: Transport from Plasma to coolant
Coolant
Heat-sink
Armor
Plasma/gas/neutrals
Transition of different sources of D/T through different interfaces
Ions/metal: Implantation source
Gas/metal: Sievert‘s law
Atoms/metal: Complex energy landscape
Metal/metal: Thermodyn. Equil.
Metal/water: Henry‘s law vs. Sievert‘s law?
Green model & parameters available
Yellow model is there but parameters are „unclear“
Red: Not sure about model or parameters
?Permeation barrier?

## Slide 5: Transport from Plasma to coolant
Coolant
Heat-sink
Sievert’s law
Henry’s law
Metal/Water equilibrium expectations: Solute concentration, Pressures
[1]
[3]
H2 in H2O
[1] Aiello FED 41 (2002) 872
[2] Chan JNM 123 (1984) 935
[3] H2 in H2O from NIST
T = 600K
During permeation depends on interface kinetics
[2]
Expected from equilibrium with PbLi
T = 600K

## Slide 6: Transport from Plasma to coolant
Metal/Water interface
We need an estimate on possible surface limits between metal & water
 See talk by A. S. Teimane
ISSP-UL | SP-C-1 | T-permeation experiments in 316L into gas and water
CEA | SP-C-1 | Permeation (D,T) through liquid/solid interfaces with interface characterization

## Slide 7: T retention Release from B layers
Ultimate goal: Scaling law for D/B like G. De Temmerman Nucl. Fusion 48 (2008) 075008
Need to co-deposit B and D not implant into B layers
Vary temperature, deposition rate and energy
a-BD layers differ greatly depending on deposition parameters: A. Annen Thin Solid Films 300 (1997) p.101
Example D/Be

## Slide 8: T retention Release from B layers
Ultimate goal is a scaling for the D/B ratio similar to what was available for Be
 For this we need co-deposited layer and no pre-deposited B layers that are then exposed to plasma
Co-deposit B and D in a linear plasma device varying:
Deposition rate (vary upstream B source)
Temperature (heated catcher sample)
upstream B source:
Di-borane gas ( challenging safety precautions necessary)
Erode a junk of B by the plasma ( homogeneity of deposition? May be a feature?)
...
[1]
[1] A. Annen et al. Journal of Non-Crystalline Solids 209 (1997) 240–246
Particle energy (bias)
 This produces very different layers

## Slide 9: T retention Release from B layers
Ultimate goal is a scaling for the D/B ratio similar to what was available for Be
Don’t just focus on D content
B density determines layer properties
Particle energy is a key input that needs to be known
(Difficult to set for magnetrons)
CEA | SP-C-2 | Fluence dependence of D retention in B layers: Damage/Production vs Annealing
DIFFER | SP-C-2 | Evaluation of D/B ratio in co-deposited boron
FZJ | SP-C-2 | Formation of a-BH layers by co-depositon
FZJ | SP-C-2 | Permeation through B:D and B:W mixed layers on steel
JSI | SP-C-2 | Influence of B layer on permeation (moved from 2024)

## Slide 10: Retention in Cu and CuCrZr
R. Delaporte-Mathurin et al, Nucl. Fusion 64 (2024) 026003
W-monoblock divertor concept is based on a Cu, CuCrZr heatsink
Very little data is available on trapping in Cu or CuCrZr
NO data is available on trapping in displacement damaged Cu or CuCrZr

## Slide 11: Retention in Cu and CuCrZr
CEA | SP-C-1 | Start developing W/Cu interatomic ML potentials for H transport studies
FZJ | SP-C-4 | H-retention in CuCrZr and Cu
MPG | SP-C-4 | D retention in displacement damaged Cu and CuCrZr
JSI | SP-C-1 | D retention in displacement damaged Cu and CuCrZr
What’s available in literature?
Nothing on displacement damaged Cu, Cu-alloys
Mainly permeation measurements  insufficient for predicting retention
I could only find very few TDS measurements
 See talk by Y. Ferro

## Slide 12: Retention in Cu and CuCrZr
H.-D. Liu, et al, Nuclear Materials and Energy 23 (2020) 100755
Cu
Literature data on undamaged Cu and CuCrZr suggest release up to very high temperatures
Retention in CuCrZr >> Cu
W-comparison
Cu releases at higher T than damaged W!?!

## Slide 13: Retention in Cu and CuCrZr
Literature data on undamaged Cu and CuCrZr suggest release up to very high temperatures
Retention in CuCrZr >> Cu
These are TDS from gas loaded membranes (thickness ~1/10 mm)
 Is the high release temperature a transport artefact?
H.-S. Zhou et al. / Journal of Nuclear Materials 493 (2017) 398

## Slide 14: Retention in Cu and CuCrZr
These are TDS from gas loaded membranes  Is the high release temperature a transport artefact?
Qualitative example: W foil
Peaks do shift with thickness
But mainly it broadens towards high-T
High release temperature could also be surface effect?

## Slide 15: Near surface energy landscape
The uptake of H into metals is described by the Pick-Sonnenberg model J. Nucl. Mat. 131 (1985) p. 208
K. Schmid Nucl. Fusion 61 (2021) 086008
 A surface limit for release can shift TDS spectra
Energy landscape can kinetically hinder D-release
Example: EUROFER

## Slide 16: Near surface energy landscape
Material parameters are model dependent: Example surface model for EUROFER [1]
Simultaneous fit of all TDS spectra
Explains lack of gas loading at 1Pa
Explains time depenence of plasma loading:
  Damaged 48h vs un-damaged 143h
Not perfect but:
Follows Sievert‘s law in equilibrium!
Same trap settings
Same surface settings
[1] K. Schmid, NME 36 (2023) 101494
Complex kinetic surface model „Pick & Sonneberg“ needed to explain experiments
ETrap = 1.1, 0.9 eV

## Slide 17: Near surface energy landscape
Material parameters are model dependent: Example surface model for EUROFER [1]
Removing surface model:
[1] K. Schmid, NME 36 (2023) 101494
Swap surface model with simple diffusion limit and try to fit data with trapping only:
Needs different de-trapping energies
ETrap = 1.3, 1.1 eV
Can‘t simultaneously fit all experiements
Onset slope too flat
Trapping parameters depend on surface model assumptions

## Slide 18: Modelling needs
Predictions for ITER and demo require diffusion trapping parameters including surface models
Experiments needed:
Gas vs ions/plasma vs. atom loading  Probe surface model
Depth profiles and TDS spectra
Experiments need to be modelled by diffusion trapping codes
Otherwise, no predictions for ITER/DEMO
Surface model was not too important for W
…but is very important for steels and Cu-alloys
See talk by S. Markelj

## Slide 19: Influence of transmutation products He, Re
Taken from 2024 report by S. Mareklj
Similar to W, He implantation in EUROFER also limits uptake
What about high temperatures?
Apart for He also Re is produces in W by n-irradiation
Effect of Re on displacement damage creation: See talk by M. Zibrov
JSI | SP-C-3 | Influence of surface He pre-implantation in EUROFER
MPG | SP-C-3 | Influence of surface He pre-implantation in EUROFER
JSI | SP-C-3 | Influence of Re presence on radiation damage and deuterium retention in tungsten
MPG | SP-C-3 | Influence of Re presence on radiation damage and deuterium retention in tungsten

## Slide 20: High temperature effects and transmutation products
Displacement damage at high temperatures leads to formation of extended defects
Presence of He or Re affects defect formation and annealing at high temperature
Need to continue high temperature experiments
Extend the scope from W to steels and Cu-alloys
JSI | SP-C-4 | H plasma exposure of deuterium loaded high-temperature self-ion irradiated W to study the retention in cavities in W
MPG | SP-C-4 | H plasma exposure of deuterium loaded high-temperature self-ion irradiated W to study the retention in cavities in W

## Slide 21: Planning
Plans for the 2026/27 programme

## Slide 22: Planning
Trapping- transport- and surface limit parameters for ITER materials Cu, CuCrZr, 316L and W.
Data lacking for displacement damaged Cu and Cu alloys
Needs TDS and depth profiles to pin down trapping parameters
Existing data is only partially interpreted by modelling
   Basically, unusable for ITER predictions
   Experiments + proper diffusion trapping modelling of results to obtain parameters

## Slide 23: Planning
Retention in co-deposits: D/B, D/"Steel", D/W etc. D/X ratios
Particle energy hard to “guess” in Magnetrons
   Try to produce co-deposits ideally in linear machines
Diagnose not just D but also B, W, Steel etc. areal densities
Typically, D/X depends on energy, temperature and growth rate

## Slide 24: Planning
Influence of Neutron damage and the presence of transmutation products
Focus is on high temperatures
Synergies between He and Re and displacement damage.
Formation of “extended defects” (e.g. Bubbles etc.)

## Slide 25: Planning
Permeation “reduction methods”
Reduce uptake by e.g. porosity in VPS-W, He-pre-implantation
Permeation barriers
A lot has been done on ceramic barriers, don’t want to repeat that.
   Try metallic multilayers or nitrides which are mechanically less challenging