## Slide 1
Sputtering of boron layers in PSI-2

## Slide 2
Mounted in PSI-2 sample holder
W-targets with boron layer – fabrication
Mo mask
W
W
W
W
W
W
W
B
SEM (FIB)
B
Pt
W
RF Ar discharge + B target, ~ 6 h deposition
~115 nm B layer on polished and annealed W PSI-2 substrates

## Slide 3
Tungsten
~ 115 nm Boron
,
Molybdenum mask
BD formation
Physical sputtering of B
Dissociation
Resonant BD band spectrum at 432.8 nm
D plasma
Chemical sputtering
Molybdenum mask
Resonant B I lines at 250 nm
Erosion channels of boron at PSI-2

## Slide 4
Physical sputtering of B
Only B I 2s22p
eV
 Population in other states  line emission
Grotrian diagram of B I
Level << 11 eV for sufficiently large
B I spectroscopy: line selection
Resonant line with the longest wavelength:
UV 250 nm!

## Slide 5
Plasma parameters and optical setup
Diagnostics
Deuteron flux density
Deuteron impact energy
depends on the floating potential
Pure deuterium plasma:
Czerny-Turner: UV
Littrow: VIS

## Slide 6
UV-Optics
PSI-2/ Hollow cathode lamp(HCL)
*
UV
holographic grating
Ratio must be 4:2
Calibration of the imaging spectrometer

## Slide 7
Spectroscopic time-of-flight measurements: B I 250 nm
Plasma on
B I 250 nm lines
Edge @ pos 2123 mm and 450 nm
Backlight illumination
Spectrum detect by the imaging spectromter @ 80 V Bias

## Slide 8
Erosion monitoring using B I 250 nm
Partial erosion: 70 s
Complete erosion ~ 20 min
Observations
Line intensity grows when increasing the bias
Experiments reproduce nicely (green, purple)
Sharp decay of line intensity after ~150 s
Weak B I signal remains even after 20 minutes!

## Slide 9
Plasma on
Plasma off
Plasma off
Avantes USB
Channel 4:
679 nm – 889 nm
Without boron
Measuring O I lines
LOS B

## Slide 10
79 grooves/mm
1200 grooves/mm
LOS B
Molecular spectrum of BD: resonant @ 432.8 nm

## Slide 11
Considering only
Blue: First 4min (Erosion of Boron layer)
Red: Last 4min (No Boron layer)
79 grooves/mm
Molecular spectrum of BD: resonant @ 432.8 nm
Molecular constants from
Main isotopes of boron:
: 20%
: 80%
Accurate constants for
Data on higher-order centrifugal terms missing for
Rotational temperature is high

## Slide 12
Considering only
Blue: First 222 s (Erosion of Boron layer)
Red: Last 222 s (No Boron layer)
1200 grooves/mm
Measurement of rotational temperature
Molecular spectrum of BD: resonant @ 432.8 nm
Spectral order m=2
10 s integration time gives sufficient BD signal!
Rotational temperature differs by less than 3% compared to

## Slide 13
Time-resolved fit
Rotational temperature
Molecular spectrum of BD: resonant @ 432.8 nm

## Slide 14
Erosion rates of thin boron layers in PSI-2
Behrisch 2006; TRIM.SP (binary collision approximation)
Hechtl 1992; graphite samples with plasma sprayed boron
mass loss
PSI-2 2024; Magnetron sputter deposited boron
Focused ion beam + Secondary electron microscopy
PSI-2 2024
SEM (FIB)
@ Pos. 3
SEM (FIB)
B
Pt
W
After PSI-2 plasma
Before PSI-2 plasma

## Slide 15
Conclusion
Boron layers with ~ 115 nm thickness erode within approx. 150 s at PSI-2
Erosion rates agree well with those from Hechtl 1992
Atomic (UV) and molecular (VIS) spectroscopy with time resolution of 10 s achieved!
PSI-2 2024

## Slide 16
Outlook
Molecular spectroscopy:
Influence of target temperature on BD signal + rotational temperature
E.g. B HCL, BH Q-branch
Atomic spectroscopy:
Upgrade Littrow to UV – first spectra of a B HCL
 Information on the velocity & angular distribution function
Attempt measuring the NIR line at 1166 nm
Simulation:
BH and BD are distinguishable
BH and BD spectra during isotope exchange
Can we distinguish the isotopes of boron @ PSI-2?

## Slide 17
Particle flux density of boron:
Mass flux density of boron:
Density of solid boron ~
Erosion rate:
Behrisch @ 100 eV*:
Sputter yield 0.0
100 eV D -> B: 0.0321
Initial estimate of the time scale
A Simple Sputter Yield Calculator
IAP/TU Wien Surface Physics Group
~ 40 s for 100 nm!
*the intent is to expose at the floating potential (~40 V). However we might have or other impurities within the plasma, so we chose 100 eV for the first estimate!

## Slide 18
LHD: T. Kawate et al 2022 Nucl. Fusion 62 126052
S Brezinsek et al 2007 Phys. Scr. 2007 40
TEXTOR
Molecular spectroscopy: BD

## Slide 19
Boron signal appears even after ~ 12min
Potentially due to redeposition!

## Slide 20
Ground state
Issue: only is reliable
Boltzmann distribution & Hönl London factors
(E.g. Eqs. (IV,81 -83) Herzberg, Spectra of Diatomic molecules)
P-branch
R-branch
Q-branch

## Slide 21
Chromatic abberation
W HCL, backlight illumination
UV mirror

## Slide 22
Example BD in magnetron plasma