## Slide 1: Transmission Electron Microscopy of He ion implanted W-based HEA at IJCLab Stéphanie Jublot-Leclerc, Antoine Combrisson, Florian Pallier, Aurélie Gentils Université Paris-Saclay, CNRS/IN2P3, IJCLab, Orsay, France 10th September, 2025
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001
2024-2025
Contact: aurelie.gentils@ijclab.in2p3.fr

## Slide 2: Updated status on HerHEA work at CNRS-IJCLab (10th Sept. 2025)
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
Cutting of the bulk as-fabricated material
subcontractor in France for EDM cutting
Material fabrication at VTT
Materials sent to CNRS-CEMHTI and UHEL for ex situ ion implantation and characterizations
Available material(s) to be studied
W, W-Ta, W-Mo, W-V
Surface mechanical polishing
SEM-EDX characterization
(to be done ?)
Electrical Discharge Machining
3 mm diameter discs
squares
Other materials from Portugal
W-Ta-V, W-Ta-Mo
half discs
Polishing performed on W, W-V, W-Ta and the ternary alloys
Mirror-polished samples (mid / end August)

## Slide 3: Updated status on HerHEA work at CNRS-IJCLab (10th Sept. 2025)
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
100 keV He ion implantation performed yesterday !
500°C (temperature of the samples)
Fluence 1x1017 cm-2
Orsay
https://mosaic.ijclab.in2p3.fr
Should be enough He to see bubbles in W
He bubbles observed in W by TEM starting 5x1015 cm-2 fluence,
see F. Luo et al, Fusion Engineering and Design 125 (2017) 463
dx.doi.org/10.1016/j.fusengdes.2017.04.014
Implantation sample holder
SRIM calculations using average Ed = 44 eV, see J. Byggmästar, F. Djurabekova, and K. Nordlund, Phys. Rev. Materials 8 (2024) 115406, https://doi.org/10.1103/PhysRevMaterials.8.115406

## Slide 4: Updated status on HerHEA work at CNRS-IJCLab (10th Sept. 2025)
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
Cutting of the bulk as-fabricated material
subcontractor in France for EDM cutting
TEM thin foils preparation
by FIB (scheduled end Sept.)
Material fabrication at VTT
Observation if any He bubbles are seen
Transmission Electron Microscopy
ex situ
(in October)
Selection of the He ion implantation conditions
High T°C (500°C), one high fluence (1x1017 cm-2)
Energy 100 keV
Analyse the experimental data
Interpretation / Comparison with other HerHEA results / Publication
M3.1 In situ TEM experiments performed (Links to D3.1) June 2025  will be delayed to Nov. ?
Materials sent to CNRS-CEMHTI and UHEL for ex situ ion implantation and characterizations
Surface mechanical polishing (done)
SEM-EDX characterization
to be done ?
Electrical Discharge Machining
3 mm diameter discs
squares
half discs
Other materials from Portugal
W-Ta-V, W-Ta-Mo
Available material(s) to be studied
W, W-Ta, W-Mo, W-V
Orsay
https://mosaic.ijclab.in2p3.fr