## Slide 1: Overview of UKAEA results under SPE: post-DTE3 component removal and distribution
Y. Zayachuk, I. Jepu, A. Widdowson, J. Likonen, JET contributors
WP PWIE review meeting
FZJ, Germany| 17-21.11.2025

## Slide 2: JET ILW
Y. Zayachuk | HWS-17 | Chamonix | 20.05.2024 | Page 2
Bulk beryllium (Be)
Castellated structure
Bulk tungsten (W)
Lamellar structure
25 µm tungsten (W) coating on carbon-fibre composite (CFC) tile
DT campaigns:
Tritium retention
Neutron-induced activation

## Slide 3: Deuterium-tritium plasma campaigns
DT campaigns:
  DTE2 – 2021.
  DTE3 – 2023.
Components removed using remote handling (MASCOT) at the end of 2024.
Following removal components stored in the ISO container in the torus hall.
Components transferred to Beryllium Handling Facility (BeHF).

## Slide 4: Deuterium-tritium plasma campaigns
Components of interest for PWIE-SPE (more were removed for internal/JDR (JET Decomissioning and Repurposing) analysis & waste characterisation):
W-CFC tiles: poloidal set (21 tiles with PWIE-SPE).
W lamellae: 3 LBSRP modules (36 lamellae, 12 W Langmuir probes with PWIE-SPE interest).
Be tiles: WPL, IWGL, UDP (20 tiles).
Inner wall protection: tiles and inserts.
Diagnostics: mirrors and mirror cassettes; sticking monitors; dust collectors; QMB covers & crystals; rotating collectors.

## Slide 5: Handling of components
During 2025 components processed in BeHF:
  Disassembled, photographed, weighed and boxed.
Gamma dose rate measurements taken of representative components at different distances (contact, 30 cm, 100 cm) using Ludlum gamma-detector  indicative of activation.
As part of JDR activities, samples of selected components were removed using band saw or coring drill, to be used in pyrolysis measurements  indicative of tritium content.
Off-gas measurements of selected components  indicative of tritium content.
Boxed components stored in BeHF – awaiting shipment.

## Slide 6: Handling of components
Activities performed in pressurized suits
Components handled in isolator (glove box)
Some “dirty” cutting done in-house for waste characterisation & detritiation studies

## Slide 7: Neutron activation analysis
Neutron-induced activation:
  Calculated using FISPACT-II neutronics code  for scientific and disposal purposes.
  For each material – plasma-facing and structural  tungsten, beryllium, CFC, TZM, Nimonic, Inconel.
  Time dependence of isotopic fingerprint  after final plasma.
Example of isotope fingerprint for W (LBSRP):
Assumed initial isotopic composition:
Assumed neutron spectra (DD and DT):

## Slide 8: Neutron activation analysis
Example of isotope fingerprint for W (LBSRP):
W activation dominated by W181.
Some tritium generated by transmutation.
(~100 kBq/lamella@2 years – total).
Activity dominated by tritium introduced by plasma-wall interaction (implantation and deposition).
(~570 MBq/lamella (see slide 10)).

## Slide 9: Results of pyrolysis
Pyrolysis performed at the Tritium Analysis Laboratory (TAL) at UKAEA by JDR team.
PFC Type | Mass of sample (g) | Sample inventory (MBq) | Inventory/g (MBq/g)
Be | 0.891 | 60.81 | 68.24
W | 8.37 | 64.92 | 7.76
W-CFC | 4.91 | 58.01 | 11.82

## Slide 10: Total tritium content – extrapolation
Tritium content resulting from activation is small relative to tritium content resulting from plasma-wall interaction (implantation and co-deposition).
It can be assumed that majority of tritium is present in the vicinity of the plasma-exposed surfaces.
To obtain full tritium content in the component (lamella/tile) it would be incorrect to extrapolate the pyrolysis results to the entire volume of the component.
Near-surface regions, where pyrolysis samples are taken from, contain majority of total tritium content  pyrolysis results should be extrapolated only to the area of plasma-exposed surface of a component.

## Slide 11: Total tritium content – extrapolation
Example – LBSRP W lamella:
Full lamellae length 60 mm.
Length of pyrolysis sample 7.25 mm → 8.28 top surface samples in a single lamella.
Full inventory of pyrolysis sample 65 MBq.
Inventory of full lamella (extrapolated to entire top surface 8.28 × 65 MBq = 537.58 MBq/Stack B W lamella

## Slide 12: Total tritium content – extrapolation
Example – LBSRP W lamella (continued):
If specific inventory in the bulk of the tile is 3% of surface specific inventory:
Specific inventory from pyrolysis = 7.8 MBq/g × 0.03 = 0.23 MBq/g for the remaining bulk
Mass of bulk removing top surface (10 mm depth) = 200 g (nominal mass of W lamella) – 70 g (mass of top lamella) ≈ 130 g
Total inventory of a W lamella component
= 537.6 MBq + 0.24 MBq/g × 130g
≈ 567.8 MBq / full W lamella
Y. Torikai et al, PFMC20

## Slide 13: Total tritium content – extrapolation
Similar calculations were made for different types of PFCs where pyrolysis was performed:
PFC Type | Based on pyrolysis of this component: | Total inventory, GBq/tile
Be | WPL 8D4 | 18.16
W | 15W RHB | 0.57
W-CFC | 2ON G8A | 9.43
Seemingly high activity associated with Be tiles.
Sample for pyrolysis likely to originate from deposition-dominated zone  potential overestimation, as it is not representative of the entirety of the tile.
Potentially also indicates a relatively lower efficiency of main-chamber clean-up.

## Slide 14: Tritium retention predictions
Tritium retention calculations based on the injected tritium content.
Total tritium injected – 7.27E+25 at / 363.5 g.
Fuel retention ratios established in post-mortem analysis of components removed in ILW1-3 campaigns.
Based on ILW results (in deuterium plasmas), it was established that long-term retention constitutes ~2-4% of injected deuterium  distributed across different components (Brezinsek et al NF 2013).
This can be further broken down by individual tiles using distribution from post mortem analysis.
~7-14 g of tritium retained.
Inner divertor
Remote divertor
Divertor
bulk tungsten
Main chamber
Be limiters
Main chamber
Recessed wall
Be castellation gaps
Outer divertor
A. Widdowson et al, Nuclear Fusion 57 (2017) 086045

## Slide 15: Tritium retention predictions
Individual tiles by type | T atoms per tile | T atoms/cm2 | Bq/cm2 | Pyrolysis of sample (Bq) | Approximate areal activity (Bq/cm2)
Tile 0/HFGC | 2.28E+21 | 1.28E+19 | 2.28E+10 |  | 
Tile 1 | 2.42E+21 | 1.05E+19 | 1.88E+10 |  | 
Tile 3 | 2.45E+21 | 5.34E+18 | 9.52E+09 |  | 
Tile 4 | 1.10E+21 | 4.06E+18 | 7.23E+09 |  | 
Tile 6 | 6.76E+20 | 2.34E+18 | 4.17E+09 |  | 
Tile 7 | 1.75E+21 | 3.21E+18 | 5.72E+09 |  | 
Tile 8 | 4.72E+20 | 1.59E+18 | 2.83E+09 | 5.80E+07 | 5.80E+07
Tile 5 Tungsten lamella | 9.43E+17 | 2.62E+17 | 4.67E+08 | 6.39E+07 | 6.39E+07
IWGL (5 tile pieces) | 2.19E+20 | 8.75E+17 | 1.56E+09 |  | 
OPL (7 tile pieces) | 5.35E+20 | 1.27E+18 | 2.27E+09 | 6.08E+07 | 6.08E+07
IWC | 3.24E+20 | 1.17E+18 | 2.51E+09 |  | 
DP | 1.08E+20 | 9.16E+17 | 8.75E+08 |  | 
Breakdown of tritium retention by component:
Predicted retention at end DTE3 2% in-vessel & distribution based on post mortem analysis
Pyrolysis of samples at UKAEA by JET JDR team

## Slide 16: Tritium retention predictions
Individual tiles by type | Bq/cm2 (2% retention) | Bq/cm2 (pyrolysis) | Ratio Prediction/pyrolysis
Tile 8 | 2.83E+09 | 5.80E+07 | 48.8
Tile 5 Tungsten lamella | 4.67E+08 | 6.39E+07 | 7.3
OPL (7 tile pieces) | 2.27E+09 | 6.08E+07 | 37.3
Predictions consistently higher than indications of pyrolysis.
Certain discrepancy in how much higher – differs from component to component.
At least two mechanisms for this can be identified:
Clean-up.
Loss of tritium on venting (~0.4 g for whole vessel measured).

## Slide 17: Tritium retention predictions
Following the end of DTE3, cleaning operations were performed.
LID-QMS was used to monitor the decrease of tritium content with time.
Measurements of 14 MeV neutron production were used in parallel to monitor the decrease of tritium content with time.
After vessel baking
End of T clean-up
End of JET ops
End of DTE3
Vessel baking
320C
End of T clean-up
End of JET plasma ops
Factor ~5

## Slide 18: Tritium retention predictions
Clean-up  decrease of tritium signal BUT potential discrepancy between the tritium reduction rates established by LID-QMS and neutron measurements.
LID-QMS ~factor 5 to 1 order of magnitude; neutron measurements ~2 orders of magnitude.
Possibly due to the difference in the location of measurement: LID-QMS – directly at the wall, neutrons – in the core plasma.
Regardless  tritium content at the end of ops lower by at least factor of ~5 then what accounting for only injected tritium would predict.
LID-QMS shows reduction in tritium retention ~ factor 5
14 MeV neutrons in plasma reduced by 2 orders of magnitude

## Slide 19: Tritium retention predictions
Preliminary summary:
At end of DTE3: 2% - 4% retention (of injected T) = 7.3 - 14.5 g T [Post mortem prediction without cleaning]
At end of T clean-up: 0.4% – 0.8% retention (of injected T) = 1.45 – 2.9 g T [factor 5 reduction in surface retention from LID-QMS]
Release on venting:
DTE1: ~33% of remaining fuel (6 g) released on venting  2 g released on venting.
In DTE3 this corresponds to 0.48 – 0.96 g T released on venting.
Preliminary data of release on venting ~ 0.4 g T  roughly consistent.
Remaining T amount ~ 0.98 – 1.96 g T remaining  retention 0.27% - 0.54% of injected fuel
Analysis ongoing
Individual tiles by type | Bq/cm2 (0.27% - 0.54% retention on removal) | Bq/cm2 (pyrolysis) | Ratio Prediction/pyrolysis
Tile 8 | 3.82 - 7.64 E+08 | 5.80E+07 | 6.5-13.0
Tile 5 Tungsten lamella | 6.30 - 12.6E+07 | 6.39E+07 | 0.99-1.98
OPL (7 tile pieces) | 3.07 - 6.14E+08 | 6.08E+07 | 5.0-10.1

## Slide 20: Plans for studies on W lamellae at UKAEA
First studies at UKAEA – microscopy on W lamellae.
  Effects of He plasma interaction.
  LIBS craters on W lamellae.
  Microstructural changes.
3 lamellae selected.
Optical microscopy; SEM surface imaging; FIB cross-sectioning.
24
1
D
C
B
A
RH
LH
14W-LBSRP
UKAEA
3 lamellae
14W LBSRP LH
  A21  MAP-LAB  MRF
  B21  MAP-LAB  MRF
  D12  MRF

## Slide 21: Plans for studies on W lamellae at UKAEA
Effects of He plasma interaction.
He plasma campaign (2022)  to “simulate” the then-planned He plasma campaign at ITER.
He fuzz observed in lab experiments  will it form in the tokamak?
A
B
C
D
LBSRP 14BN
No evidence of fuzz formation found during in-vessel imaging (even though conditions favourable, based on the results from linear plasma devices).
Systematic feature on stack C
Origin unknown
Imaging artifact
Approximate strike point position (highest heat flux)

## Slide 22: Plans for studies on W lamellae at UKAEA
Some evidence of surface modification found in the infrared and visible camera images.
Stack B – He strike point – appears to not be affected.
Stack A – private flux region – appears to form some features.
High-resolution surface SEM combined with FIB surface cross-sectioning  will there be any evidence for onset of fuzz formation?
Lamellae from stacks A and B to be investigated.
A. Hakola et al, Nucl. Fusion 64 (2024) 096022

## Slide 23: Plans for studies on W lamellae at UKAEA
LIBS craters on W lamellae.
Plans for experiments:
High-resolution optical imaging of craters  depth measurements.
High-resolution SEM imaging of craters.
FIB cross-sectioning of craters  depth measurements and studies of microstructural / morphological changes in the sub-surface region surrounding the craters.
Microstructural changes.
W lamella from stack D  strike point during DTE operations  high surface temperature and ion flux.
SEM and FIB to study microstructural effects (recrystallization?)

## Slide 24: Plans for shipments of W lamellae
IAP
16 lamellae
14N LBSRP RH
  A14/A15
  B3/B4, B14/B15, B23/B24
  C3/C4,C14/C15, C23/C24
  D14/D15
Distribute samples for analysis
Cutting plan in preparation
Assumed T content:
Max ~570 MBq / lamella
Even whole shipment of 16 lamella <40 GBq  excepted
2013-14 & 2018-23
2018-2023
2011-12 & 2018-23
24
1
RH
LH
D
C
B
A
14N-LBSRP

## Slide 25: Plans for shipments of W lamellae
FZJ
1 lamella
14W LBSRP LH
  B12
IST
1 lamella for IBA
14W LBSRP LH
  C12  VTT (LIBS)  FZJ (LID-QMS)
VTT
2 lamellae for LIBS (Can be in 2026)
14W LBSRP LH
  A12
  D12 (after analysis at UKAEA)  FZJ (LID-QMS)
24
1
D
C
B
A
RH
LH
2011-2023
2011-2023 & LIBS
14W-LBSRP

## Slide 26: Plans for studies on the RE-induced damage on Be limiters
7
8
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
c)
d)
3
4
5
6
7
8
1
2
Removed in the 2024 intervention
3X14 & 8Z14
Toroidal limiter damage map due to RE impact
3X14 damage part of single day of ops (18th Dec 23)
8Z14 damage part of multiple RE damages
(6th , 14th & 18th single RE shot Dec 2023)
3X14
8Z14

## Slide 27: Plans for studies on the RE-induced damage on Be limiters
7
8
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
c)
d)
3
4
5
6
7
8
1
2
Removed in the 2024 intervention
3X14 & 8Z14
Toroidal limiter damage map due to RE impact
3X14
8Z14
Near term (UKAEA):
High-resolution optical imaging of full tiles;
High-resolution optical imaging of LIBS craters;
Laser 3D profiling →;
Toroidal and poloidal assessments of LIBS spots for material composition and fuel retention (with the help of LIBS team).
Long term:
Cutting @ IAP;
Assessment of melt in gaps;
Fuel retention in and outside the RE damaged area (IBA/TDS)
SAMPLE
ONLY

## Slide 28: Plans for shipments of W-CFC divertor tiles
W-CFC tiles
6
7
0
3
4
5
8
1
HFGC: LH14W 2011-2023
HFGC: RH14W 2011-2023
HFGC: LH14N 2018-2023
HFGC: RH14N 2018-2023
LIBS points
LID-QMS points
Chosen tiles for SPE

## Slide 29: Plans for shipments of W-CFC divertor tiles
Tritium content is estimated based on pyrolysis results from tile 8 and relative distribution between the tiles established with ILW data.
7
0
3
5
8
1
 | VTT (coring) | Estimated tritium content, GBq/tile
2IW G1B (2010-2023) | X | 48.2
14N HFGC RH​ (2018-2023) | X | 45.6
14 IW G1A (2018-2023) | X | 48.2
14 BW G4A (2010-2023) | X | 22.1
LIBS+LID-QMS
LIBS
LID-QMS
Above the excepted limit of 40 GBq/shipment
 Type A container likely needed.

## Slide 30: Summary of 2025 and outlook
Post-DTE component removal completed.
Processing of assemblies completed  plasma-facing components separated and boxed.
First batch of shipments of W lamellae imminent.
Samples packed and shipment requirements being assessed by UKAEA.
First results of microscopy on W lamella imminent (UKAEA).
Approval of transfer of first samples from DTE3 to UKAEA Materials Research Facility obtained.
Analysis planned near-term.
Shipments of W-CFC tiles in preparation for 2026.

## Slide 31
SUPPORT SLIDES

## Slide 32: Total tritium content – extrapolation to all divertor tile types
Tile type | Location | Material | Tritium Bq/tile | Specific activity Tritium Bq/g
Tile 0/HFGC | Divertor | W-CFC | 4.56E+10 | 3.50E+07
Tile 1 | Divertor | W-CFC | 4.82E+10 | 1.72E+07
Tile 3 | Divertor | W-CFC | 4.88E+10 | 1.16E+07
Tile 4 | Divertor | W-CFC | 2.21E+10 | 1.05E+07
Tile 6 | Divertor | W-CFC | 1.35E+10 | 6.42E+06
Tile 7 | Divertor | W-CFC | 3.49E+10 | 7.11E+06
Tile 8 | Divertor | W-CFC | 9.43E+09 | 2.69E+06
Tile 5 lamella | Divertor | Tungsten | 5.67E+08 | 2.70E+06
“Excepted” likely for W lamellae
Package limits:
Type A total T = 40 x1012 Bq
Excepted package T
< 4 x 1010 Bq
Type A for W-CFC tile transport for cutting
Extrapolation to all divertor tile types from pyrolysis measurements of JET tile samples
Order of magnitude lower inventory than previously estimated from worst case retention without cleaning and venting taken into account
Prioritising W-lamellae and W-CFC  Be tiles still to be assessed

## Slide 33: Total tritium content – old predictions
7.18x1025 T atoms injected between 2020-2023
0.19% retention fraction
 | Whole tiles |  |  | Samples | 
Tile type | T atoms/tile | Bq/tile | Specific activity (Bq/g) | Bq/sample | Specific activity (Bq/g)
Tile 0/HFGC | 2.14E+20 | 4.00E+11 | 3.08E+08 | 6.00E+09 | 1.07E+09
Tile 1 | 2.27E+20 | 5.00E+11 | 1.79E+08 | 5.00E+09 | 8.82E+08
Tile 3 | 2.30E+20 | 5.00E+11 | 1.19E+08 | 3.00E+09 | 4.47E+08
Tile 4 | 1.04E+20 | 2.00E+11 | 9.52E+07 | 2.00E+09 | 3.40E+08
Tile 6 | 6.35E+19 | 2.00E+11 | 9.52E+07 | 1.00E+09 | 1.96E+08
Tile 7 | 1.64E+20 | 3.00E+11 | 6.12E+07 | 2.00E+09 | 2.69E+08
Tile 8 | 4.44E+19 | 8.00E+10 | 2.29E+07 | 7.00E+08 | 1.33E+08
Tile 5 Tungsten lamella | 8.86E+16 | 2.00E+08 | 1.00E+06 | 4.00E+07 | 2.31E+06
IWGL (5 tile pieces) | 2.05E+19 | 4.00E+10 | 1.60E+07 | 3.00E+08 | 7.32E+07
OPL (7 tile pieces) | 5.03E+19 | 9.00E+10 | 3.10E+07 | 4.00E+08 | 1.07E+08
IWC | 3.04E+19 | 6.00E+10 | 4.29E+07 | 6.00E+08 | 5.89E+07
DP | 1.02E+19 | 2.00E+10 | 2.86E+07 | 2.00E+08 | 6.35E+07
“Excepted” likely for W lamellae
Package limits:
Type A total T = 40 x1012 Bq
Excepted package T
< 4 x 1010 Bq
Type A for W-CFC tile transport for cutting
Type A/Excepted border for Be tiles