## Slide 1
R&D issues for PWIE: Full Tungsten Walls and Boronization in ITER
Tom Wauters
WPPWIE Review Meeting, November 17th – 21st 2025

## Slide 2
Be
Beryllium
4
9.012
W
Tungsten
74
183.84
Tmelt = 1287C
Tmelt = 3422C
B
Boron
5
10.81
New baseline and IRP
Boronization and boron studies
Tritium transport in materials
  Tritium retention and removal
  Permeation during baking & mitigation
  Open-source framework: PFC-Tritium-Transport
First wall of SRO and DT
Divertor
Conclusion
Outline
* Application of thin boron coating on the W PFC’s to retrieve the gettering function of Be in the full-tungsten ITER
Baseline 2016
Baseline 2024

## Slide 3
Robust achievement of ITER Project goals, in view of past challenges (delays due to the Covid-19 pandemic, technical challenges in completing first-of-a-kind components and in nuclear licensing)
Realistic and reliable assembly – commissioning - operation
Achievement of earliest start of the ITER Nuclear Phase (DD operation) and minimization of technical risks  a new 1st phase “Start of Research Operation” (SRO)
Stepwise safety demonstration  2 new DT phases (DT-1,2)
New Baseline rationale
Key elements of the new baseline driven by physics/operations:
    First Wall: beryllium (Be)  tungsten (W), start with inertially cooled W wall
    Optimized heating mix + boronization  ease path to Q = 10 with added W

## Slide 4
New Baseline publications
https://www.sciencedirect.com/science/article/pii/S2352179124002771?via%3Dihub
https://doi.org/10.1088/1361-6587/add9c9
R&D needs for the new Baseline and the complete Level 3 ITER Research Plan now available as ITER Technical Reports:

## Slide 5
Overall Project Schedule for new Baseline
IC: Integrated Commissioning
SRO: Start of Research Operation
FPO: Fusion Power Operation
Cryostat Closure
Full Field
Divertor Plasma
Start DD operation
Full Ip & BT
Q=10
>50s
Q=10
>300s
Assembly-I
IC-I
IC
-II
Assem
bly-II
SRO
FPO-I
FPO-II
FPO-III
FPO-IV
FPO
-V
Operation
16 Months
Maintenance
8 Months
Mar.
2033
18
Months
27 Months
Oct.
2034
Dec.
2036
24 Months
Dec.
2038
Sep.
2039
10 M
Sep.
2041
Sep.
2043
Sep.
2045
Sep.
2047
Operation
16 Months
Maintenance
8 Months
Operation
16 Months
Maintenance
8 Months
Operation
16 Months
Maintenance
8 Months
Operation
16 Months
Target dates:
DT-2
DT-1
Approval chronology:
    ITER STAC-30 (May 2024) endorses Level 1 Research Plan and proposed Level 1 Construction Schedule
    ITER Council 35 (Nov. 2024) endorsed the overall approach proposed for the 2024 Baseline
    ITER STAC-32 (May 2025) endorses Level 2 and Level 3 Research Plan  reviewed favourably by ITER Council 36 in June 2025

## Slide 6
Boronization - I
Modelling of boronization GDC indicated need for LFS and HFS diborane injection points + 11 GCD anodes
Non-symmetric GDC anode distribution at in SRO & non-uniform boronization  experiments show boronization needed but spatial distribution not too critical
B2H6 ionization and dissociation in SRO
T. Wauters NME 2025
Need for validating and improving boronization simulations
B deposition assuming 20% surface loss probability of [Mayer NME2025]

## Slide 7
Boronization - II
Lifetime of B layer evaluated by erosion-deposition using WallDYN3D
  short on plasma exposed areas
  ~ few 104 s in remote areas  O2 gettering not to cover W by B
50 nm B binds ∼1–5 × 1020 O2/m2  10% wall area absorbs 2.5 -12.5 weeks 316 SL outgassing
K. Schmid NME 2024 and ISFN R&D
t = 0 s
100 nm B
t = 105 s
< 10 mm B:W
    Maximum boronization frequency 2 weeks (STM)
Wall deposited B erodes and migrates to divertor or is covered by W
Need for (i) validating layer lifetime estimates and (ii) criteria for layer to dust conversion

## Slide 8
6.7% N 3.6% C
H retention in mixed material deposits
Boronization layers using B2H6, B10H12, B2C10H12
Pitts, NME 2025
W containing magnetron sputtered B layers, proxy (?) for divertor deposits
Gautam, PFMC O-4
[1] Abe, NME 2025
[2] Rohde, PFMC I-7
0.5 H/B
0.1-0.25 in 3 AUG boronizations [2]
0.4 in DIII-D boronization mainly in B-C-D bond (10% of C in layer) [1]
[3] Wampler, JNM 1999
[4] Krieger, NME 2023
Divertor co-deposits in C-mod [3] and AUG [4]: 0.1 H/B
W content lowers O uptake capability
0.1 H/B
Need for retention properties of ITER relevant deposits
Notes: Boron layers have the capability to take up significant amounts of H

## Slide 9: Outline ITER fuel removal strategy
BT off: GDC and GDC boronization @ 70oC
10-12 operational days and 2-4 Short Term Maintenance days
BT off: GDC and baking @ 240C
Dedicated time for T clean-up: e.g. 1 RISP + ICWC pulse per day
T inventory management aims at 70-80% inventory reduction
  Methods based on JET DTE-2 experience: Raised Inner Strike Point (RISP) + Ion Cyclotron Wall Conditioning (ICWC)
  15% of DT-1 FPO campaign time allocated to T removal
RISP in JET
RISP
V5
RISP in JET
Notes: The removal strategy aims at an up to 80% reduction of the amounts shown on the previous slide

## Slide 10: Outline ITER fuel removal strategy
BT off: GDC and GDC boronization @ 70oC
10-12 operational days and 2-4 Short Term Maintenance days
BT off: GDC and baking @ 240C
Dedicated time for T clean-up: e.g. RISP + ICWC before STM / before boronization
T inventory management aims at 70-80% inventory reduction
  Methods based on JET DTE-2 experience: Raised Inner Strike Point (RISP) + Ion Cyclotron Wall Conditioning (ICWC)
  15% of DT-1 FPO campaign time allocated to T removal
RISP
V5
RISP in JET
Need for validating fuel recovery strategy in full-W devices with boronization

## Slide 11: Isotope exchange from W and B
D concentration (at.%)
Need to specify mechanisms for isotopic release/exchange from boron layers
W pre-loaded at 1024 D/m2
Exposed to H (200 eV)
343 K
200 eV H
Hodille, ISFN
MHIMS simulation with material parameters of [Oya JNM 2004]
Roth, JNM 2013
D concentration (at.%)
Fluence of 1021 H/m2 sufficient to deplete near surface layers in W and B
Tungsten
Boron
1021 atoms/m2 is feasible in 20 min ICWC in ITER at 15% duty cycle, based on
  TOMAS and TORE SUPRA ICWC charge exchange spectra scaled to ITER power / surface area
  EAST ICWC charge exchange spectra at ITER relevant power / surface area
Notes: Isotope exchange experiments in W on the left and simulations for Boron on the right show that …

## Slide 12: Thermal release from B layers
Thermal release from B layers simulated by CRDS [1] & MHIMS [2] in 1D
  D trapping parameters in B adapted to experimental data of [3-5]
[1] Matveev, Phys Scr 2020
[2] Hodille, JNM 2015
[3] Nakahata, JNM 2007
[4] Annen, J Non-Crystalline Solids 1997
[5] Oya, JNM 2004
[6] DeTemmerman, NME 2017
Hodille, ISFN
Baking at 220oC is not efficient for removal from > 10 micron thick deposits
(Similar to Be [6])
MHIMS
Param: [5]
  Baking for 2 weeks
T release
Raised Inner Strike Point (RISP) scenario 10 MA deuterium L-mode 20 MW ECH [2]
B:D Deposit
Rc
W monoblock
~5 µm
Layer temperature oC
Release fraction, %
  10s of layer heating by plasma
20 to 50 micron
CRDS [1]
Param: [3]
1 to 5 micron
Notes: Operating normal baking for several weeks, at the end of the campaign when layers are …

## Slide 13: Thermal release from B layers
Thermal release from B layers simulated by CRDS [1] & MHIMS [2] in 1D
  D trapping parameters in B adapted to experimental data of [3-5]
[1] Matveev, Phys Scr 2020
[2] Hodille, JNM 2015
[3] Nakahata, JNM 2007
[4] Annen, J Non-Crystalline Solids 1997
[5] Oya, JNM 2004
[6] DeTemmerman, NME 2017
Hodille, ISFN
Baking at 220oC is not efficient for removal from > 10 micron thick deposits
(Similar to Be [6])
MHIMS
Param: [5]
  Baking for 2 weeks
T release
Raised Inner Strike Point (RISP) scenario 10 MA deuterium L-mode 20 MW ECH [2]
B:D Deposit
Rc
W monoblock
~5 µm
Layer temperature oC
Release fraction, %
  10s of layer heating by plasma
20 to 50 micron
CRDS [1]
Param: [3]
1 to 5 micron
Need for better understanding of
thermal release / isotopic exchange from ITER relevant material deposits (B/W/O)
means to improve baking efficiency (gas atmosphere or combined with GDC?)
release of T during vessel venting
Notes: Operating normal baking for several weeks, at the end of the campaign when layers are …

## Slide 14: Permeation through SS316L diagnostic first wall
Diagnostic first wall = water-cooled plasma-facing surface of ports with diagnostic apertures
Depending on material parameters, permeation through Stainless Steel 316L surfaces during baking can be significant
Predictions for permeation barriers rely on material parameters and material interface conditions
SS
Cu
1 mm
W
1 mm
SS
W
2 mm
SS
W
SS
50 µm
50 µm
SS
W
SS
SS
Al203
SS
5 mm
Integrated permeation flux into coolant (%) |  |  |  |  | 
100 | 74 | 3 | 0.2 | 10-7 | <10-7
Charge exchange atoms
Need for hydrogen transport parameters for ITER materials and material interfaces
Need to assess role of boron layers on permeation and retention
Notes: When ITER is baked, …

## Slide 15: Fuel inventory measurements in ITER
① Tritium monitor (LID-QMS)
② Erosion monitor
In-vessel viewing system
Pressure gauges
Diagnostic RGA
PVTc analysis at Tokamak Exhaust Processing (TEP)
PVTc analysis at Storage and Delivery System (SDS)
① First wall samples
② Dust monitor
Intra- and inter-shot gas balance
Global gas balance
Post-mortem analysis
Local measurement
Single discharge
Single cryo-regeneration
Short-term retention
Multiple operation days
Includes inter-shot outgassing
Long-term retention
Entire campaign or longer
Long-term retention
Inter-shot
Short- or long-term
①
②
Φ
Φ
injected
Φ
pumped
retained
Gin
Gout
Gwall
JET example
①
②
~20 mm
Need for experience on in-vessel inventory measurement in W/B environment
Need for continued development of LIBS presently considered for in-between campaign surface characterization using Agile Robot Transport system in ITER
Notes: Such simulations need of course to be supported by measurements…

## Slide 16: Numeric tracking of T inventory in ITER
Bake
Divertor 47
6 mm
First wall row 4
Shadowed
10 mm
W at inner wall shadowed area
T inventory starting from empty surfaces:
10 days of DT pulses
Bake
Divertor 53
6 mm
W at inner divertor
Tritium inventory determined by boron
Baking is effective for removal from W
Divertor 59
5 µm boron deposit
6.8x1022
Bake
Bake
Bake
W near inner strike point
1.2x1020
7.6x1019
1.8x1018
Atoms/m2
Atoms/m2
Atoms/m2
Atoms/m2
Based on FESTIM2: https://github.com/iterorganization/PFC-Tritium-Transport + https://github.com/festim-dev/hisp
Based on MHIMS: https://git.iter.org/projects/BND/repos/hisp
Need to validate inventory tracking approach based on inventory measurement and simulations
Dunnell, to be submitted to NME
Notes: An example of a simulation performed using this platform, is shown on this slide…

## Slide 17
SRO wall : Scenarios + resilience to unmitigated loads :
In-vessel VS to decrease risk of downwards VDE
W (wt.%) 97
Ni (wt.%) 2
Fe (wt.%) 1
Tmelt~1500 oC
Tmelt ~ 3400 oC
Cost: choice of W material based on stationary & transient loads (up to 15 MA)
Optimized for resiliency to unmitigated/partially mitigated transient loads
ITER 15 MA unmitigated VDE – JOREK – Artola
Need for qualifying W coatings and HWA under ITER relevant loads conditions

## Slide 18
Suppressed/no-ELM regime required for Q ≥ 10  modelled with Dped, cped anomalous for main ions and anomalous + neoclassical for W
Improved evaluations : W sources from modelling + self-consistent SOL plasma (largest Pwall and Gwall compatible with design)  Ne main driver for W wall source
ITER - SOLPS – Pshenov
ERO2.0 (W gross erosion) – C. Bauman
Impact of W wall on Q ≥ 10 is low/moderate
Need for validating W erosion/migration codes in present devices

## Slide 19
Divertor
54 Cassette Assemblies, 8 t each, ~140 m2 W monoblocks and flat tiles
Full-scale prototypes complete for all major components (IVT, OVT, Dome, CB)  supply chains established for manufacture in all concerned DA’s  3 OVT already completed at JA-DA
Need for experience on long-pulse operation with ITER-like PFUs, including performance limits and in-vessel monitoring, strategies for managing material deposits and handling of dust

## Slide 20
Conclusion
New baseline includes new/modified systems and operational strategies to mitigate risks of W wall : boronization, increase of PECH & Ptot (also for Q ≥ 10 with 3.1025 n in DT-1), operation with central ECH at 2.65 T and 5.3 T, etc.
Staged installation of systems (SRO and DT-1) includes risk minimization : inertially cooled W wall and ELM control schemes in SRO
In preparation of ITER operations, it is essential to assess the advantages/risks of W wall in ITER using experiments and modelling
Work of PWIE is essential and well aligned with open R&D issues ITR-25-005
  Thank you for your support and I wish you a successful meeting

## Slide 21
Video of sector installation in tokamak pit
18 June 2025