## Slide 1: Erosion and redeposition on WEST PFUs phase 2
M. Diez et al.
November 19, 2025

## Slide 2: Outline
Erosion of the lower divertor
Redeposited layers on the HFS of the divertor

## Slide 3: Introduction / Context / Objectives
WEST phase 1 (2016-2020)
Erosion depends on toroidal position (ripple)
Erosion in the orders of 10µm
  8µm at ISP > 6 µm et OSP
  eroded area at OSP > eroded area at ISP
Total eroded volume ~2,5 cm3 over the whole divertor after 7h of plasma
WEST phase 2 (2021-present)
Erosion behaviour of W coating vs bulk W ?
Erosion rate phase 1 vs phase 2 ?
No marker layers on PFUs phase 2
how to measure erosion ?
W-coated graphite PFUs
Bulk W ITER-like PFUs
[M. Balden Phys. Scripta 2021]
[M. Balden PFMC 2025]
[A. Huart PFMC 2025]
[A. Hakola IAEA 2025]

## Slide 4: Indentations used as erosion markers
#21
#22
#31
#32
Q3B
Max ISP
Max OSP
Plasma-exposed area
PFU#357
PFU#361
PFU#356
PFU#355
Reference indentation
Width : 350 µm
Depth: 50 µm
plasma
Min OSP
Min ISP
Markers on the plasma-exposed are of the monoblocks
Change of morphology (depth, shape)  information about erosion
Hardness machine to make the markers (indentations)
4 PFUs equipped with « erosion markers » installed in sector Q3B

## Slide 5: Erosion monitoring directly on divertor sector
At each shutdown the sector is put on the confocal microscopy bench to acquire 3D mapping of each indentation (no PFUs removal + non destructive)

## Slide 6: Erosion monitoring directly on divertor sector
6
2025 - PFU356, MB14 - Post C11
2024 - PFU356, MB14 - Post C9
2022 - PFU356, MB14 – initial
plasma
2023 - PFU356, MB14 - Post C7
plasma
100 µm
100 µm
100 µm
100 µm
plasma

## Slide 7: The average depth is determined using Python
Average depth
3D mean plane
lowest point
Each CLSM 3d map is then post treated using Python to determine the average depth of the indentation
C6-C7
C8-C9
C10-C11
2023
2024
2025

## Slide 8: Results
Results at ISP
No erosion on MB 17
Erosion MB 14 > MB 15 > MB 16
15-20 µm of erosion ?
Results at OSP
Erosion MB 26 > MB 27 > MB 28, MB 29
Erosion at max OSP (30 µm) > min OSP (20µm) ?

## Slide 9: Future steps (2026)
How can we be sure that a change of depth necessarily represents erosion ?
MB 15
Analysis plan
1 PFU removed from the sector after C9
PFU cut into samples
High magnification observation of the indentations (CEA)
HR CLSM (MPG)
Destructive analysis (FIB) to observe the cross section of the indentations and see whether there is deposited layers inside (MPG)
MB 13
[C. Martin]

## Slide 10: Outline
Erosion of the lower divertor
Redeposited layers on the HFS of the divertor

## Slide 11: Introduction / Context / Objectives
WEST phase 1 (2016-2020)
~ 50 µm deposits after 7 hours of plasma
Complex structure, multi layers / difficult to relate with plasma history
Mainly W + traces of Mo, Fe, Cu, O, B
Main source of D retention
WEST phase 2 (2021- now)
W-coated graphite PFUs
Bulk W ITER-like PFUs
[C. Martin Phys. Scripta 2021]
[M. Balden Phys. Scripta 2021]
[A. Hakola NME 2025]
[R. Mateus PFMC 2025]
[I. Jogi JNE 2023
[I. Jogi NME 2025]
Layers may not be much different from those of phase 1 BUT:
Same deposition rate as during phase 1 ?
Effect of the ripple on the deposited layers ?
Effect of the toroidal bevel on the deposited layers?
[J. Gaspar NME 2024]
[C. Martin NME 2024]
[A. Marin JNM 2025]

## Slide 12: Experimental procedure
Laser cleaning of the divertor for scientific purposes
Sector Q1A : completely cleaned, except for 2 PFUs that were partially cleaned in order to study deposition
1 divertor target at min ISP (#391)
1 divertor target at max ISP (#419)
Evaluation of the thickness of the deposited layers using confocal microscopy
MB 1 to MB 12  radial profile
3 measurements / MB  toroidal profile
#391
(min ISP)
#419
(max ISP)
0
46 µm
110 µm
42 µm
50
100
Q1A, before cleaning, june 2025
Q1A, after cleaning, july 2025
MB 6
PFU#419
-7 mm
0 mm
7 mm
[M.Firdaouss ICFRM 2025]

## Slide 13: Results – thickness of the layers
Clear effect of the ripple : thicker layers at max ripple (~100µm)
Clear effect of the toroidal bevel : non uniform thickness
  very thin on the magnetically shadowed area
  grow linearly toward the exposed area
Maximum thickness on MB 8 and MB 9
MB 1
MB 5
MB 14
MB 10
MB 1
MB 5
MB 14
MB 10
#391
(min ISP)
plasma
#419
(max ISP)

## Slide 14: Results – amount of redeposition on the divertor
121 mm3
Volume of redeposited layers over a 1/2 ripple pattern ~ 0,98 cm3
Over 1 ripple pattern ~1,9 cm3
1,9 cm3 x 19 ripple patterns = total amount on the divertor ~ 37 cm3 *
The erosion of the divertor alone cannot explain such a large amount of deposited layers in the HFS!
* Layers formed between C6-C11 (18 hours of plasma) with partial cleaning after C7 and C9
1 ripple pattern
42 mm3
Max ISP
Min ISP

## Slide 15: Results – amount of redeposition on the divertor
With partial cleaning ~100 µm thick layers – 37 cm3
If layers 100% dense and made of W  714 g of W
If layers 80% made of W  573 g of W
If layers 50% made of W  357 g of W
No cleaning at all ~ 300 µm thick layers
[C. Martin et al., NME 2024]
W density : 19,3 g/cm3
2 mm
If no cleaning performed  > 1 kg of W on the lower divertor of WEST after 18h of plasma?

## Slide 16: Thank you

## Slide 17: Optical images – PFU#357 min ISP, 2024
MB 15
MB 28
MB 26
REF
MB 13

## Slide 18: Results – evolution of layers with plasma time
The layers grow with plasma time
end of phase 1: 50 µm
phase 2 : > 100 µm when cleaning is performed but can reach > 300 µm with no cleaning
> 1 kg of W after 18 hours of plasma when no cleaning is performed ?
2 mm

## Slide 19
PFU 355 MB10 - depots
Desalignement ?