## Slide 1: Ion-beam analyses of boronization samples originating from WEST
E. Pitthan1, P. Petersson2, D. Gautam1, M. Rubel1,2, D. Primetzhofer1, M. Diez3
1Department of Physics and Astronomy, Uppsala University, 751 20 Uppsala, Sweden
2Department of Fusion Plasma Physics, KTH Royal Institute of Technology, 100 44 Stockholm, Sweden
3CEA, IRFM, F-13108 Saint-Paul-Lez-Durance, France
Jülich, 19th of November, 2025
WPPWIE Review Meeting 2025

## Slide 2: Spatially non uniform B layer predicted for ITER
Normalized B2D6 reaction distribution:
ITER
equatorial
plane
Recent simulations suggest strongly non-uniform B2D6 reaction distribution:
0.3 Pa with 88 % He and 12 % D2
Diborane molecules injection points
4 anodes in the equatorial plane (30 A/anode)
Non-uniform B layer formation?
Enough for ITER commissioning with full-W environment?
Non-uniform boronization in WEST with 3/6 feed location (February 2025)
T. Wauters et al. Nucl. Mater. Energy, (2025) 42

## Slide 3: Non uniform boronization performed in WEST (04 February 2025)
Spatially non-uniform boronization tested in WEST
 6 glow electrodes (anodes) on top
 3 (out of 6) diborane B2D6 feed locations
bottom LFS Q1, Q2, Q3 (half of the torus)
Boronization of ~5h, 70°C
>85% He / <15% B2D6, 0.5 Pa, 10 g of B
Two collector probes (cathodes) with 42 samples (W and SS) located in:
    Q3 (B-rich region)
    Q4 (B-depleted region)
Q1
Q2
Q3
Q4
Q6
Glow electrode

## Slide 4: Non uniform boronization performed in WEST
B2D6
Glow electrode
(anode)
Q4 probe
(cathode)
1
2
3
4
5
no diborane injection at this location during the experiment
- for illustration purposes only -
H
G

## Slide 5: 42 samples strategically positioned on the probes
5
W
low cobalt SS
1
2
3
4
5
Ra=0,65 µm
Ra=0,28 µm
1
2
3
4
5
1
2
3
4
5
Q4 probe
(E,F,G,H)
Q3 probe
(A,B,C,D)
Q3
Q4
B
A
C
D
E
F
G
H
Samples distributed over the 4 sides of the probes
  A,B,C,D (Q3 probe)
  E,F,G,H (Q4 probe)
21 samples / probe
  Row #1,4 : SS
  Row #2,5,bottom : W
  Row #3: mix of SS and W

## Slide 6: Visual observation of the probes and samples after the non-uniform boronization
Q4 probe
(B-depleted region)
316L
316L
W
W
Q3 probe
(B-rich region)
Higher color contrast on the probe located near the injection point (Q3)
Color gradient visible both on the probes and on the samples
316L
Samples extracted from Q4 probe after boronization
Q3 probe after boronization

## Slide 7: Post mortem analysis of the exposed samples
7
Gold coating applied on the sample surface (25 nm) to protect them from oxidation
3 batches of samples (division made by substrates and location)
Characterization at regular intervals to determine the evolution of B layers over time
IBA + SEM/FIB (+ SIMS + XPS)
VR (16 SS samples + 1 ref. sample)
Demokritos (18 W samples + 1 ref. sample)
MPG (3 W + 2 SS samples)
Gold coating process
Transportation under vacuum sealed bags
This presentation

## Slide 8: Ion Beam Analysis of boronization samples from WEST
Q3
Q4
E
1
2
3
4
5
316L
316L
316L
316L
+1 ref Au/316
Non-uniform
Boronization in WEST:
Samples received: Au/boron layer/316L
Evaluate the uniformity of B layers in WEST:
  Homogeneity in toroidal position (Q3A and Q4B).
  Homogeneity along Z direction (vertical direction).
  Homogeneity in 4 toroidal directions.
Determine the amount of oxygen trapped in the boron layers and study how to desorb it.
Presence of He in layers?
Stability of layers in air?
Q3
Q4
B
A
C
D
E
F
G
H

## Slide 9: Ion Beam Analysis of boronization samples from WEST
IBA measurements at Tandemlab-UU (VR):
2025-04-28 (t0):
1st: EBS+NRA+PIXE using H+ 2.6 MeV (higher sensitivity to B).
2nd: ToF-ERDA I 36 MeV (depth profile of all isotopes).
2025-05-07 (t0 + 9 days in vacuum):
1st: EBS+NRA+PIXE 3He 2.5 MeV (higher sensitivity to D).
2nd: ToF-ERDA I 36 MeV.
2025-06-26 (t0 + 9 days in vacuum + 51 days in air):
Single measurement: ToF-ERDA 79Br9+ 28 MeV
t0
H
D
10B
11B
C
N
O
Fe+Cr+Ni
Scattered I
Au
He
Si+Al
ToF-ERDA for sample B4:
Measurements in different days at different spots separated by ~2 mm from each other.
× × ×

## Slide 10: Ion Beam Analysis of boronization samples from WEST: PIXE
PIXE results: Identify main element (medium and high-Z) in samples
Fe was identified as most common element from substrate (Fe was used as substrate component in ToF-ERDA results); followed by Cr and Ni.
Au, Si, and was also identified in samples.
Ar was observed in samples H1 and A4.

## Slide 11: Ion Beam Analysis of boronization samples from WEST: ToF-ERDA
Depth profile (t0):
Fe was used as representative element from substrate (confirmed by PIXE).
Boron layer in samples A4-H4 significantly thicker than A1-H1.
Indication of intermixing between Au/B layer and B/316L from depth profiles is a known pitfall from multiple scattering effects for heavy atoms*.
*E. Pitthan et al., Surface &Coatings Technology, 417, 127188 (2021).
RBS does not indicate significant roughness nor intermixing in layers:
well-defined shift in Fe signal in boron layer in comparison to reference.
H and D loss during measurements are possible: comparison with 3He NRA.

## Slide 12: Ion Beam Analysis of boronization samples from WEST: ToF-ERDA
H+D+O region:
Sample A4 – comparison between measurements in different days with beam spots separated by 2 mm:
Oxygen presence mainly around B/substrate region.
No indication of change in composition 1 week after open of packages (t0 + 9 days in vacuum).

## Slide 13: Ion Beam Analysis of boronization samples from WEST: ToF-ERDA
Q3
Q4
B
A
C
D
E
F
G
H
Non-uniform
Boronization in WEST:
H+D+O region:
Q3
(B-rich region)
Q4
(B-depleted region)

## Slide 14: Ion Beam Analysis of boronization samples from WEST: ToF-ERDA
1
4
A-H
A-H
Row 1 (thin layers):
Row 4 (thick layers):
Main observations:
Boron layer in row 4 (A4-H4) significantly thicker than row 1 (A1-H1):
Row 1: 9.8 nm*.
Row 4: 34.4 nm*.
*Assuming a density of 2.351 g/cm3.
Slightly thicker boron layers in Q3 samples (A-D).
Higher oxygen + hydrogen and lower deuterium in Q4 samples (E-H).
Inverse correlation between boron and oxygen.
Q3
Q4
B
A
C
D
E
F
G
H
Non-uniform
Boronization in WEST:
Q3
Q4
Q3
Q4

## Slide 15: Ion Beam Analysis of boronization samples from WEST: p-NRA/EBS
Proton beam 2.6 MeV used for quantification of boron and comparison to ToF-ERDA results.
Incident at 0° with the surface normal and scattering angle of 170°.
Simulation using SIMNRA.
Cross sections used in SIMNRA: M. Mayer 1998.
Gold thickness varies from 60-100×1015 atoms/cm2 with average at 85.5×1015 atoms/cm2, corresponding to 14.5 nm assuming density of 19.31 g/cm3.
Overall agreement between ToF-ERDA and EBS/NRA.
High background (EBS) and low statistics (NRA) hinders quantification for samples with low amounts of boron (A1-H1).
Q3
Q4

## Slide 16: Ion Beam Analysis of boronization samples from WEST: 3He-NRA
3He beam 2.5 MeV used for quantification of deuterium and comparison to ToF-ERDA results. Incident at 12.5° with the surface normal and scattering angle of 135°. Simulation using SIMNRA.
Cross sections used in SIMNRA: B. Wielunska 2015.
Higher amounts of D in comparison to ToF-ERDA due to higher probing depths and D loss against the beam in ToF-ERDA.
Combination of 3He-NRA (D) and p-NRA/EBS (B) to obtain average D/B ratios:
A-D samples (Q3): 0.32.
E-H samples (Q4): 0.13.
Q3
Q4
Q3
Q4

## Slide 17: Stability in air: ToF-ERDA after 51 days in air
Average at. composition (%) in films – (t0 + 9 days in vacuum + 51 days in air):
Average composition in thin layers (A-H 1): from 50 to 200×1015 atoms/cm2
Average composition in thicker layers (A-H 4): from 200 to 400×1015 atoms/cm2
Slight increase of (O+H)/B ratio in Samples E4-H4 (Q4, row 4).
No consistent effect in deuterium/boron loss, or oxygen in air.
Average composition in films subtracting Fe and Au contribution:

## Slide 18: Conclusions:
Vertical direction: Boron layer in samples A4-H4 (row 4) significantly thicker than A1-H1 (row 1).
Toroidal position: Slightly thicker boron layers collected in Q3 in comparison to Q4.
Chemical composition: Higher contamination (O+H) and lower deuterium in E-H samples (Q4).
D/B ratios: 0.32 for A-D (Q3) samples and 0.13 for E-H (Q4) samples.
Presence of He: Indication of He in some samples but in very low concentrations (≤0.1 at.%).
Stability in air: No consistent effect in deuterium/boron loss, or oxygen.
1
4
A-H
A-H
Q3
Q4
B
A
C
D
E
F
G
H
Non-uniform
Boronization in WEST:

## Slide 19: Open questions and future work:
1
4
A-H
A-H
Q3
Q4
B
A
C
D
E
F
G
H
Non-uniform
Boronization in WEST:
Effect of homogeneity in vertical direction just from geometrical effect (higher field close to the tip of probe)?
Why samples further from B2D6 feed locations present different chemical composition? Lower porosity?
Can the O/B ratio be used as measure of the efficiency of oxygen gettering properties? Effect from air exposure (entire time-line)?
Inverse correlation between boron and oxygen suggests that use of thinner layers can also be efficiency. Ideal B thickness?
Comparison with uniform boronization (future work).