## Slide 1
M. Rasinski, Ch. Baumann, K. Krieger, R. Dux, A. Hakola, J. Karhunen, V. Rohde, S. Samuli
W erosion and redeposition in AUG Ne seeded experiment

## Slide 2: Preparation
On each sample 2-4 FIB cross-sections with line marking were prepared
Cross-section examined after AUG Ne campaign to determine the erosion and redeposition
Results will be used for ERO 2.0 modeling
AUG exposure
H-mode and L-mode D plasma with Ne seeding
Set of W and Mo samples for each experiment
17mm
6 mm
2.5mm
2
1

## Slide 3: H-mode
OSP
OSP
VIS
W
Mo
H-mode series – Mo I line intensity (5528 A)

## Slide 4: H-mode results
H-mode
x
before
after
W
Erosion– not possible to measure due to technique sensitivity
Mo
Erosion ~ 80 nm
W
Mo
x
W
Mo
80 nm

## Slide 5: H-mode results
H-mode
x
before
after
W
Erosion below 50 nm – not possible to measure due to technique sensitivity
Mo
Erosion ~ 50 nm
W
Mo
x
W
Mo
50 nm

## Slide 6: H-mode results
H-mode
x
Deposition – thin layer of deposition present on the surface of W, at location above the OSP
The thickness is too thin for detailed analysis using FIB sectioning.
TEM lamella preparation in progress in order to assess the thickness and composition.
W
Mo

## Slide 7: L-mode
OSP
OSP
VIS
W
Mo
L-mode series – Mo I line intensity (5528 A)

## Slide 8: L-mode results
L-mode
x
before
after
W
Erosion – not possible to measure due to technique sensitivity
Mo
Erosion – not possible to measure due to technique sensitivity
No visible surface modification on both W and Mo
W
Mo
x
W
Mo

## Slide 9: L-mode results
L-mode
x
before
after
W
Erosion – not possible to measure due to technique sensitivity
Mo
Erosion – not possible to measure due to technique sensitivity
Deposition – present due to disruptions
W
Mo
x
W
Mo

## Slide 10: L-mode results
L-mode
W
Mo
W
Mo
230 nm
170 nm
a)
b)
a)
b)

## Slide 11: L-mode results
Pt
B
N
O
W

## Slide 12: Sp B.1 Exposure of W-nano samples to PSI-2 plasmas
O. Marchuk, M. Sackers, M. Rasinski, S. Brezinsek, A. Houben, M. Klein and A. Kreter
Forschungszentrum Jülich GmbH – Institute of Fusion Energy and Nuclear Waste Management - Plasmaphysik,
Partner of the Trilateral Euregio Cluster (TEC), 52425 Jülich, Germany

## Slide 13: Setup of Psi-2

## Slide 14: Spectroscopic studies on W-nano in PSI-2
5
Front optics of the LOS (#5, along the normal to the target) :
A3 sample (B on W sample) was put to the top
The A3 sample was exposed to 25 minutes in Ar
Two type of lines:
direct photons
reflected photons

## Slide 15: First results (A3)
Wavelength, nm
Variation in intensity /Sputtering yield
Variation in reflectance /optical properties
SEM image of the surface and cross-section after PSI-2 exposure. Spot with coating leftover presents lower erosion rate as compared to bulk surrounding.

## Slide 16
Example of Molecular spectroscopy: BD A-X (B on W)
High-resolution Littrow
Overview Littrow
Calibration
PSI-2
Excellent agreement at several spectral resolutions
H
Marcin Rasiński | WPPWIE Review Meeting 2025 | Page 16

## Slide 17
Molecular spectroscopy: time-resolution
B I 250 nm
Marcin Rasiński | WPPWIE Review Meeting 2025 | Page 17
Sackers M et al, NME 45 (2025)