## Slide 1: Review of previous characterization of collected dust particles from different machines
Marek Rubel
With very important contributions from nearly 70 colleagues coworking on the topic for over 40 years

## Slide 2
B. Emmoth†, H. Bergsåker, N. Almqvist, J.R. Drake, J. Malmberg, M. Cecconello, D. Hasselbrunner†, H. Ferm, A. Hedqvist, P. Sundelin, P. Petersson, D. Ivanova, A. Weckmann, P. Ström, A. Garcia-Carrasco, S.W. Moon, L. Dittrich, E. Pitthan, D. Primetzhofer, D. Gautan
P. Wienhold, M. Freisinger, H. Reimer, V. Philipps, G. Sergienko, A. Huber, E. Wessel, H. Penkalla, M. Rödig, W. Biel, J. Linke, S. Brezinsek
E. Fortuna-Zaleśna, M. Psoda†, J. Grzonka, T. Płociński, A. Balcerzak
J.P. Coad, A. Widdowson, G.F. Matthews, A. Baron-Wiecheć, I. Jepu, A. Zayachuk
N. Ashikawa, T. Otsuka, Y. Hatano, Y. Torikai, S. Masuzaki, K. Osobe, M. Oyaidzu, N. Asakura, T. Hayashi, M. Hara
B. Pegourie
S. Fazinić, I. Božičević Mihalić, G. Provatas, T. Tadić
C. Lungu, C. Porosnicu
J. Varju, J. Adamek, M. Hron
L. Dittrich, C.P. Dhard
This talk could be prepared thanks to the work of many, many colleagues.
Thank you!

## Slide 3: Studies over the years 1984 - 2025: The devices
JET
TEXTOR
EXTRAP-T2
Tore Supra
COMPASS
1987
Graphite cladding and belt limiters
1989-1992
Beryllium: limiters and open divertor Mk-0
Graphite
cladding
1983
Limiters & wall: all metal
1994-1995
1997-1998
Mk-I
Mk-IIA
a
b
c
d
e
1982
Metal liner and metal poloidal limiters
1988
Graphite poloidal & toroidal limiters
a
1986
Carbonised wall
b
c
h
C wall
2013
With Dynamic Ergodig Divertor
W
Be
2011- 2023: ILW
i
W7-X

## Slide 4
Interest in Dust
Driving force in studies: Safety & economy of reactor operation
Safety hazard: ignition, H2 generation, Be, tritiated matter
Impact on operation:
  mobilization (disruptions),
  degradation of optical diagnostics,
  impact on pumping systems.
Dust/metal splashing studies started in 1984 (e.g. JET),
very systematic studies since 1997 (TEXTOR, JET)
Key points:
  quantity and fuel retention properties,
  behaviour in plasma.

## Slide 5
There will be many pictures, but this work is far beyond ”picturology”.
Dust is unpleasant, difficult in handling, in many cases just dangereous.
Dust is fascinating
2 mm
PARTICLE FROM A DIESEL ENGINE
Dr. Tricard, ELF Acquitaine, France
Inconel
Be-rich tubes
Boiling Be ”hives”
A mix of everything
10 mm
r: 7.5 µm
V: 1767 µm3
W sphere
empty inside

## Slide 6
Integrated / Holistic Approach
Collection
and retrieval methods
Ex-situ analyses
Dust diagnosis in plasma
Fuel (tritium)
retention studies
Impact on diagnostic components
Quantity assessment
Dedicated
in-situ
&
ex-situ experiments
Mobility under machine
maintenance
Moisture impact on dust generation
Dust generation under laser impact
Mechanism of formation/
generation

## Slide 7
In-Vessel
HR Imaging
Fast Cameras
IR Cameras
Thermocouples
Marker
Techniques
Magnetic
Diagnostics
Optical
spectroscopy
Performance of Optical
Components:
Mirrors
Windows
Long Distance
Microsccopy

## Slide 8
Dust Collection: Facts, Advantages, Drawbacks
Vacuum cleaning: 360 o
Local sampling: sticky pads
Advantage: Detailed local analyses.
Drawbacks:
The top layer of samples represents
the bottom of deposits.
Force is applied during the collection;
more than just dust may be collected.
Messages:
Fairly small amount sampled.
Good adherence of particles to tiles.
Dust monitors
Silicon plate
Message:
Tiny amount collected.
Advantages:
Collection of undisturbed mobilized particles.
Precise analyses.
Message:
Around 1 g found after each campaign (20 h of plasma)
Drawbacks:
Composition: a mix of all particles.
Not possible to associate dust morphology with a place of collection.

## Slide 9
µ-NRA
SEM
Radiography:
Imaging plate
Radiography:
BIX
GDMS
µ-EPS
µ-PIXE
Full
Combustion
µ-RBS
TDS
AES
AFM
STM
XPS
OM
MS
FIB
Laser
Profilometry
TEM
STEM
WDS
EELS
Colorimetry
Raman
AMS
LSC
ERDA
HIERDA
ICPOS
SIMS
EPMA
XRD

## Slide 10: TEXTOR plasma: detachment of co-deposits
(b)
4.64 s
4.70 s
4.74 s
4.66 s
Time sequence showing a cloud of particles
Dust release is immediately
detected by spectroscopy.
A debris motion caused by the rocket effect.

## Slide 11: JET-ILW: Beryllium melting and splashing. A rain of droplets from the upper limiters
#84832

## Slide 12: Beryllium splashes
#84832
#85807
80 mm
30 µm
e
On dust monitors
On the outer divertor tiles
Messages:
Be droplets and splashes adhere fairly well to surfaces.
Splashes are mostly round and only very thinly coated by deposits  ”rain” of fine droplets at right angle from dump plates in the run-away experiment, last in ILW-2.
500 µm
On a diagnostic mirror

## Slide 13: Brittle destruction of carbon by wall locking modes at the EXTRAP-T2 RFP device
A burst of particles is caused by wall locking mode  extreme local energy deposition.
Particles’ release from the wall is accompanied by a drastic increase of all spectroscopy signals: ne Te Zeff ncarbon
Magnetic diagnostics

## Slide 14: Extrap-T2 RFP: crystalline debris and co-deposits
(b)
a
15 mm
b
15 mm
Debris after passing through the plasma.
Dark field image of a co-deposit with embedded crystallites (bright spots) and a diffraction pattern.
(
Large graphite debris (2 mm) with a co-deposit.

## Slide 15
Carbon-based polymer-like films. Precursors of co-deposits?
20 µm
20 µm
20 µm
EXTRAP-T2
TEXTOR
COMPASS

## Slide 16: Metal splashes: JET with full metal wall (1984)
1983
Limiters & wall: all metal
500 mm
125 mm
125 mm
600 mm
125 mm
200 mm
125 mm

## Slide 17: Metal splashes: TEXTOR
Carbon deposits
112 µm
v
ω
300 mm
c
b
X
Inconel splash on the graphite limiter.
Origin: the liner or the ICRH antenna grill.
Rotation of molten
material after splashing.
Arc track

## Slide 18: Metal melting & splashes: What about tungsten?
J.W. Coenen et al., JNM 463 (2015) 78
Dedidated experiments on W melting
W plate, 2 mm thick
Melt zone
TEXTOR: Test limiter with W plate)
JET-ILW: special lamella in bulk W divertor
W droplets in the melt zone.
No W droplets found in the collected debris.
No single loose W droplet has been found on that damaged piece and on the adjacent lamellae.
Nothing in other regions of JET-ILW.
G. Sergienko et al.,
Phys. Scr. T128 (2007) 81
Evolution of melt damage.

## Slide 19: Metal melting & splashes: What about tungsten?
JET-ILW: Langmuir probes
No single loose W droplet found in the matter retrieved from JET-ILW.
Boiling W
Deficit of W: blown out?
Exfoliation of the
overheated surface?

## Slide 20: Metal melting & splashes: What about tungsten?
JET-ILW: Langmuir probes
Metal exfoliation in the overheated region. This may be a real contributor in the W erosion.
Are these pure W flakes or …?
LP26, Tile 6, 16BW
> 0.5 µm
> 0.5 µm

## Slide 21: Comparison of W and C flaking. Identical?
> 0.5 µm
170 nm
43 mm
Cross - section
Top surface
Single
flaking
layer
~ 15 000 s of plasma operation
W
JET-ILW
C
TEXTOR

## Slide 22: W melting: Castellated W test limiter in TEXTOR
Deliberate melting.

## Slide 23: W melting: Castellated W test limiter in TEXTOR The role of chemistry in W transport.
WO2 “leaves”
WO2
Cu
Cu
WO2
WO2
WO2
W
W
2 Q scale
Intensity
1500
500
1000
0
40o
30o
50o
b
What is the source of oxygen?
O2 or H2O desorption from bulk Cu or W?
Poloidal direction
Cu base
W
W + WO
2
Cu
W + WO
2
W
melt zone
Toroidal
gap
WO2
W
10 mm
Evolution of signals when melting occured at 2.34 s.

## Slide 24
Categories of dust in JET-ILW
ITER not relevant
Be flakes of coatings from inner wall cladding tiles
Debris of CFC or BN (probes heads)
W-Mo coatings from CFC
Small debris, flakes not molten.
Partly molten (glassy structure)
Spheroids by aggregation of W flakes .
ITER relevant
Be-rich flakes of co-deposited layers
Be droplets and splashes
W droplets and splashes
Steel (and Inconel) droplets and splashes e.g. from antennae grills
Swarf from in-vessel work
Cu chunks from NBI systems, etc
5 mm
5 mm
2 mm
Formation phase

## Slide 25: Fuel tracing in individual dust particles

## Slide 26: JET-ILW: Deuterium in particles on dust monitors
Message:
Only traces of deuterium detected in/on metallic dust particles
S. Fazinić et al., Anal. Chem. 90 (2018) 5744; Nucl. Fusion 60 (2020) 126061; MDPI Materials 15 (2022) 08353.
Combination of several methods: µ-NRA, µ-PIXE with SEM and EDX (different laboratories).
Main difficulty: identification of the same study object in the two labs.

## Slide 27: JET-ILW: Deuterium in particles on dust monitors
Messages: Deuterium presence is amainly associated with carbon.
In quantitative terms, the D content even in C dust is small, 0.01-0.05 (also experience from TEXTOR)
S. Fazinić et al., Anal. Chem. 90 (2018) 5744; Nucl. Fusion 60 (2020) 126061; MDPI Materials 15 (2022) 08353.

## Slide 28: JET-ILW: Tritium in individual particles
Radiography of T in different particles (ILW-1)
b - (T) recorded by radiography.
Superposition of profiles.
Beryllium
Tungsten
Carbon
Note the scale. 100x more in C than in metals
Message:
T presence is associated with C (legacy from JET-C)
T. Otsuka, Osaka-Kindai U. / IFERC
Dust particles are placed on In disk.
Composition of individual particles is identified with EPMA (WDS).

## Slide 29: Boron dust crystals
30 mm
20 mm
4 mm
Precipitation of boron from co-deposit?
T plates ~600 – 700 oC (thermocouples)
T deposit >2000 oC (still below Tm of B and/or B4C)

## Slide 30: Boron/Boronisation as a marker
P. Wienhold et al., JNM 313-316 (2003) 311.
A flake of a stratified co-deposit with three boronisation layers: SEM and SIMS.

## Slide 31
Example of data for from sample 209:
Sample from Module M1, Divertor (DU18).
Identified the presence of B, Fe, Cr, and W in sample. Ti, Ni, and Cu also present in tape.
Ion beam analyses of dust from W7-X (VR)
E. Pitthan et al., VR
Sample-holder at Tandem Laboratory
W originates from a marker tile.
Dust with W is a material transport tracer.
Boronisation with B-10 diborane would contribute to transport studies.

## Slide 32
Outlook: Proposal for studies of W7-X dust
Sample-holder at Tandem Laboratory
SIGMA apparatus for in-situ experiments and measurements.
IBA
Heating to 1000 oC
QMS
Gas inlets (gas mixing)
Ion source
W7-X dust is deuterium free  good chance for:
  stepwise desorption – re-saturation exercise;
  H-D isotope exchange
  …

## Slide 33
Extra slides
Sample-holder at Tandem Laboratory

## Slide 34: ILW 2011-2012 Dust studies: Beryllium flakes
M. Rubel et al., Fusion Eng. Design 2018.
Dust removed by vacuum cleaning. Studies performed at IFERC- Rokkasho
0.4 mm
8.9 mm
Bottom
Middle – 1 mm from top
Top
Large amount of tiny W particles
Very few W particles
Messages:
TEM Dark Field images reveal heavy particles (white) of nm size in deposits.
Particles of nm size identified by EDS as Tungsten.
The amount of particles increases towards the top, i.e. rises with the power of the JET-ILW operation.
Tile side

## Slide 35: ILW 2013-2014: Be splashes on test mirrors
Mirror 127, Mo bulk, Main chamber wall
80 mm
5 mm
1 cm
Droplets or bubbles?
(boiling beryllium)
A. Garcia-Carrasco at al. Nucl. Mater. Ener. 2017
X. Litaudon, IAEA-27, Nucl. Fusion 57 (2017)
2 mm

## Slide 36: Tungsten: Droplets (?)

## Slide 37
W on dust collector (outer divertor)
V: 131 µm3
r: 3.15 µm
V: 0.21 µm3
r: 0.37 µm
5 mm
1 mm
10 mm
2 mm
V: 1767 µm3
r: 7.5 µm
Most probably ”spheroids” (shell with empty interior) in the phase of formation by agglomeration of W flakes detached from the coatings.
Message: There is no evidence of W droplets which would indicate tungsten melting (either W coatings or Tile 5).
E. Fortuna, M. Rubel, Phys. Scr. 2017

## Slide 38
LPs in JET

## Slide 39: JET-C and JET-ILW: Tritium in dust
Specific T activities in dust from JET-C, ILW-1 and ILW-3 measured by FCM.
STEP 1: Compare total amount of dust in the JET-C and JET-ILW campaigns
>200 g of dust from JET-C versus 1 g (total) after ILW campaign!
STEP 2: Find the location of tritium.

## Slide 40
Categories of dust in JET-ILW
ITER not relevant
Be flakes of coatings from inner wall cladding tiles
Debris of CFC or BN (probes heads)
W-Mo coatings from CFC
Small debris, flakes not molten.
Partly molten (glassy structure)
Spheroids by aggregation of W flakes .
ITER relevant
Be-rich flakes of co-deposited layers
Be droplets and splashes
W droplets and splashes
Steel (and Inconel) droplets and splashes e.g. from antennae grills
Swarf from in-vessel work
Cu chunks from NBI systems, etc
5 mm
5 mm
2 mm
Formation phase