## Slide 1: LIBS induced D outgassing in Magnum-PSI exposed samples
Indrek Jõgi, Peeter Paris, Jasper Ristkok, Jort van Kesteren, Beata Tyburska-Pueschel, Jordy Vernimmen, Sanath Jagannath Shetty, Pavel Veis, Hennie van der Meiden
University of Tartu, DIFFER, Comenius University

## Slide 2: Motivation
Laser pulse
Laser pulse heats the material below ablated layer
D will diffuse out – LIBS induced outgassing
D. Matveev et al. Phys. Scr. 96 (2021) 124079
D. Matveev et al. „thermal outgassing removes about 50% of D from a 100 nm thick W layer below the LIBS crater, contributing at least 25% to the amount of D released by ablation itself“
Calculations:
Material with D/T
LIBS – in-situ measurement of elemental depth profiles in the plasma facing components of fusion reactors

## Slide 3: Motivation
Chart: Shot number
 | 228.7111 | 148.667 | 76.3701 | 28.7257 | 42.1646 | 36.282 | 32.8414 | 40.463
 | 123.0876 | 157.6158 | 90.8672 | 67.6262 | 43.895 | 37.1492 | 25.699 | 46.5875
 | 244.4536 | 187.7058 | 137.6218 | 47.192 | 27.3501 | 39.7031 | 55.1434 | 41.3688
 | 198.7507 | 164.6629 | 101.6197 | 47.848 | 37.8032 | 37.7114 | 37.8946 | 42.8064
 | -67.7888 | 4.6582 | 975.9923 | 4169.2208 | 5072.549 | 6098.8558 | 6486.1732 | 8573.3515
Chart: Depth (nm)
| 0 | 0 | 48.5 | 48.5 | 344.2 | 344.2 | 630.79999999999995 | 630.79999999999995 | 758 | 758 | 1321 | 1321 | 5343
z=171.1 | 0 | 6.533 | 6.533 | 3.391 | 3.391 | 2.193 | 2.193 | 1.42 | 1.42 | 0.4177 | 0.4177 | 0 | 0
z=173.4 | 0 | 6.634 | 6.634 | 5.043 | 5.043 | 4.432 | 4.432 | 2.87 | 2.87 | 0.5677 | 0.5677
z=175.7 | 0 | 4.539 | 4.539 | 3.198 | 3.198 | 2.106 | 2.106 | 0.6237 | 0.6237
z=178.0 | 0 | 7.938 | 7.938 | 3.998 | 3.998 | 2.749 | 2.749 | 2.299 | 2.299 | 1.439 | 1.439 | 0.6012 | 0.6012 | 0.1286 | 0.1286 | 0 | 0
z=180.3 | 0 | 5.499 | 5.499 | 3.627 | 3.627 | 2.554 | 2.554 | 1.733 | 1.733 | 0.7286 | 0.7286 | 0.3596 | 0.3596 | 0 | 0
z=182.6 | 0 | 3.25 | 3.25 | 1.563 | 1.563 | 2.519 | 2.519 | 1.126 | 1.126 | 0.5749 | 0.5749 | 0 | 0
z=184.9 | 0 | 4.273 | 4.273 | 2.569 | 2.569 | 0.8365 | 0.8365 | 2.341 | 2.341 | 0.5346 | 0.5346
 | 5.4857 | 5.4857 | 4.3857 | 4.3857 | 3.9143 | 3.9143 | 3.5714 | 3.5714 | 3.3286 | 3.3286 | 2.8857 | 2.8857 | 2.6571 | 2.6571 | 2.6571 | 2.6571 | 2.6857 | 2.6857 | 2.5714 | 2.5714 | 2.5714 | 2.5714 | 2.5429 | 2.5429 | 2.3714 | 2.3714 | 2.2429 | 2.2429 | 1.9571 | 1.9571 | 1.0714 | 1.0714 | 0.64286 | 0.64286 | 0.6 | 0.6 | 0.57143 | 0.57143 | 0.54286 | 0.54286 | 0.54286 | 0.54286 | 0.376 | 0.376 | 0.28 | 0.28 | 0.226 | 0.226
Chart: Shot number
 | 66.177 | 63.1489 | 35.2735 | 7.3676 | 12.7935 | 15.2462
 | 76.0342 | 33.5537 | 32.1369 | 7.9407 | 9.2634 | 25.6474 | 36.881 | 27.5122
 | 66.6895 | 65.9445 | 44.5805 | 9.4516 | 14.0421 | 18.3879 | 25.5959 | 26.5264
 | 68.8571 | 66.9918 | 28.4246 | 6.1475 | 9.7838 | 11.3789
 | 71.0466 | 61.1335 | 35.5863 | 7.2308 | 14.2345 | 12.6089
 | 57.4906 | 67.7669 | 35.4337 | 7.3993 | 13.0401 | 17.0773
 | 66.8013 | 53.9076 | 32.3424 | 6.6089 | 12.8669 | 16.7778 | 20.7254 | 16.7014
 | 66.177 | 63.1489 | 35.2735 | 7.3676 | 12.7935 | 15.2462 | 17.7716 | 19.0048
 | 11.0429 | -9.3392 | 103.0651 | 592.575 | 1032.4155 | 1415.1687 | 1816.7986 | 2124.8816
Chart: Depth (nm)
| 0 | 0 | 49.93 | 49.93 | 238.8 | 238.8 | 515.20000000000005 | 515.20000000000005 | 802.4 | 802.4 | 998.7
z=171.1 | 0 | 12.22 | 12.22 | 6.627 | 6.627 | 4.267 | 4.267 | 2.415 | 2.415 | 0.7991 | 0.7991
z=173.4 | 0 | 6.581 | 6.581 | 4.167 | 4.167 | 2.511 | 2.511 | 0.9944 | 0.9944 | 0.3057 | 0.3057 | 0 | 0 | 0 | 0
z=175.7 | 0 | 6.748 | 6.748 | 3.122 | 3.122
z=178.0 | 0 | 7.068 | 7.068 | 5.954 | 5.954 | 4.077 | 4.077 | 0 | 0 | 5.099 | 5.099 | 1.092 | 1.092 | 0.4051 | 0.4051 | 0.4352 | 0.4352
z=180.3 | 0 | 9.971 | 9.971 | 5.79 | 5.79 | 3.739 | 3.739 | 2.212 | 2.212 | 0.6572 | 0.6572 | 0 | 0
z=182.6 | 0 | 9.626 | 9.626 | 5.416 | 5.416 | 3.413 | 3.413 | 1.904 | 1.904 | 1.001 | 1.001 | 0.3347 | 0.3347 | 0 | 0
z=184.9 | 0 | 9.877 | 9.877 | 4.586 | 4.586 | 3.99 | 3.99 | 3.387 | 3.387 | 2.387 | 2.387 | 1.182 | 1.182 | 0.4401 | 0.4401 | 0 | 0
 | 8.8429 | 8.8429 | 6.1143 | 6.1143 | 6.1143 | 6.1143 | 6.1143 | 6.1143 | 5.9 | 5.9 | 4.8428 | 4.8428 | 4 | 4 | 3.8428 | 3.8428 | 3.8286 | 3.8286 | 3.7714 | 3.7714 | 3.5571 | 3.5571 | 3.4143 | 3.4143 | 3.2286 | 3.2286 | 3.2286 | 3.2286 | 2.5571 | 2.5571 | 2.7429 | 2.7429 | 1.6143 | 1.6143 | 1.2714 | 1.2714 | 0.96667 | 0.96667 | 0.85 | 0.85 | 0.568 | 0.568 | 0.435 | 0.435 | 0.435 | 0.435 | 0.303 | 0.303
LIBS induced outgassing not always apparent – example of 1 µm porous WO on Mo exposed to D2 plasma in Magnum PSI

## Slide 4: Motivation
Magnum-PSI
TEAC (Target Exchange and Analysis Chamber)
LIBS + NRA/RBS
Experimental validation?
NRA fresh surface
new NRA at LIBS spot
D (at.%)
Depth (nm)
Nuclear Reaction Analysis (NRA) for D depth profiles

## Slide 5: Feasibility of the approach?
Depth resolution and sensitivity of NRA is sufficient?
Relative importance of ordinary outgassing?
D retention is sufficiently uniform along the surface?
LIBS crater with diameter 1 mm is comparable with NRA area (0.5x0.5 mm)

## Slide 6: Experimental setup
Magnum-PSI plasma parameters
6 slm D2 plasma
Exposure time 3000 s
Magnetic field 0.6 T
Voltage -40 V
Electron temp. Te ≈ 1 eV
Electron density ne ≈ 2.6·1019 cm-3
Plasma beam FWHM ≈ 21 mm
Surface temp. ≈ 160/255°C
Laser beam
TEAC
Magnum-PSI
Spectrometer
Mirror
Fiber
Sample holder
Ion-Beam channel for NRA/RBS
Notes: Low surf temp for high D retention

## Slide 7: Experimental setup
Laser beam
TEAC
Magnum-PSI
Spectrometer
Mirror
Fiber
Sample holder
Ion-Beam channel for NRA/RBS
LIBS at TEAC
1064 nm, 8 ns ja 180/760 mJ (fluence 14/7 J/cm2)
Delay time 1300 ns and gate width 2000 ns
Pressure 1 mbar Ar
Spectral window 10 nm around 656 nm Hα line
Larger LIBS spot size for NRA!
NRA
LIBS
LIBS crater 1 mm
NRA area 0.5 mm
new LIBS crater 3 mm
NRA
LIBS
Notes: Usually NRA measurements 2-3 mm outside from the crater

## Slide 8: Experimental setup
Laser beam
TEAC
Magnum-PSI
Spectrometer
Mirror
Fiber
Sample holder
Ion-Beam channel for NRA/RBS
NRA (in-situ in TEAC, 4-8 dec.2024)
2300 keV, 0.5 x 0.5 mm, (α = 41°)
RBS: depth limit 0.9 μm
NRA: depth limit 1.8 μm
NRA (ex-situ in IBAS, 13 and 18 dec.2024)
2300 keV, 0.5 x 0.5 mm (α = 0°)
RBS depth limit 1.4 μm
NRA depth limit 3.1 μm
Notes: Usually NRA measurements 2-3 mm outside from the crater

## Slide 9: Investigated samples and SEM/EDX measurements
c-W
p-WO
EDX:
66%W, 34% Mo
EDX:
24%W, 76% O
Center of crater
Center of crater
1 μm compact W (c-W) on Mo substrate (160 °C)
1 μm porous WO (p-WO) with 150 nm c-W interayer on Mo substrate (255 °C)
10 µm
10 µm
1 mm
1 mm

## Slide 10: RBS results for W and O concentrations
c-W coating
W and Mo are mixed after first shot (60%-40%)
O increased from initial 0-3% to 20 %
Crater depth can’t be determined
Chart: Energy (channels)
Chart: Energy (channels)
p-W coating
Crater depth 300-400 nm when assuming 50%W-50%O

## Slide 11: LIBS induced D outgassing in c-W coating (NRA)
Strong LIBS induced outgassing
D diffusion into c-W coating
Comparable results by TEAC and IBAS (made a week later)
D depth profiles at 3 spots quite similar
1330
443
1773
0
Depth (nm)
886
Chart: Depth (1015 D/cm2)
| 0 | 3201.1089999999999 | 3201.1089999999999 | 6311.9390000000003 | 6311.9390000000003 | 16208.633 | 16208.633
 | 4.9848 | 4.9848 | 2.8496 | 2.8496 | 0.2476 | 0.2476 | 0.0001
 | 5.0044 | 5.0044 | 2.4405 | 2.4405 | 0.4632 | 0.4632 | 0.0001
 | 5.0675 | 5.0675 | 2.9393 | 2.9393 | 0.2072 | 0.2072 | 0.0001
 | 0.0009 | 0.0009 | 1.0776 | 1.0776 | 0.293 | 0.293 | 0.08 | 0.08 | 0.0001
 | 0.0567 | 0.0567 | 1.1975 | 1.1975 | 0.4114 | 0.4114 | 0.22 | 0.22 | 0.0001
 | 0.0348 | 0.0348 | 1.1004 | 1.1004 | 0.4196 | 0.4196 | 0.088 | 0.088 | 0.0001
1330
443
1773
0
Depth (nm)
886
Chart: Depth (1015 D/cm2)
| 0 | 3761.0210000000002 | 3761.0210000000002 | 6636.902 | 6636.902
 | 4.2607 | 4.2607 | 2.0619 | 2.0619 | 0.0001
 | 4.2501 | 4.2501 | 1.8746 | 1.8746 | 0.0001
 | 4.3168 | 4.3168 | 2.2003 | 2.2003 | 0.0001
 | 0.0109 | 0.0109 | 0.7527 | 0.7527 | 0.8491 | 0.8491 | 0.48 | 0.48 | 0.24 | 0.24 | 0.04 | 0.04
 | 0.0143 | 0.0143 | 0.6659 | 0.6659 | 0.8554 | 0.8554 | 0.755 | 0.755 | 0.42 | 0.42 | 0.17 | 0.17 | 0.0001
 | 0.0159 | 0.0159 | 0.7564 | 0.7564 | 0.9329 | 0.9329 | 0.5 | 0.5 | 0.22 | 0.22 | 0.042 | 0.042 | 0.0001
Chart: Average D in 250 nm (at. %)
| before | after
TEAC | 2.74 | 0.33723
IBAS | 2.67 | 0.21667

## Slide 12: LIBS induced D outgassing in p-WO coating (NRA)
Strong LIBS induced outgassing
Somewhat thicker D deficient layer in p-WO
considerably lower D by IBAS (made a week later) – ordinary D outgassing
D depth profiles at 3 spots vary more for p-WO coating
1330
443
1773
0
Depth (nm)
886
Chart: Depth (1015 D/cm2)
| 0 | 2404.587 | 2404.587 | 8429.9969999999994 | 8429.9969999999994 | 26140.95 | 26140.95
 | 1.0535 | 1.0535 | 0.3093 | 0.3093 | 0.0251 | 0.0251 | 0.0001
 | 1.5243 | 1.5243 | 0.1053 | 0.1053 | 0.0154 | 0.0154 | 0.0001
 | 1.7067 | 1.7067 | 0.1146 | 0.1146 | 0.015 | 0.015 | 0.0001
 | 0.0035 | 0.0035 | 0.2071 | 0.2071 | 0.0197 | 0.0197 | 0.0001
 | 0.0202 | 0.0202 | 0.2082 | 0.2082 | 0.0191 | 0.0191 | 0.0001
 | 0.1686 | 0.1686 | 0.204 | 0.204 | 0.0152 | 0.0152 | 0.0001
1330
443
1773
0
Depth (nm)
886
Chart: Depth (1015 D/cm2)
| 0 | 4196.6679999999997 | 4196.6679999999997 | 9276.9699999999993 | 9276.9699999999993
 | 3.1193 | 3.1193 | 0.899 | 0.899 | 0.001
 | 3.5019 | 3.5019 | 0.9597 | 0.9597 | 0.001
 | 0.0432 | 0.0432 | 0.9979 | 0.9979 | 0.2717 | 0.2717 | 0.017 | 0.017 | 0.001
 | 0.0381 | 0.0381 | 0.7601 | 0.7601 | 0.2312 | 0.2312 | 0.03 | 0.03 | 0.001
 | 0.0272 | 0.0272 | 0.4461 | 0.4461 | 0.1269 | 0.126 | 0.001
Chart: Average D in 350 nm (at.%)
| before | after
TEAC | 0.995 | 0.265
IBAS | 0.17633 | 0.1014

## Slide 13: LIBS results
Chart: Wavelength (nm)
c-W
p-WO
Chart: Wavelength (nm)
W line intensities are considerably larger in the case of large crater
W and D intensities are comparable for different craters
Chart: LIBS intensity (a.u.) NRA D concentration (at.%)
| c-W | p-WO
LIBS | 4.8325 | 3.53
NRA | 5 | 3.3
LIBS D intensity correlates with D concentration in 300-400 nm surface layer

## Slide 14: Summary
LIBS induced D outgassing can be studied in Magnum-PSI TEAC
ns-LIBS at relatively small fluence resulted in strong LIBS induced D outgassing in c-W and p-WO coatings
p-WO coating has considerable long-term ordinary outgassing
Mo/W mixing in the LIBS crater of c-W coating was an unexpected finding
CONCLUSION: experiments confirmed that actual D retention may be considerably larger than predicted by LIBS after 1st laser shots

## Slide 15: Future plans
Application of several consecutive LIBS shots to study the cumulative effect
Experiments with ps-LIBS with expectedly smaller LIBS induced outgassing
Investigate the effect in different types of W coatings
Thank you for your attention!