## Slide 1: Overview of recent ENEA-PoliMi contributions to plasma-wall interaction modelling in SP D
Gabriele Alberti, Politecnico di Milano
on behalf of F. Mombelli, C. Tuccari, A. Uccello, M. Passoni

## Slide 2: Overview of ENEA-PoliMi contribution in SP D
Production of He and Ar background plasmas with SOLPS-ITER for linear device GyM
SP D.1
SP D.3
ERO2.0 erosion studies including microscale morphology
ERO2.0 global modelling of erosion and migration in GyM
ERO2.0 modelling of L-mode and H-mode He plasma discharges in AUG
Links to WP TE
RT06
Links to SP B.1 and B.4
Links to
SP B.1
Links to
SP B.1

## Slide 3: Microscale morphology studies
Investigate role of roughness and morphology on W erosion
W films with different roughness produced under SP B.4 and exposed to He or Ar plasmas in GyM under SP B.1
AFM topography of samples imported in ERO2.0 for comparison
Simulation geometry: quadrangular volume above AFM topography
net erosion
=
particles leaving Z upper boundary
Compared to mass loss measurements

## Slide 4: Impact of surface roughness
No clear Yeff,norm dependence on average roughness Ra
Yeff,norm = normalised sputtering yield wrt flat surface
Good sigmoid fit using mean surface inclination angle δm
C. Cupak, et al. Applied Surface Science 570 (2021): 151204

## Slide 5: Impact of dynamic retention
Ar plasma, -70 V
x10
Generally lower absolute yields in He experiments than ERO2.0
He plasma
Role of dynamic He retention on sample surface and/or He bubble formation layer?
R. P. Doerner, Scripta Materialia 143 (2018): 137-141
R. Sakamoto et al., Nucl. Fusion 64, 036008 (2024)
Not observed (or significantly reduced) with Ar plasma
Use of 50-50 W-He SDTrimSP yields reduces observed discrepancy
(surface He observed in RBS measurements)

## Slide 6: Microscale morphology studies: conclusions & perspectives
G. Alberti, et al. "ERO2.0 modelling of nanoscale surface morphology evolution”, Nuclear Fusion 61.6 (2021): 066039
A. Uccello, et al. “Exploring the role of topography in the sputtering process of tungsten by GyM helium plasma”, Nuclear Fusion 65.5 (2025): 056006
Verification of mean surface inclination angle δm as better descriptor of sputtering dependence on topography
Support to estimation of dynamic retention impact on GyM erosion results
Next: model the erosion of B samples?

## Slide 7: Global erosion/migration simulations in GyM
Study GyM wall erosion and its impact on exposed samples
2D SOLPS-ITER He-plasma solution (from SP D.1) imported in 3D ERO2.0 volume using axial symmetry
GyM 3D walls and sample-holder (SH) drawn in CAD and imported in ERO2.0
Stainless steel (SS) composition of GyM wall included in ERO2.0 and compared to full-Fe assumption
(not further discussed here)
Negative bias voltage applied to sample-holder as in experiments (0-320V in absolute values)

## Slide 8: Effect of sample-holder (SH) inclusion
Impact of SH on Fe wall erosion
Low bias (0 V): negligible effect
High bias (320 V): noticeable wall erosion close to SH due to sputtering of Mo mask
Impact of Fe wall/Mo mask eroded impurities on sample erosion
Low bias (0-50 V): no He plasma erosion, net deposition on samples
High bias (200-320 V): He plasma erosion dominated
Close to He sputtering threshold (120 V): non negligible erosion from Mo

## Slide 9: Comparison with experiments
SH
Plasma-facing side
Back
Cr deposition on catcher 2
Experimental
ERO2.0
Approach
Migration experiment: erosion of the exposed target and re-deposition on Si wafers (catchers)
Preliminary simulations using background plasma from SOLPS-ITER SP D.1 activity to optimize the exp. setup (target material choice, exposure time, biasing voltage, catchers positioning...)
Experiment performed under SP B.1
Results
Final setup: two Cr coatings exposed to Ar for 5 hours in total at –70V, with catchers shown in figure
Factor ≈1.5 higher erosion rate of Cr target in modelling compared to exp.
Good agreement in terms of deposited Cr thickness on catcher 2 (30-40 nm) and screw shadow
Low deposition area due to screw shadow
100 nm

## Slide 10: Global simulations in GyM: conclusions & perspectives
Successful coupling between SOLPS-ITER and ERO2.0 in linear geometry for global erosion/migration studies
Mo eroded from biased mask identified as main impurity contributor to wall and sample erosion
G. Alberti, et al. "Global SOLPS-ITER and ERO2.0 coupling in a linear device for the study of plasma–wall interaction in helium plasma“, Nuclear Fusion 63.2 (2023): 026020
F. Mombelli, et al. "Numerical simulation of a helium plasma–material interaction experiment in GyM linear device through SOLPS-ITER and ERO2.0 codes" Nuclear Fusion 65.2 (2025): 026023
Next: apply this tool to BiGyM?

## Slide 11: Erosion/migration in AUG He-plasma discharges
Investigate AUG W divertor erosion in L- and H-mode He plasma discharges
150 - 250 nm net erosion
(2022)
50 - 100 nm net erosion (2019)
Deposition
zone
Picture from 2019 experiment
M. Rasiński et al. NME 37 (2023) 101539
A. Hakola et al. NF 64.9 (2024) 096022
T. Vuoriheimo et al. NME 41 (2024) 101766
2019 and 2022 experiments
Poloidal shift of a few cm between L- and H-mode outer strike-points (OSP)
Post-mortem erosion measurements via focused ion beam marking on W
Net erosion near L- and H-mode OSPs, net deposition in between but little info about He+/2+ contribution
SOLPS-ITER background plasmas from WP TE
ERO2.0 wall geometry
(toroidal symmetry)

## Slide 12: Erosion results in L-mode discharges
From SOLPS-ITER: 50-50% He+/2+ fraction close to OSP
erosion contribution of the two He ions?
Results of the comparison
Significantly lower erosion with full-He+ wrt SOLPS-ITER fraction
30% higher erosion for full-He2+ close to OSP
Erosion with (c) SOLPS plasma vs. (b) full-He+ and (a) full-He2+ cases (fixed ne)
(a)
(b)
(c)
Comparison with experiments
Fairly good approximation

## Slide 13: Erosion results in L-mode discharges
L-mode experiment (2019): 50-100 nm erosion near strike-point after 1024 He m-2 fluence
ERO2.0: 1-2 nm maximum erosion
Oxygen (O) used as proxy for impurities, 6+ charge (previous experience e.g. in WEST and coronal equilibrium)
O strongly impacts erosion even at 1% concentration
Stronger impact close to strike-point
BUT: good agreement only with too high concentration
Combination with other effects is needed (e.g. electron and/or ion temperature uncertainties)
See G. Alberti et al. arXiv:2506.03883
Effect of impurities in plasma

## Slide 14: Erosion results in H-mode discharges
H-mode experiment (2022): 150-250 nm erosion near OSP after 3.4 ∙ 1024 He m-2 fluence
M. Rasiński et al. NME 37 (2023) 101539
ERO2.0: 35 nm maximum erosion far from OSP, even including oxygen (inter-ELM phase)
Effect of ELMs
Assumptions: 1 keV He in OSP area, same flux as inter-ELM, 1 ms duration, ≈ 150 Hz (5 ms between ELMs)
Incidence angle as free parameter (close to magnetic, 80°- 87°)
Observations:
Net erosion during ELMs, net deposition in inter-ELM phase
Erosion peak: 120 nm close to OSP, net deposition in private flux region with 85° incidence
Good agreement with experiments
from exp.
A. Kirschner et al. NME 18 (2019): 239-244

## Slide 15: Erosion in AUG He-plasma discharges: conclusions & perspectives
He2+ dominates W erosion despite 50-50% He+/2+ fraction close to OSP
Important role of impurities (and other uncertainties) in L-mode,
of ELMs in H-mode
E. Tonello, et al. "Global modelling of helium Plasma-Wall Interaction experiments in ASDEX-Upgrade”, PSI-26 conference, oral
G. Alberti, et al. “Tungsten erosion and scrape-off layer transport modelling in L-mode helium plasma discharges in ASDEX Upgrade”, under review
Next: move to other scenarios of interest for ITER

## Slide 16: Thank you for your attention

## Slide 17: Impact of (110) crystallinity
MORPHOLOGY

## Slide 18: Impact of (110) crystallinity
Chart: Effect of (110) crystallinity
| Si Flat | Si 300 | Si 600 | Si 900
Amorphous OLD | 0.010693 | 0.006987 | 0.0072833 | 0.0062763
Amorphous | 0.0064658 | 0.0043987 | 0.0046185 | 0.0040664
Crystalline | 0.015978 | 0.0073945 | 0.0051537 | 0.0041531
Effect of mask shadowing

## Slide 19: RBS measurements of He static retention after exposure
By Iva Bogdanović Radović and Zdravko Siketić (RBI)
Ex. compact W sample
He retained in the first 30-50 nm for all exposed samples
Now samples at AMU for TEM analysis

## Slide 20
x2

## Slide 23: Impact of (110) crystallinity
GyM global simulations

## Slide 24: SOLPS-ITER He-plasma modelling in GyM

## Slide 25: SOLPS-ITER vs He-plasma LP data in GyM

## Slide 26
30% higher gross erosion for Fe wall wrt stainless steel due to Cr presence
SS composition (AISI 304L): 73% Fe, 18% Cr, 9% Ni

## Slide 27: SOLPS-ITER Ar plasma modelling in GyM
A good agreement with the experimental data is found for the following choice of the SOLPS-ITER free input parameters
Dn = 20 m2/s
χi,e = 1.50 m2/s
P = 240 W
albedo = 0.0176
λ = 3 cm
ne (m-3)
Te (eV)
Vpl (V)
Γ (m-2s-1)
R (cm)
R (cm)
exp
exp
exp
num
num
num
3U
4U
5U

## Slide 28: SOLPS-ITER Ar plasma modelling in GyM
Weakly ionized plasma, ionization fraction 2.39%
Ar+ is the only relevant plasma species
Arn+ (n ≥ 3) are virtually nonexistent
Average ion temperature: 0.11 eV
Average neutral temperature: 0.03 eV
Neutral pressure peaked at the targets, where recycling occurs
× 1013
× 1016
× 10-3
Ar+ density map (m-3)
Ar++ density map (m-3)
Neutral pressure map (Pa)

## Slide 29: Impact of (110) crystallinity
AUG global simulations

## Slide 30
Impact of He ion concentration on divertor erosion: analytical model
Simplified model to evaluate physical sputtered flux of W, Γero, as function of the fraction of He2+ ions:
Hypotheses
Te ≈ Ti , fixed jsat (if f =1, Γwall = 0.5 jsat )
He2+ erosion
He+ erosion
At low Te , erosion increases with the fraction of He2+
At high Te , erosion decreases with the fraction of He2+: sputtering yield is flat and ion flux reduction dominates

## Slide 31: The modelling approach
SOLPS-ITER: 2D multi-fluid (main species + n. impurities) + 3D kinetic neutrals
ERO2.0: 3D kinetic Monte-Carlo transport of eroded impurities on fixed background plasma
Validation of SOLPS-ITER background plasma against AUG experimental profiles
Evaluation of He ion concentration (He2+, He+) by SOLPS -ITER
Impact on erosion in the divertor area by ERO2.0
SOLPS-ITER / ERO2.0 coupling:
S. Wiesen et al. JNM 463 (2015) 480–484
X. Bonnin et al. Plasma and Fusion Res. 11 (2016) 1403102
J. Romazanov et al. Phys. Scr. (2017) 014018

## Slide 32: SOLPS-ITER results
OUTER DIVERTOR PROFILES
ASDEX-Upgrade
#41471
L-mode (2019)
H-mode (2022)
OUTER MIDPLANE PROFILES

## Slide 33
L-mode
Outer divertor
He2+
He+
H-mode
OSP
50% He2+ - 50% He+
@ OSP
Outer divertor
OSP
OSP

## Slide 34: ERO2.0 inputs

## Slide 35: Comparison with experimental data
FIB marking: 50-100 nm erosion near strike-point after 1024 He m-2 fluence
M. Rasiński et al. NME 37 (2023) 101539
ERO2.0: 1-2 nm maximum erosion (even considering Maxwellian distributions for incidence angle and energy)
Possible uncertainties
Te only benchmarked against median value of LP data
Ti not benchmarked in SOLPS
Presence of impurities (e.g. O)
Sputtering yields for redeposited W
Temperature variation
Stronger impact of Te due to 3q factor
Te effect closer to strike-point
Partial agreement only with unrealistically high Te

## Slide 36: Impact of uncertainties: light impurities in plasma
Assumptions
Oxygen used as proxy for light impurities
Concentration range: 0.1 – 10% (of ne )
Low (1+) and high (6+) charge states (from WEST experience and coronal equilibrium)
C. C. Klepper et al. PPCF 64 (2022) 104008
R. Dufresne et al. 2021 Monthly Notices of the Royal Astronomical Society 503 1976–1986
Oxygen impact
Mild effect for O+, even at high concentration
O6+ has strong impact close to strike-point
Partial agreement only with very high concentration (10%)
Combination of uncertainties is needed

## Slide 37
2*Te and 2*Ti

## Slide 38
Impact of other species in plasma in H-mode

## Slide 39
ELMs modelling
Assumptions (from Kirschner et al, NME 2019)
1 keV He in OSP area, same flux as no-ELM simulations
Incidence angle varied between 80° and 87° (close to magnetic)
1 ms duration
≈ 150 Hz (5 ms between ELMs)
2*ne in ELM phase (small impact on obtained results)
Particles traced through variable background plasma
Good agreement found with 85° incidence
ELM impact area around OSP (image from DTT but same idea)
H. Kumpulainen et al. NME 33 (2022) 101264