## Slide 1
LIBS vs LID-QMS @ JET
Analysis proposal for joint meeting
Ionuț Jepu, Anna Widdowson

## Slide 2: Outlook
  LID-QMS vs LIBS
  Common area for comparison
  Detailed pulse-based comparison plan

## Slide 3
LIBS – Laser Induced Breakdown Spectroscopy
LID-QMS – Laser Induced Desorption via QMS
LID-QMS
Fuel retention
LIBS
Material composition
Fuel retention
J. Likonen
M. Zlobinski

## Slide 4
W – coated CFC
Bulk W
Bulk Be
Be coated inconel
Inconel (vacuum vessel)
LIBS
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
4D
VW
Oct5
VW
Oct1

## Slide 5
W – coated CFC
Bulk W
Bulk Be
Be coated inconel
Inconel (vacuum vessel)
LIBS and LID-QMS common target location – OCT 5 Mod 14
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
X
Z
4D
VW
Oct5
VW
Oct1

## Slide 6
LIBS and LID-QMS common target location – OCT 5 Mod 14
6
14IWG1A
2019-23
LH14W 2011-23
LH14N 2019-23
14IWG1B
2011-23
RH14W 2011-23
RH14N 2019-23
14IWG3A
2011-23
LIBS spots
14ING1C
2019-23
14ING1D
2011-23
RE damage

## Slide 7
LIBS and LID-QMS common target location – OCT 5 Mod 14
7
14IWG1A
2019-23
LH14W 2011-23
LH14N 2019-23
14IWG1B
2011-23
RH14W 2011-23
RH14N 2019-23
14IWG3A
2011-23
LIBS spots
LH14W 2011-23
RH14W 2011-23
14IWG1A
2019-23
14IWG1B
2011-23

## Slide 8
LIBS and LID-QMS common target location – OCT 5 Mod 14
8
14IWG1A
2019-23
LH14W 2011-23
LH14N 2019-23
14IWG1B
2011-23
RH14W 2011-23
RH14N 2019-23
14IWG3A
2011-23
LIBS spots
Proposed LIDs for comparison
LH14W 2011-23
RH14W 2011-23
14IWG1A
2019-23
14IWG1B
2011-23

## Slide 9
Tile |  |  | Initial Pulse no. |  |  | Additional pulse no.(relatively same location) | 
HFGC (LH 14W) |  |  | 59 – 63 |  |  | 777 – 780 | 
Tile 1 (14IW G1B) |  |  | 808; 12 – 15; 73 – 74 |  |  | 786 (a repeat of 74) | 
Tile 3 (14IW G3A) |  |  | 809 – 811 |  |  | Same as above | 
Tile 4 (14BW G4A) |  |  | 75 – 77 |  |  | 787 – 788 | 
Tile 5 LBSRP_14WLH | C1 | Stack A | 20 |  | 20 | 765 | 
 |  | Stack B | 23 |  | 23 | 766 | 
 |  | Stack C | 26 |  | 26 | 768 | 
 |  | Stack D | 29 |  | 29 | 769 | 
 | C21 | Stack A | 40 |  | 40 | 770 | 
 |  | Stack B | 43 |  | 43 | 771 | 
 |  | Stack B (C12) |  |  | 34 |  | 
 |  | Stack C | 46 |  | 46 | 773 | 
 |  | Stack D | 49 |  | 49 | - | 
Tile 6 |  |  | NO LIBS on T6 | NO LIBS on T6 |  | NO LIBS on T6 | NO LIBS on T6
Tile 7 (14ON G7A) |  |  | 805 | 805 |  | - | -
Tile 8 (14ON G8A) |  |  | 802; 54; 57 | 802; 54; 57 |  | 775 (between 54 and 57) | 775 (between 54 and 57)
Tile 8 (2ON G8B) |  |  | 360 & 368 | 360 & 368 |  | No repeated pulses | No repeated pulses
Top of tile 8 (14ON G8A) |  |  | 51 | 51 |  | - | -
1
LBSRP_14W LH
C1 & C21
14BWG4A
14ON G7A
6
7
0
3
4
5
8
1
HFGC_LH 14W
14IWG1B
14IWG3A
14ON G8A
Divertor poloidal assessment (partially/fully completed)
part of PFMC contributions
Common area with LID-QMS experiment

## Slide 10
1
LBSRP_14W LH
C1 & C21
14BWG4A
14ON G7A
6
7
0
3
4
5
8
1
HFGC_LH 14W
14IWG1B
14IWG3A
14ON G8A
+ T4, 5, 7 and 8
Previous LIBS assessment done
Divertor poloidal assessment (partially/fully completed)
part of PFMC contributions

## Slide 11
DETAILED PULSE comparison
LIBS vs LID-QMS

## Slide 12
HFGC
LH14W (2011-23)
852
853
854
855
856
858
859
860
861
864
865
866
867
63
62
61
60
59
LID-QMS pulses: #105abc
LIBS pulses: #xy
HFGC LH14W (2011-23) |  | 
LID-QMS #no | LIBS #no | Comment
105852 | 63 | Poloidal assessment
105853 |  | 
105854 | 62 | 
105855 |  | 
105856 | 60 | 
105858 | 61 | Toroidal assessment
105859 |  | 
105860 |  | 
105855 | 60 | 
105866 |  | 
105865 |  | 
105864 |  | 
105867 | 59 | 
Proposal for LIBS vs LID-QMS joint analysis meeting
LIBS pulses completed from previous assessment
Toroidal
Poloidal

## Slide 13
HFGC
LH14W (2011-23)
852
853
854
855
856
858
859
860
861
864
865
866
867
63
62
61
60
59
LID-QMS pulses: #105abc
LIBS pulses: #xy
Proposal for LIBS vs LID-QMS joint analysis meeting
LIBS pulses completed from previous assessment
Toroidal
Poloidal
S coordinates
JET – ILW

## Slide 14
HFGC
LH14W (2011-23)
852
853
854
855
856
858
859
860
861
864
865
866
867
63
62
61
60
59
LID-QMS pulses: #105abc
LIBS pulses: #xy
HFGC LH14W (2011-23) |  |  |  | 
LID-QMS #no | S- coord | LIBS #no | S-coord | Comment
105852 | 40 | 63 | 52 | Poloidal assessment
105853 | 60 |  |  | 
105854 | 80 | 62 | 102 | 
105855 | 100 |  |  | 
105856 | 120 | 60 | 130 | 
105858 | -61 | 61 | -62 | Toroidal assessment
105859 | -50 |  |  | 
105860 | -39 |  |  | 
105855 | -22 | 60 | 0 | 
105866 | -6 |  |  | 
105865 | 11 |  |  | 
105864 | 32 |  |  | 
105867 | 53 | 59 | 54 | 
Toroidal
Proposal for LIBS vs LID-QMS joint analysis meeting
LIBS pulses completed from previous assessment
0
S-coordinate
Poloidal
40
80
120
142
0
-60
50
S-coordinate
Toroidal
Poloidal

## Slide 15
HFGC
RH14W (2011-23)
LID-QMS pulses: #105abc
LIBS pulses: #xy
HFGC RH14W (2011-23) |  |  | 
LID-QMS #no | LIBS #no | S-coord | Comment
NO LIDs | 70 | 50 | Poloidal assessment
NO LIDs | 69 | 73 | 
NO LIDs | 67 | 98 | 
NO LIDs | 65 | 125 | 
NO LIDs | 67 | 0 | 1st Toroidal assessment Area 1 – fuel removed by LIDs
Area 1 | 68 | -21 | 
NO LIDs | 64 | 54 | 2nd Toroidal assessment
NO LIDs | 65 | 0 | 
NO LIDs | 66 | -62 | 
Poloidal
Proposal for LIBS vs LID-QMS joint analysis meeting
65
64
66
68
69
70
67
LIBS trends comparison with LH14W (previous slide)
No LID-QMS data (4x4 squares) on this tile to compare
LIBS pulses completed from previous assessment
0
S-coordinate
Poloidal
35
80
120
142
0
-60
50
S-coordinate
Toroidal

## Slide 16
LID-QMS pulses: #105abc
LIBS pulses: #xy
14IW G1A (2011-23) |  |  |  | 
LID-QMS #no | S-coord. | LIBS #no | S- coord. | Comment
105868 | 186 | 72 | 187 | Poloidal assessment
105869 | 200 | NO LIBS |  | 
105870 | 214 | 71 | 215 | 
NO LIDs |  | 11 | 254 | 
105871 | 301 | 10 | 290 | 
NO LIDs |  | 8 | 306 | 
NO LIDs |  | 7 | 340 | 
NO LIDs |  | 807 | 395 | 
105875 | -63 |  |  | Toroidal assessment
105874 | -53 |  |  | 
105873 | -44 | 9 | -34 | 
105872 | -34 |  |  | 
105871 | -18 | 8 | -4 | 
Poloidal
Toroidal
Proposal for LIBS vs LID-QMS joint analysis meeting
9
8
10
71
72
11
7
807
868
869
870
871
872
873
874
875
LIBS pulses completed from previous assessment
14IW G1A (2019-23)
142
S-coordinate
Poloidal
186
226
214
200
301

## Slide 17
14IW G1B (2011-23)
LID-QMS pulses: #105abc
LIBS pulses: #xy
14IW G1B (2011-23) |  |  |  | 
LID-QMS #no | S-coordinate | LIBS #no | S-coordinate | Comment
105899 | 186 | 74 | 186 | Poloidal assessment
105900 | 200 |  |  | 
105901 | 214 | 73 | 214 | 
105923 | 240 | 15 | 253 | 
105924 | 266 |  |  | 
105925 | 294 | 14 | 280 | 
 |  | 13 | 320 | 
NO LIDs that low on the tile |  | 12 | 354 | 
 |  | 808 | 407 | 
Poloidal
Toroidal
Proposal for LIBS vs LID-QMS joint analysis meeting
13
14
73
74
15
12
808
899
900
901
923
924
925
LIBS pulses completed from previous assessment
142
S-coordinate
Poloidal
186
226
214
200
296

## Slide 18
LID-QMS pulses: #105abc
LIBS pulses: #xy
FULL pulse distribution MAP
LIBS pulses completed from previous assessment

## Slide 20
Proposal for LIBS vs LID-QMS joint analysis meeting
LID QMS area + LIBS pulse comparison
Proposed LIDs for comparison
LIBS points to compare
63
62
60
59
61
857(guide)
852
853
854
855
856
858
859
860
861
864
865
866
867
65
64
66
67
68
69
70
72
71
14
73
74
15
868
869
870
871
872
873
874
875
899
900
901
923
924
925
11
10

## Slide 21
Proposal for LIBS vs LID-QMS joint analysis meeting
For the comparison purpose ( due to the LID-QMS limitation)
the selected tiles are: HFGC LH&RH 14W;
14IW G1A; 14IW G1B (marked with )
+ T4, 5, 7 and 8
Previous LIBS assessment done
LID QMS area + LIBS spots
+ 4 extra points
+ 3 extra points

## Slide 22
Proposal for LIBS vs LID-QMS joint analysis meeting
LID QMS area + LIBS spots to be compared
Proposed LIDs for comparison
LIBS points to compare

## Slide 23: LID-QMS areal fuel retention at end of JET operations 19 & 20 December 2023
Assumptions:
AMU4 calibration factor used for AMUs
19/12/2023 AMU4 calibration factor used for 20/12/2023 data points
Calibration = Jump method