## Slide 1: JET LIBS data in the QMS region-HFGC LH14W (2011-2023)
Rongxing Yi et al.
Forschungszentrum Jülich GmbH, Institute of Fusion Energy and Nuclear Waste Management – Plasma Physics, Partner of the Trilateral Euregio Cluster (TEC), 52425 Jülich, Germany

## Slide 2: Outline
Fitting method
Results in the LID-QMS region(Module 14)
Conclusions

## Slide 3: Fitting method
Read spectral data, check if there is significant (6 times larger than noise)W line @ 657.39nm (pixel 840+-5)
Use the W line do calibration, pixel difference between H D T, other W lines and W 657.39 nm is solid
Give the pixel position to each peak and do voigt fitting(solid and shared gaussian part, Lorentz part only shared by HDT )
Do the fitting directly with H. Set the original value for H peak position(526-531) , get the fixed value,
Save all data, but in red color when signal intensity <6N(only when signal >6N, it is regarded good signal)
yes
no
Spectral fitting
T changed in 2 weeks experiment
Wavelength 6 pixels deviation
No solid initial value for H
W line interference make it difficult to find the accurate wavelength for H
Problems:

## Slide 4: Results in the LID-QMS region (Module 14)
Delay 4 us
Delay 8 us
Weak H signal in the first spectra
Significant H signal in the first spectra

## Slide 5: Results in the LID-QMS region (Module 14)
D empty position
1
10

## Slide 6: Results in the LID-QMS region (Module 14)
1
6

## Slide 7: Results in the LID-QMS region (Module 14)

## Slide 8: Results in the LID-QMS region (Module 14)

## Slide 9: Conclusions
  Conclusions
  Distribution of DT/HDT is different in different position. DT mainly exist in the initial 30 pulses
  Quantitative results is on going, but ratio should be very accurate
  Next
  We can integrate all LIBS signal in 1 position to get the total ratio, but due to the matrix effect, it may be not very accurate(weight of each pulse is unsure)
  We have several 8us spectra data, we can compare it if needed.

## Slide 10
Thanks for your attention!