## Slide 1: LIBS retention (T, D, H) measured at tile HFGC RH14W (2011-2023)
64_HFGC_RH14W - R1 C1
65_HFGC_RH14W - R1 C2
66_HFGC_RH14W - R1 C4
67_HFGC_RH14W - R2 C2
68_HFGC_RH14W - R2 C3
69_HFGC_RH14W - R3 C2
70_HFGC_RH14W - R4 C2

## Slide 2: LIBS retention (T, D, H) measured at tile HFGC RH14W (2011-2023)
Highest D ratio
1
11

## Slide 3: LIBS retention (T, D, H) measured at tile HFGC RH14W (2011-2023)
1
6

## Slide 4: Depth profiling of W and Ti by Littrow spectrometer