## Slide 1: Erosion studies on W-B layers in laboratories
R. Gurschl, M. Fellinger, B. Burazor Domazet, J. Brötzner, G. Nagy, R.A. Wilhelm and F. Aumayr
WPPWIE SP B Monitoring Meeting
10.10.2025
Deliverable 2025: Erosion rates of co-deposited W-and B-based model systems following exposure to controlled ion beams

## Slide 2: Experimental method
Utilization of a Quartz Crystal Microbalance (QCM)
Sauerbrey equation relates mass changes to eigenfrequency changes [1]
Mass changes (implantation, sputtering) are induced by ion irradiation (in this study 2keV Ar+, 2keV D2+)
Investigation of five samples with different W-B composition (Pure W, W:B ≈ 4:1, W:B ≈ 1:1, W:B ≈ 1:4, Pure B)
Elemental composition profiles obtained via ion beam analysis techniques at Uppsala University (UU)
2keV D2+ irradiation performed at elevated temperature (~150°C)
[1] G.Sauerbrey, Zeitschrift f. Physik 155 (1959)
Ions
α

## Slide 3: Results – 2keV Ar+ and D2+ irradiation

## Slide 4: Results – 2keV Ar+ and D2+ irradiation
Conversion from amu/ion into atoms/ion possible with assumption

## Slide 5: Conclusions & open questions
Conclusions:
  Amount of sputtered tungsten particles decreases with increasing boron concentration
  Beneficial for a fusion reactor because influx of high-Z impurities is reduced
Open questions:
  Investigation of temperature dependence of sputter yield
  Investigation of remaining disagreement between SDTrimSP data and experimental results

## Slide 6: Elemental depth profiles

## Slide 7: Pure W

## Slide 8: W:B ≈ 4:1

## Slide 9: W:B ≈ 1:1

## Slide 10: W:B ≈ 1:4

## Slide 11: Pure B

## Slide 12: Comparison – Ar

## Slide 13: Comparison – D2