## Slide 1
M. Rasinski, Ch. Baumann, K. Krieger, R. Dux, A. Hakola, J. Karhunen, V. Rohde, S. Samuli
W erosion and redeposition in AUG Ne seeded experiment

## Slide 2: FIB cross-section preparation
On each sample 2-4 FIB cross-sections with line marking were prepared
Cross-section examined after AUG Ne campaign to determine the erosion and redeposition
Results will be used for ERO 2.0 modeling
AUG exposure
H-mode and L-mode D plasma with Ne seeding
Set of W and Mo samples for each experiment
17mm
6 mm
2.5mm
2
1

## Slide 3
OSP
OSP
VIS
W
Mo
H-mode series – Mo I line intensity (5528 A)
x
x

## Slide 4: Results
H-mode
x
before
after
W
Erosion below 50 nm – not possible to measure due to technique sensitivity
Mo
Erosion ~ 50 nm
Deposition – if present to thin to be measured by FIB cross-sections. TEM required on selected location
W
Mo
x
W
Mo
50 nm

## Slide 5: Sp B.1 Exposure of W-nano samples to PSI-2 plasmas
O. Marchuk, M. Sackers, M. Rasinski, S. Brezinsek, A. Houben, M. Klein and A. Kreter
Forschungszentrum Jülich GmbH – Institute of Fusion Energy and Nuclear Waste Management - Plasmaphysik,
Partner of the Trilateral Euregio Cluster (TEC), 52425 Jülich, Germany

## Slide 6: Setup of Psi-2

## Slide 7: Spectroscopic studies on W-nano in PSI-2
5
Front optics of the LOS (#5, along the normal to the target) :
A3 sample was put to the top
The A3 sample was exposed to 25 minutes in Ar
Two type of lines:
Direct photons
reflected photons

## Slide 8: First results (A3)
Wavelength, nm
Variation in intensity /Sputtering yield
Variation in reflectance /optical properties
Some mistakes in the optical set-up were done for other targets. No data