## Slide 1
Analyses of Monoblock 28 and boronized samples from WEST
P. Tsavalas1, K. Mergia1, A. Lagoyannis1, M. Axiotis1, D. Papadakis1, M. Diez2, A. Benmoumen3, C. Martin3, I. Bogdanovic Radovic4, Z. Siketic4, E. Fortuna – Zaleśna5, M. Spychalski5, A. Hakola6
1National Center for Scientific Research “Demokritos”, Athens, Greece
2CEA, IRFM, F-13108 Saint-Paul-Lez-Durance, France
3Aix Marseille University, CNRS, PIIM, Marseille
4Ruđer Bošković Institute, Bijenička 54, 10000 Zagreb, Croatia
5Faculty of Materials Science and Engineering, Warsaw University of Technology, Woloska 141, Warsaw, 02-507, Poland
6VTT Technical Research Centre of Finland Ltd, Espoo, Finland

## Slide 2
ITER-like W-monoblock 28 from WEST divertor (Phase I)

## Slide 3
ITER-like actively cooled PFUs - MB 28
PFU#13
Plasma-exposed
12 mm
26 mm
30.7 mm
6 mm
Trailing edge (TE)
plasma
Leading edge (LE)
MB28
PFU#13
vertically misaligned of ~+0.3 mm

## Slide 4
Experimental Methods
2 mm
Leading edge
Trailing edge
Toroidal direction
Analysis along the toroidal direction
NRA/RBS (1.6 MeV D beam)
SEM with EDX
Optical profilometry
Tof ERDA (23 MeV 127I8+ )
Optical microscopy
FIB - SEM
National Center for Scientific Research “Demokritos”
Ruđer Bošković Institute
Aix Marseille University
Warsaw University of Technology

## Slide 5
Optical image & Roughness
Optical microscopy
4 Different zones observed optically (gray dotted lines)
Roughness
From LE to 17 mm: lower than non-exposed (smooth surface)
From 19 to 23 mm: similar to non – exposed (surface depressions)
Near TE: highest values (scratches)
TE
LE
Zone 1
Zone 2
Zone 3
Zone 4
LE
TE
Toroidal direction

## Slide 6
Zone 1
Zone 2
Zone 3
Zone 4
Fuel retention & material deposition
Zone 1
Low D and He retention
Low B, N, Cu and Fe deposition
Highest C deposition near LE
High W concentration
Zone 2
Highest fuel (D and He) retention
Highest B, N, Cu and Fe deposition
Zone 3
D & He retention decreases
B, N, Cu and Fe deposition decreases
Zone 4
Near TE: C & H deposition increase
Material deposition further decreases
fuel retention almost constant
Oxygen: large fluctuations

## Slide 7
Formation of deposition areas
Zone 2: Mainly covered by B, N, O and Cu rich areas
Zones 3: Deposition concentrated along linear grooves and depressions
Near TE: linear deposition parallel to TE
Surface Morphology
Formation of deposition areas
B
C
O
W
50 μm
Zone 2
10 mm
Near TE
LE
TE
Zone 3
300 µm
Zone 3
Elongated pointy objects
Artificial W coating
5 mm
~58o
LE
TE
Pointy objects (observed all over the surface)
Oriented: 50o - 60o angle between the long axis and the LE/TE
Max length of 25 μm
Length-to-width ratio from 2 to 4
Stratified structures with, in some cases, embedded dust particles
Cracks
Zone 1
250-300 m
~700 m
LE
Near LE
P. Tsavalas et al Nuclear Fusion (submitted)
TE
Cracks
Perpendicular to LE: length ~ 700 μm
Along grain boundaries, visible where there is no deposition
Erosion observed in Zone 1

## Slide 8
Motivation: In initial phase of ITER operations (SRO), the boronization will be toroidally non-symmetric
Recent simulations suggest strongly non-uniform B2D6
Aim: how (non-)uniform is B layer formation?
A. Gallo, PFMC 2025
Q4
Q3
Non uniform boronization performed in WEST
A. Gallo, PFMC 2025
Glow electrode
Spatially non-uniform boronization tested in WEST:
6 glow electrodes (anodes) on top LFS
3 (out of 6) diborane (B2D6) feed locations
bottom LFS Q1, Q2, Q3 (half of the torus)
Q1
Q2
Q3
Q4
Q5
Q6

## Slide 9
1
2
3
4
5
Sample holder | Pos | Side | Composition
Q3 | Pos 2 | A | Bulk W coated with Au
 |  | B | 
 |  | C | 
 |  | D | 
 | Pos 5 | A | 
 |  | B | 
 |  | C | 
 |  | D | 
 | bottom | Y | 
Q4B | Pos 2 | E | 
 |  | F | 
 |  | G | 
 |  | H | 
 | Pos 5 | E | 
 |  | F | 
 |  | G | 
 |  | H | 
 | bottom | Z | 
 | Pos 3 | F | Bulk Al coated with Au
Reference W |  |  | Bulk W coated with Au
W
W
W
1
2
3
4
5
W
W
W
Q3
Q4
Al
Pos 2
Pos 5
Side Y
Side Z
Pos 3
Boronized Samples
Collector Probes
Q4
Q3
    Q3 (B-rich region)
    Q4 (B-depleted region)

## Slide 10
Methodology – Spectra
Beam: deuteron
Energy: 1.4 ΜeV
12.5 mm Kapton between the sample and the detector
Sample Q4 pos 2 side H was measured exactly after the air exposure and 22 days later
RBS/NRA measurements:
Representative W sample spectra
Al sample spectra
11B(d,α0)
B
10B(d,p2)
10B(d,p4,5)
11B(d,α2)

## Slide 11
Elemental Amount
Boron
No dependence on probe & side; dependence on vertical position
~3.5 × more B in pos 5 than in pos 2
Bottom sides present similar & the highest values
Pos 3 (Al) similar with pos 2
Same amount after 22 days air expose
Carbon
W samples: similar amount with reference one
high C amount Pos 3 (Al)
Deuterium
Dependence on probe; dependence on vertical position only for Q3
Q3: ~3.5 × more D in pos 5 than in pos 2
Q3 bottom side Y: the highest amount
Low values for Q4 presenting max. variation by factor of 5
Oxygen
Q3: similar amount with reference independent on position
Q4: pos 5 & bottom side present 3 times more than pos 2 & reference
Pos 5
Pos 2
Boron
Oxygen
Pos 5
Pos 2
Deuterium
Carbon
Pos 5
Pos 5
Pos 2
Pos 2
Bottom sides
22 days later
22 days later
Pos 2
Pos 5
H2 after 22 days
Average pos 2
Average pos 5
Pos 3 (Al)
Reference
Bottom side Y
Bottom side Z

## Slide 12
D/B ratio & Conclusions
D/B ratio:
Q3: no dependence on side & position (~0.23)
Q4:
  almost no dependence on side
  dependence on position (pos 2 ~ 0.14 & pos 5 ~ 0.05)
Q1
Q2
Q3
Q4
Q5
Q6
Pos 2
Pos 5
Bottom
Bottom
D/B ratio
The non-symmetric feed locations B2D6 and symmetric glow elecrodes result in (Q3 & Q4 results):
Boron
Uniform deposition regarding side & region (probe)
Dependence on vertical position
No change after 22 days air exposure
Deuterium
Non-uniform deposition for different regions (probes)
Q3: No dependence on side; dependence on vertical position
Q4: small dependence on side; small variation with vertical position
22% decrease after 22 days air exposure

## Slide 13
Thank you for your attention