## Slide 1
WPPWIE SP B: Monitoring meeting, 10 October, 2025
Production of B reference layers
C. Porosnicu, P. Dinca, B. Butoi, O. G. Pompilian, C. Staicu, B. Solomonea, C. P. Lungu
IAP-Romania

## Slide 2
Previous expertise used for coatings within the facility was redirected to B
TVA Deposition system used for obtaining B (/W,etc). layers
2024 was dedicated in setup and coating recipe development and plasma charactherisation methods
Magnetron systems (1-5 available): RF, DC, HiPIMS, mp- HiPIMS, BP-HiPIMS
Thermionic vacuum arc
Picture of deposition system used for obtaining B (-W)-D/H/etc. layers
Picture of the coating system used for B(/W)-D (Ne, N, He) layer deposition
Picture of the coating system used for B-D (Ne, N, He) layer deposition
B/D coating process – available setups

## Slide 3
Picture of deposition system used for obtaining B (-W)-D/H/etc. layers
Picture of the coating system used for B(/W)-D (Ne, N, He) layer deposition
B/D coating process – available setups
Previous expertise used for coatings within the facility was redirected to B
TVA Deposition system used for obtaining B (/W). layers
2024 was dedicated in setup and coating recipe development and plasma charactherisation methods
Picture of the coating system used for B-D (Ne, N, He) layer deposition
Magnetron systems (1-5 available): RF, DC, HiPIMS, mp- HiPIMS, BP-HiPIMS
Thermionic vacuum arc

## Slide 4: Plasma characterisation - Ion energy measurements
RF plasma, Ion energy DF
RF plasma, Ion energy overview
Parameters varied
Ar/D ratio
RF Power
Pressure
BIAS Voltage
2024 was dedicated in setup and coating recipe development and plasma charactherisation methods

## Slide 5: Plasma characterisation - Ion energy measurements
RF plasma, Ion energy DF
RF plasma, Ion energy overview
Parameters varied
Ar/D ratio
RF Power
Pressure
BIAS Voltage
2024 was dedicated in setup and coating recipe development and plasma charactherisation methods

## Slide 6: Plasma characterisation - Ion energy measurements
HiPIMS Monopulse, Frequency, Voltage, Pulse duration
Positive pulse duration varried
Positive pulse voltage varried
B+Ar+D, Ar/D: 1/1,
Bipolar HiPIMS,
RF+HiPIMS+DC = ~90 types of plasmas
For each one we know:
Ion energy
Coating rate (Particle flux)
D/B ratio by TDS
Useful for recipe development and future production
2024 was dedicated in setup and coating recipe development and plasma charactherisation methods

## Slide 7: Results form the B layers production task in 2025 under SBP4
Pre-deposition. Calibration
Coating parameters
4x Si substrates
2 RF sources opperated at 100W each
Working pressure: 1x10-2mbar
Ar flow= 20sccm
D2 flow= 20 sccm
Measurements
SEM cross-section
In situ photo of the deposition
Cross-section-SEM results
TDS results (D concentration and quantity)
TDS

## Slide 8: Results form the B layers production taskin 2025 under SBP4
Thermal Treatment- 50oC- 500oC_Ramp 5oC/min
Deuterium quantity as a function of the thermal treatment
TDS result on B+D2_1050oC
Temperature (oC) | D released (at/cm2) | D released during the TT (%)
50 | 7.45E+14 | 0.01
100 | 8.25E+15 | 0.08
150 | 2.21E+16 | 0.22
200 | 2.98E+16 | 0.29
250 | 2.82E+17 | 2.76
300 | 1.06E+18 | 10.39
350 | 2.22E+18 | 21.76
400 | 3.24E+18 | 31.76
450 | 4.95E+18 | 48.53
500 | 6.45E+18 | 63.24
1050 | 1.02E+19 | 100.00
TDS measurement during Thermal Treatment
60 tungsten substrates 5x5 mm
2 RF sources opperated at 100W each
Working pressure: 1x10-2mbar
Ar flow= 20sccm
D2 flow= 20 sccm
Boron+D2(10%) 5μm
Preparation of 5x5 mm2 W samples coated with B+D2(10%)
Subject to thermal treatment post-coating
Sample holder
In situ photo of the deposition

## Slide 9: Results form the B layers production taskin 2025 under SBP4
12 tungsten substrates 10x10 mm
2 RF sources opperated at 100W each
Working pressure: 1x10-2mbar
Ar flow= 20sccm
D2 flow= 20 sccm
Sample holder
In situ photo of the deposition
Boron deposition (5μm) with and without D
Boron deposition (100nm)
8 tungsten substrates
Eurofer φ 40 mm - for permeation studies
2 RF sources opperated at 100W each
Working pressure: 1x10-2mbar
Ar flow= 20sccm
D2 flow= 20 sccm
In situ photo of the deposition
Analisys (TDS, XRD,SEM, etc.) was be performed.
Samples sent - sealed bags in vacuum
All samples were stable after the deposition (at least before shipping)

## Slide 10: XPS on tungsten-boride formation
Si2-6_340 nm | B1s | C1s | O1s | W4f | B/W
0.0 min sputtering | 15.1 | 45.3 | 32.9 | 6.7 | 2.3
0.5 min sputtering | 45.9 | - | 38.8 | 15.3 | 3.0
1.0 min sputtering | 58.3 | - | 15.8 | 25.9 | 2.3
5.0 min sputtering | 63.0 | - | 13.5 | 23.5 | 2.7
10.0 min sputtering | 63.3 | - | 13.1 | 23.6 | 2.7
Elemental relative concentrations (at. %)
Request for tungsten boride layers from Penn State University (A. Marin) under a PSU - WEST collaboration.
Samples coated by TVA – task performed.
TVA parameters variation- W/B coatings with and without boride formation

## Slide 11: 2025 Status report of the B coatings at IAP under SBP4
1. Boron coatings with controlled deuterium inclusions (10 at%) - Completed : End of February 2025
B+D2 (10 at%) with a nominal thickness of 5 um deposited on W (5x5 mm). Exposure to distinct temperatures 50 – 500 oC
Measurements performed on the samples: TDS and SEM
Sample sent to: CEA_France (10 pieces), JSI_Slovenia (10 piece), NCSRD_Greece (10 pieces), RBI_Croatia (10 pieces), VTT_Finland (10 piece)
2. Boron Layers with a nominal thickness of 100 nm - Completed : End of February 2025
100 nm boron layers deposited on W (10x10 mm ) and Si substrates (2025
Measurements performed on the samples: SEM
Sample sent to: DIFFER_The Netherlands (1 piece Si, 1 piece W), CEA_France (1 piece), FZJ_Germany (1 piece), IPPLM_Poland (1 piece), IST_Portugal (1 piece), JSI_Slovenia (1 piece), NCSRD_Greece (1 piece), VR_Sweden (1 piece), VTT_Finland (1 piece), CIEMAT_Sapin (1 piece)
3. Boron Layers with a nominal thickness of 5 um - Completed : March 2025
5um boron layer deposited on Ø 40 Eurofer substrate, W(10 x10 mm) and Si substrate
Measurements performed on the samples: SEM
Samples sent to : JSI_Slovenia (1 piece Eurofer ), CEA_France (1 piece Si),JSI_Slovenia (5 pieces W), IST_Portugal (1 piece W), CIEMAT_Spain (1 piece W)
4. Boron Layers with controlled D ratio (10 at%) - Completed : March 2025
5um B+D (10 at%) layer deposited on Ø 40 Eurofer substrate, W(10 x10 mm) and Si substrate
Measurements performed on the samples: SEM
Samples sent to : JSI_Slovenia (1 piece Eurofer ), CEA_France (1 piece Si),JSI_Slovenia (5 pieces W), IST_Portugal (1 piece W), CIEMAT_Spain (1 piece W)

## Slide 12: 2025 Status report of the B coatings at IAP under SBP4
Planned until the end of 2025
Deposition of pure boron layers with a nominal thickness of 100 nm and 5 um on W(12 x 15 mm) substrates – (Deadline: September 2025) substrates to be received from Rodrigo
Deposition of B+D2 (10 at%) with a nominal thickness of 100 nm and 5 um on W(12 x 15 mm) (Deadline: September 2025) - ongoing
Deposition of B (5 µm) on Mo (⌀30 mm, 3 pcs) (Deadline : September 2025)- Mo substrates just received
Boron coatings with controlled deuterium inclusions (10 at%). Exposure to distinct temperatures 50 – 500 oC. (Deadline: January 2026)
Problems:
Two turbo-pumps failures in August and September. One was replaced, activity re-started.
The remaining tasks planned until the end of 2025 are on track, there are no issues to report concerning the sample production. Some delays due to substrates delivery delay and pump failure(see above) but nothing to be worried.

## Slide 13
  Different aproach than under SPB: Focus on plasma parameters instead of coating properties.
  For each set of parameters, very well defined plasma characterization
  Ionisation degree (Langmuir probe), Ion energy (IEDF), species identification (MS, OES), etc.
  Sistematic study
  Fixed plasma parameters – well characterized plasma => what will we obtain??
  stability, morphology, composition, adhesion, hardness, fuel retention
  Work plan has to be established by SP Leaders under SPB, SPC, SP D, SPX and SPF since the need of a “database of artificial B layers for physics studies: stability, fuel content, and release”
Prospects for studying B layers under SPF
Proposal of an experimental plan - Example and ideas:
Parameters to be varied: |  | 
RF-MS parameters (Input power) |  | Pressure (1e-03 – 1e-01 mbar)
HiPIMS MP and BP plasma parameters (Pulse duration and frequency, voltage for negative and positive pulse) |  | Acceleration voltage (0 to-200V for MS;-700V for TVA),
TVA parameters (voltage and current) |  | D/Ar ratio (1/20 – 1/1)