## Slide 1
WPPWIE SP B: Monitoring Meeting, 10 October 2025
Ion-beam measurements of B layers and other samples at IST
Rodrigo Mateus, Norberto Catarino,
Rui Silva, Sérgio Magalhães, Eduardo Alves
Notes: Please Indicate your subproject

## Slide 2: Analysis of WEST samples: core disks retrieved from lower marker tiles exposed along C3, C4, C5
S  242 mm / erosion-ISP
S  31 mm / thin deposition
nearby HFS
Erosion-deposition net
along the S-coordinate
after the C3 campaign
Locations of the EM tiles at the lower divertor of WEST
SIMS analysis at VTT
IBA experiment at IST following the SIMS points ;
simultaneous:
EBS + PIXE / 2.3 MeV 1H+ incident ion beams
RBS + NRA / 2.3 MeV 3He+ incident ion beams
Selected core disks:
C3-34iB , C3-34iK , C3-34iM , C3-22oE , C3-22oJ
C4-32iB , C4-32iK , C4-32iM , C4-20oE , C4-20oJ
C5-33iB , C5-33iK , C5-33iM , C5-21oE , C5-21oJ
(1) (2) (3) (4) (5)
M. Diez et al. Nucl. Mater. Energy 12 (2017) 559
M. Balden et al. Phys. Scripta 96 (2021) 124020
THIS WORK
Selected
core disks:
- Zone (5)
- Zone (4)
- Zone (3)
- Zone (2)
- Zone (1)
Erosion
Marker (EM)
tile

## Slide 3: Analysis of WEST samples: core disks retrieved from lower marker tiles exposed along C3, C4, C5
IBA quantification for D, B, C, O after C5 nearby OSP:
from the entire C5-21o tile
from the C5-21oE core disk
PIXE analysis:
superposition of Ni-K and W-LL peaks
evidence of Ni deposition
Fe:Cr:Ni contents  stainless steel
SIMS + EBS :
C5-33iM core disk (ISP)
erosion rate after C5  0.2-0.3 nm/s (7.3 h oper. in Phase 1)
PFMC-20 conference:
IST et al.,
Elemental analysis of divertor marker tiles
exposed during the 2018 (C3), 2019 (C4)
and 2020 (C5) WEST campaigns
Zone (4) , after C5
Notes: Ni-K (7.48 keV) and W-LL (7.39 keV)

## Slide 4: Reference B-based coatings for ITER and DEMO
Any evidence of fast oxidation of the B layers over time at RT
PhD student - scholarship from the Portuguese foundation
Fundação para a Ciência e a Técnologia (FCT)
Title of the thesis:
Oxidation behaviour of boron coatings for nuclear fusion applications
(collaboration with INFLPR)

## Slide 5: Reference W-based coatings for ITER and DEMO
IBA experiment :
simultaneous ERDA + RBS / 2.0 MeV 4He+ incident beams
EBS / 1.75 MeV , 2.15 MeV 1H+ incident beams
simultaneous RBS + NRA / 1.75 MeV 3He+ incident beams
IBA spectra under analysis
W-N
W-N-O
W-O
W-H-D
W-H
W-D
(110)
(200)
(211)
(220)