## Slide 1
Suppression of helium clustering in bcc W across temperature via dilute V alloying
Guanying Wei
14th Nov.2025

## Slide 2
He cluster fraction in Wvx and WTax

## Slide 3: Further verification

## Slide 4: He cluster distribution

## Slide 5: Self trapping

## Slide 6: Interaction between He-He and He-V/Ta

## Slide 7: Element around He

## Slide 8: Pressure-volume

## Slide 9: The presence of a small amount of V : 1.Suppresses He clustering at high temperatures (900-1500 K). 2. Inhibits He self-trapping and the creation of vacancy traps (Frenkel pairs). 3. Acts as a potent trapping site for mobile He atoms. 4. Creates stable, low-pressure "comfort sites" via elastic strain compensation.
Summary

## Slide 10: He release
Simulation setup
Cell: 40 × 40 × 60 bcc unit cells (~192,000 metal atoms)
He loading: 1,152 He atoms randomly placed within the central 60% of the box height (z-axis)
Vacuum: 3 lattice constants at the bottom, 20 at the top
Boundaries: non-periodic along z (open surfaces), periodic in x and y
Thermal protocol: ramp from room temperature to 850 °C over 50 ps (NVT), then anneal at 850 °C
Relaxation time: 2,200 ps for W; 1,750 ps for W–V
Results
W: He largely forms clusters; 23 He atoms are released to vacuum.
W–V: He atoms mostly vibrate near their initial positions; none are released.

## Slide 11: Screenshots