## Slide 1: Transmission Electron Microscopy of He ion implanted W-based HEA at IJCLab Stéphanie Jublot-Leclerc, Antoine Combrisson, Florian Pallier, Aurélie Gentils Université Paris-Saclay, CNRS/IN2P3, IJCLab, Orsay, France 14th November, 2025
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001
2024-2025
Contact: aurelie.gentils@ijclab.in2p3.fr

## Slide 2: Updated status on HerHEA work at CNRS-IJCLab (14th Nov. 2025)
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
Cutting of the bulk as-fabricated material
subcontractor in France for EDM cutting
Material fabrication at VTT
Materials sent to CNRS-CEMHTI and UHEL for ex situ ion implantation and characterizations
Available material(s) to be studied
W, W-Ta, W-Mo, W-V
Electrical Discharge Machining
3 mm diameter discs
squares
Polishing performed on W, W-V, W-Ta and the ternary alloys
WTaV, WTaMo
Mirror-polished samples (mid August / Sept.)
Other materials from Portugal
W-Ta-V, W-Ta-Mo
half discs
Quick SEM-EDX characterization
of binary alloys
Surface mechanical polishing

## Slide 3: Updated status on HerHEA work at CNRS-IJCLab (14th Nov. 2025)
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
Cutting of the bulk as-fabricated material
subcontractor in France for EDM cutting
Material fabrication at VTT
Materials sent to CNRS-CEMHTI and UHEL for ex situ ion implantation and characterizations
Available material(s) to be studied
W, W-Ta, W-Mo, W-V
Quick SEM-EDX characterization
of binary alloys
Surface mechanical polishing
Electrical Discharge Machining
3 mm diameter discs
squares
Other materials from Portugal
W-Ta-V, W-Ta-Mo
half discs
From literature: should be enough He to see bubbles in W  He bubbles observed in W by TEM starting 5x1015 cm-2 fluence (12 keV, 600°C), see F. Luo et al, Fusion Engineering and Design 125 (2017) 463, dx.doi.org/10.1016/j.fusengdes.2017.04.014
Selection of conditions and performing He implantation
High T°C (500°C), one high fluence (1x1017 He.cm-2)
Energy 100 keV
SRIM calculations using average Ed = 44 eV, see J. Byggmästar, F. Djurabekova, and K. Nordlund, Phys. Rev. Materials 8 (2024) 115406, https://doi.org/10.1103/PhysRevMaterials.8.115406
Notes: J. Byggmästar, F. Djurabekova, and K. Nordlund, Threshold displacement energies in refractory high-entropy alloys, Phys. Rev. Materials 8 (2024) 115406
https://doi.org/10.1103/PhysRevMaterials.8.115406

## Slide 4: Updated status on HerHEA work at CNRS-IJCLab (14th Nov. 2025)
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
Cutting of the bulk as-fabricated material
subcontractor in France for EDM cutting
Material fabrication at VTT
Available material(s) to be studied
W, W-Ta, W-Mo, W-V
Quick SEM-EDX characterization
of binary alloys
Surface mechanical polishing
Electrical Discharge Machining
3 mm diameter discs
squares
Other materials from Portugal
W-Ta-V, W-Ta-Mo
half discs
Selection of conditions and performing He implantation
High T°C (500°C), one high fluence (1x1017 He.cm-2)
Energy 100 keV
Samples attached on the implantation sample holder
Ion implantation performed
in Sept. 2025 using 190 kV IRMA ion implanter
He energy: 100 keV
He fluence : 1x1017 cm-2
Temperature of the samples: 500°C
Orsay
https://mosaic.ijclab.in2p3.fr
3 mm disc
WV
WTaV
WTa
W
WTaMo
From literature: should be enough He to see bubbles in W  He bubbles observed in W by TEM starting 5x1015 cm-2 fluence (12 keV, 600°C), see F. Luo et al, Fusion Engineering and Design 125 (2017) 463, dx.doi.org/10.1016/j.fusengdes.2017.04.014

## Slide 5: Updated status on HerHEA work at CNRS-IJCLab (14th Nov. 2025)
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
Cutting of the bulk as-fabricated material
subcontractor in France for EDM cutting
Material fabrication at VTT
Available material(s) to be studied
W, W-Ta, W-Mo, W-V
Quick SEM-EDX characterization
of binary alloys
Surface mechanical polishing
Electrical Discharge Machining
3 mm diameter discs
squares
Other materials from Portugal
W-Ta-V, W-Ta-Mo
half discs
Selection of conditions and performing He implantation
High T°C (500°C), one high fluence (1x1017 He.cm-2)
Energy 100 keV
Materials sent to CNRS-CEMHTI and UHEL for ex situ ion implantation and characterizations
TEM thin foils
preparation by FIB
(end Sept./Oct., IEMN and NCBJ)
FIB lift-out performed
at IEMN (D. Troadec) and NCBJ (D. Kalita)
250924_1015_WTaMo_G3
250924_1016_WTaV_G2
4C_W_1700X_0091
Pt protective layer
surface
depth
He ions

## Slide 6: Updated status on HerHEA work at CNRS-IJCLab (14th Nov. 2025)
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
Cutting of the bulk as-fabricated material
subcontractor in France for EDM cutting
Material fabrication at VTT
Available material(s) to be studied
W, W-Ta, W-Mo, W-V
Quick SEM-EDX characterization
of binary alloys
Surface mechanical polishing
Electrical Discharge Machining
3 mm diameter discs
squares
Other materials from Portugal
W-Ta-V, W-Ta-Mo
half discs
Selection of conditions and performing He implantation
High T°C (500°C), one high fluence (1x1017 He.cm-2)
Energy 100 keV
Materials sent to CNRS-CEMHTI and UHEL for ex situ ion implantation and characterizations
TEM thin foils
preparation by FIB
(end Sept./Oct., IEMN and NCBJ)
Observation if any He bubbles are seen
Transmission Electron Microscopy
ex situ (in October/November)
Cutting of the bulk as-fabricated material
subcontractor in France for EDM cutting
Material fabrication at VTT
Available material(s) to be studied
W, W-Ta, W-Mo, W-V
Electrical Discharge Machining
squares
Other materials from Portugal
W-Ta-V, W-Ta-Mo
half discs
Through focus series of bright field images showing bubbles
See details next slides
Beware ! Not the same scale (to be updated ;-) )
W
WTa
WV
WTaV
WTaMo

## Slide 7: Bright field TEM images of He-implanted W
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
underfocus
overfocus
surface
Pt protective layer
surface
! very thick foil – need further study
4C_W_100kX_0082 -500nm
4C_W_100kX_0080 +500nm

## Slide 8: Bright field TEM images of He-implanted W
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
surface
underfocus
overfocus
4C_W_280kX_0060 -500nm
4C_W_280kX_0062 +500nm

## Slide 9: Bright field TEM images of He-implanted WTa
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
G4_WTa_100kX_0081 -1.5 um
G4_WTa_100kX_0085 +1.5 um
underfocus
overfocus
surface
Pt protective layer
surface

## Slide 10: Bright field TEM images of He-implanted WTa
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
surface
G4_WTa_200kX_0091 -500nm
underfocus
overfocus
G4_WTa_200kX_0093 +735nm

## Slide 11: Bright field TEM images of He-implanted WV
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
underfocus
overfocus
surface
Pt protective layer
surface
G5_WV_100kX_0109 -735nm
G5_WV_100kX_0110 +735nm

## Slide 12: Bright field TEM images of He-implanted WV
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
surface
underfocus
overfocus
G5_WV_240kX_0118 +735nm
G5_WV_240kX_0120 -1.04nm
V homogeneity
to be checked later

## Slide 13: Bright field TEM images of He-implanted WTaV
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
G2_WTaV_100kX_0032 -1.59 um
G2_WTaV_100kX_0030 +1.59 um
underfocus
overfocus
surface
surface
Pt protective layer

## Slide 14: Bright field TEM images of He-implanted WTaV
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
G2_WTaV_280kX_0041 -750nm
G2_WTaV_280kX_0042 +750nm
underfocus
overfocus
surface

## Slide 15: Bright field TEM images of He-implanted WTaMo
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
underfocus
overfocus
surface
Pt protective layer
surface
G3_WTaMo_100kX_0056 -1.4um
G3_WTaMo_100kX_0058 +1.4um

## Slide 16: Bright field TEM images of He-implanted WTaMo
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
surface
underfocus
overfocus
G3_WTaMo_200kX_0065 -735nm
G3_WTaMo_200kX_0064 +735nm

## Slide 17: Updated status on HerHEA work at CNRS-IJCLab (14th Nov. 2025)
HerHEA project, EUROfusion, ENR-MAT.02.VTT-T001, 2024-2025
Cutting of the bulk as-fabricated material
subcontractor in France for EDM cutting
TEM thin foils preparation
by FIB
Material fabrication at VTT
TEM observation of
He bubbles
Selection of conditions and performing He implantation
High T°C (500°C), one high fluence (1x1017 He.cm-2)
Energy 100 keV
Analyse the experimental data
Interpretation / Comparison with other HerHEA results / Publication
M3.1  delayed to early 2026 ?
Materials sent to CNRS-CEMHTI and UHEL for ex situ ion implantation and characterizations
Electrical Discharge Machining
3 mm diameter discs
squares
Orsay
https://mosaic.ijclab.in2p3.fr
Quick SEM-EDX characterization
of binary alloys
Surface mechanical polishing
Available material(s) to be studied
W, W-Ta, W-Mo, W-V
Other materials from Portugal
W-Ta-V, W-Ta-Mo
half discs
Still lot of work to be done !