## Slide 1: PFCs concepts and qualification for the first wall PFCs (WPDIV)
M. Richou
CEA, IRFM
No task on first wall in WPDIV
Qualification of F4E components
Advanced PFCs : Goal sustain heat loads higher than the monoblock concept
Instrumentation (thermocouple) of normal heat flux components
This presentation: Focus on the qualification of F4E components

## Slide 2: Status on the qualification of F4E components
M. Richou
W transition meeting
28h of April 2026
ISM01_02_03
FSM00_01_02

## Slide 3: CONTENT
Procedure
Components
Results
M. Richou | W transition meeting | 28th of April 2026

## Slide 4: Qualification procedure
Non destructive testing
Ultrasonic testing (ENEA, RTC company)
Infrared thermography (CEA))
High Heat Flux test (Gladis (IPP), CEA (Hades))
At GLADIS:
  Screening (Increase of power) 6 – 10 MW/m²
  Cyclic loading, 100 x 10 MW/m², 10 s
  Screening 15 MW/m², 5 - 12 s pulse length
  Cyclic loading, 100 x 15 MW/m², 10 s
  High power transient loading, 3 x 20 MW/m²
AT HADES : High number of cycling (up to 2000cycles)
  Screening (Increase of power) 6 – 10 MW/m²
  Cyclic loading, 2000 x 10 MW/m², 10 s
  Screening at 5 MW/m²
Non destructive testing
Ultrasonic testing (ENEA, RTC company)
Infrared thermography (CEA))
M. Richou | W transition meeting | 28th of April 2026

## Slide 5: Components
Monoblock | HHF Tested
11_4 | 03/2025
14_5 | 01/2025
ISM | HHF Tested
ISM_01 | 09/25 (Gladis)
ISM_02 | 09/25(Gladis)
ISM_03 | 04/26 (Gladis)
FSM | HHF Tested
FSM_00 | 01/26
FSM_01 | 01/26
FSM_02 | 01/26

## Slide 6: Testing and results
Mock-ups | UT | SATIR | HHF | UT | SATIR
11_4 10 blocks |  | Bl10 | Bl 10 | Bl10 | Bl10
14_5 8 blocks |  |  |  |  | 
ISM_01 10 bl+ 5 TP |  |  |  | Bl 29 All FTs | Bl 29 All FTs
ISM_02 |  |  | Bl 2 | Bl 17; 10 All FT | Bl 16; 10 All FT
FSM_00 25bl +5 TP (W) |  | Bl 10;19;25 | Under inv. | ? | Under inv.
FSM_01 25bl +5 TP (W) |  | Bl 115; 20;23 All FTs | Under inv | ? | Under inv
FSM_02 25bl +5 TP (W) |  | Bl 615; 25 FT5 | Under inv | ? | Under inv
ISM_03 |  |  | Under inv | Planned | Planned
Not tested | Tested: Thermal imperefection detected | Tested No thermal imperfection | Tested Under inv. | Planned

## Slide 7: Monoblock (T1 2025)

## Slide 8: Monoblock 11_4
Mock-up HHF_SSM_11.4:
10 monoblocks
11.4 width per block
different blocks labeled ATM and RTC
Cold water cooling 15°C, flow 0.8 l/s
Screening 6 – 10 MW/m², up to 15 s pulse length, 15 MW/m², 5 s
Cyclic loading, 100 x 10 MW/m², 10 s – No evolution
Screening 15 MW/m², 5 - 12 s pulse length
Cyclic loading, 100 x 15 MW/m², 10 s – No evolution – B10 >B1
High power transient loading, 3 x 20 MW/m²
1
10
1
10
1
10
1
10

## Slide 9: Monoblock 14_5
8 monoblocks
14.5 mm width per block
different blocks labeled ATM and RTC
Cold water cooling 15°C, flow 0.8 l/s
Screening 6 – 10 MW/m², up to 15 s pulse length, 15 MW/m², 5 s
Cyclic loading, 100 x 10 MW/m², 10 s – No evolution
Screening 15 MW/m², 5 - 12 s pulse length
Cyclic loading, 100 x 15 MW/m², 10 s – No evolution
High power transient loading, 3 x 20 MW/m²

## Slide 10: (2) SATIR tests pre and post HHF
10
Imperfection still present after HHF tests
14_5
14_5
14_5
11_4
11_4
11_4
Imperfection with effect on thermal exhaust

## Slide 11: ISM (T2 2025 and T1 2026)

## Slide 12: ISM_02 and 01
Block and Flat tiles exposed
Higher temperature fo MB2
The first flat tile showed an increase ot the temperature of both edge during the cycling at 10 MW/m² - > Flat tile were screened
-> INFO FROM F4E: the company did not apply the planned manufacturing process for this particular mock-up
Only block exposed
Successful tests since temperatures are stable along cycle

## Slide 13: Non-destructive testing (Correlation with HHF tests ?)
 | GLADIS | SATIR | UT
ISM-01 | OK (FT not tested) | MB#2 to 9 FT#5 (larger) | From outside: MB#2 to 9 (detachement at Cu/CuCrZr) FT#all
ISM-02 | Failure Sign on MB#2 and FT#1 | MB#1; FT#1; FT#4 (larger) MB#2 to 6; MB#10 | No swirl – conventional method MB#1 (larger) MB#2 to 7; MB#10 FT#4 (larger) FT#all
Good correlation between SATIR and UT
Metallographic examination performed after HHF tests lead to confirm the Cu/CuCrZr detachment

## Slide 14: Test mock-up ISM-03 - Proposal (GLADIS, 2026)
ISM-03 manufacturing technologies and steps integrate the feedback from the other ISM fab. and test.
Non destructive testing (UT by ENEA)- OK
No sign of degradation after the completion of the HHF test
SATIR test post HHF and UT tests planned

## Slide 15: Full Scale mock-up

## Slide 16: High heat flux tests of full-scale mock-ups
FSM02
FSM01
FSM00
Potential thermal imperfection detected on SATIR before HHF tests
FSM02, loading 2x 10 blocks Mb5 &Mb14 and M12 & Mb21
FSM01, loading between Mb8 & Mb17
FSM00, loading on calibrated defaults, between Mb8 & Mb17
14s Beam ON (@10 and 15 MW/m²)
Mb1
Mb13
Up to 2600 c@10 MW/m² (Monoblock part)
Some cycles at 15MW/m² and 20 MM/m²
Flat tile
Mb8
Mb17

## Slide 17: Preliminar analysis
 | # cycles | Heat flux (MW/m²) | Duration on (s) | Duration off (s)
Blue framed zones | 685 | 10 | 14 | 66
Green framed zones | 685 | 10 | 14 | 16
 | 2 | 5 | 14 | 14
 | 3 | 15 | 14 | 14
 | 15 | 20 | 2 | 17
 | 2 | 5 | 14 | 14
Summary of heat loads on FSM1 for the different blocks
IR pictures during cool down phase, during the step related to the test at 20 MW/m²
Analysing the IR films, it is clear that this crack had appeared during 20MW/m² cycles, precisely the cool down phase. It appeared after the 3rd shot, and did not show large evolution during the cycles.
Results of SATIR tests pending
Sent to RTC (company) for examinations
M. Richou | W transition meeting | 28th of April 2026

## Slide 18: Nest steps
F4E qualification : finalise the analyses (SOFT + Publication outside conference )
Summary of the performance of the advanced concepts (BACM, TCM, SOFT)
2026 mid-term meeting in Garching 21st and 22nd of June (combined with WPDIV W7X)