## Slide 1: WP SP B.1 : Erosion studies for W and B layers on PSI-2 O. Marchuk, M. Sackers, M. Rasinski, M. Klein, S. Brezinsek, A. Houben, E. Warketin and A. Kreter
Notes: Please Indicate your subproject

## Slide 2: Plans for 2026: Exposition of W/B reference layers to PSI-2 plasmas
High resolution (HRS) and imaging spectroscopy (IS) of bulk and redeposited W and B layers in PSI-2
Study of sputtering rates of W+B layers in PSI-2
Analysis of B I and BD lines in UV and VIS at different flux of D
Discrimination between the chemical and physical erosion
Measurements of energy and angular distribution of B I lines
Erosion rates of W in linear cross machine comparison study by impact of different gases such as Ar or Ne.
Emission of BD molecules @ PSI-2
Time-of-Flight Experiments @PSI-2
Sputtering of W(poly) (solid lines) and W(111) (dashed lines) by Ne ions.
Emission of spectral lines from different excited levels will be analyzed.

## Slide 3
Operating range:
Chromatic aberration acts as a „filter“:
  New Focusing Lens (OptoSigma)
  1st order 499.6 nm cm
  2nd order 249.8 nm cm
High Resolution „Blue“ Spectrometer

## Slide 4
Tungsten W I 498.4 nm
Boron B I 249.7 nm
Status: Line shape of sputtered B
Dispersion from B HCL: 1.14 pm/px
Position of the lens depends on wavelength
Grating
Lens
to CCD
(motorized drive 2026)

## Slide 5: First HRS PSI-2 Spectra for B I Lines
We are trying to improve the statistic now by using other UV fibers

## Slide 6: Results Time-of-flight experiment
Incident energy: 86.5 eV
498.259 nm: Aij = 4.2e+05 s-1 τ = 1.9 μs 0.00000 – 2.48766 eV
505.327 nm: Aij = 1.9e+06 s-1 τ = 0.27 μs 0.20709 – 2.65995 eV
505.459 nm: Aij = 3.3e+05 s-1 τ = 3 μs 0.20709 – 2.65931 eV
Notes: Some physics to start with. Linien mit kleinem Einsteinkoeffizienten kommen früher, steilerer Anstieg.

## Slide 7
Comparison Between Poly- and Monocrystal Tungsten
We do not entirely see confirmation of the High-Res Result in the ToF result.
Further investigation still required.

## Slide 8: Plans for 2026: Exposition of W/B reference layers to PSI-2 plasmas
High resolution (HRS) and imaging spectroscopy (IS) of bulk and redeposited W and B layers in PSI-2
Study of sputtering rates of W+B layers in PSI-2
Analysis of B I and BD lines in UV and VIS at different flux of D
Discrimination between the chemical and physical erosion
Measurements of energy and angular distribution of B I lines
Erosion rates of W in linear cross machine comparison study by impact of different gases such as Ar or Ne.