## Slide 1
Analysis plan for WEST components at NCSRD
P. Tsavalas, A. Lagoyannis, M. Axiotis, K. Mergia
National Center for Scientific Research “Demokritos”, Athens, Greece
M. Diez and the WEST team
CEA, IRFM, F-13108 Saint-Paul-Lez-Durance, France

## Slide 2
Background
Plasma restart has been proven difficult on pristine, unboronised W wall at both WEST and AUG
Predictive simulations of glow discharge boronisation (GDB) performance for ITER require experimental validation
WEST simulations ‘predict’ 100x less B2D6 reactions in sectors 4-5-6 if only gas inlets in sectors 1-2-3 are utilized (left). If all inlets are utilized, toroidal symmetry is predicted (right).
Source: A. Gallo
B-rich area
B-depleted area
Q3
Q4
Pos 5
Pos 2
1
2
3
4
5
22 days later
No dependence on the toroidal location
1st non-uniform boronization at WEST
Boron

## Slide 3
2026 activities
Completed (Jan – Apr 2026)
Ion beam analysis of samples from 2nd non-uniform boronisation (4-5-6) in WEST using a 1.4 MeV deuterium beam
  Determination of B, D, O, N and C content as a function of vertical position on the probe (poloidal direction), toroidal location (rich and depleted B area), facing surface and substrate
  SEM image analysis of the boronised samples with EDX elemental mapping (in some samples non-uniform covering of B layer by the Au layer is observed)
1
2
3
4
5
Q3
Q4
Pos 2
Side Y
Side Z
Pos 3
A
B
C
D
E
F
G
H
W
SS
Al
Boron
Al
SS
Q1
Q2
Q3
Q4
Q5
Q6
Deuterium
SS
Al
Oxygen
Al
SS
Reference
B-rich area
B-depleted area
B-rich area
B-depleted area
B-rich area
B-depleted area

## Slide 4
On-going and planned activities
Contribution to PSI paper (Sehoon Ann)
1st and 2nd non-uniform boronisation (1-2-3 & 4-5-6) at WEST: Results post-processing and comparison of the two batches of boronised samples
Post-mortem analysis (ion beam analysis & SEM/EDX) of the 3rd batch of samples from uniform boronisation (scheduled for May 2026, samples to be delivered in summer)
Comparison of the results of all boronised samples
2026 planned activities