## Slide 1: WP PWIE SP B - kick-off meeting for 2026 activities SP B.2 - IBA capabilities for SP B samples (IST)
Rodrigo Mateus, Norberto Catarino, Rui Silva
Notes: Please Indicate your subproject

## Slide 2
JET chamber - EBS, RBS, NRA, PIXE, from small samples to full tiles
RBS/C chamber - EBS, RBS, NRA, small samples
m-probe – EBS, RBS, NRA, PIXE, PIGE, up to 75 mm long samples
JET
IBA laboratory of IST
Experimental JET chamber

## Slide 3
MB 25 - 30
MB 25
MB 26
MB 27
MB 28
MB 29
MB 30
Experimental measurements
IBA
2200 keV 1H+ , 2µC , 2 nA , EBS-PIXE
2200 keV 3He+ , 5µC , 8 nA , NRA-RBS
SP B.3 - Analysis of WEST PFU #484 / high fluence C7 campaign (2023)
z 118
z 105
z 93
z 81
z 69
z 37
Glass
Be
W+D
NbLiO3
56
28
42
49
35
z 25
z 130
PFU #484

## Slide 4
A
B
E
C
D
Chart: PIXE / MB 30
W-L
Chart: NRA / MB 30
2H(3He.p0)4He
Chart: EBS / MB 30
IBA and ion implantation of D2+ in W and B coatings / Oxidation behaviour of B coatings
MB 30
1 - Targets for LIBS depth profiling (prepared for delivery)
(Univ. Tartu , Comenius Univ.)
IBA and D implantation in W coatings (IST):
Step 1 - 150 keV D2+ / 2 x 1017 at./cm2
Step 2 - 75 keV D2+ / 2 x 1017 at./cm2
Step 3 - 50 keV D2+ / 1 x 1017 at./cm2
Four 5 m compact-W on Mo plates (IU-961-8/9/12/13 ; INFLPR)
Two 5 m porous-W on Mo plates (EU-156-12/15 ; INFLPR)
2 - PSI-27 conference (Comenius Univ., INFLPR, IST) / LIBS depth profiling
B and B+D co-deposited coatings on W and Si plates (INFLPR)
IBA and D implantation in B coatings (IST):
D implantation - Step 1 - 75 keV D2+ / 1 x 1017 at./cm2
- Step 2 - 50 keV D2+ / 1 x 1017 at./cm2
- Step 3 - 25 keV D2+ / 0.5 x 1017 at./cm2
3 - Study of Oxidation behaviour of B coatings (INFLPR , IST)