## Slide 1: LID-QMS, LIBS/LIA-QMS, TDS analysis and metallography of JET PFCs Plans for 2026, 2027
Miroslaw Zlobinski et al.
Forschungszentrum Jülich GmbH, Institute of Fusion Energy and Nuclear Waste Management – Plasma Physics, Partner of the Trilateral Euregio Cluster (TEC), 52425 Jülich, Germany
WP PWIE, SP E.3 Kickoff Meeting 29.5.2026

## Slide 2: in/ex situ retention comparison with LID-QMS, LIBS, LIA-QMS
Final Measurements at JET after last plasma in December 2023: Plan: direct comparison of ex situ to in situ LID-QMS in 70 positions ( ) on tiles retrieved from the torus
JET divertor tile 0 (= HFGC)
tile 1
Plan: ex situ LID-QMS ( ) and ex situ LIBS ( )incl. LIA-QMS around in situ laser spots
Ratio
Spatial distribution of H, D, T, C, W, …
Depth distribution
TDS on cut samples for temperature dependence
in FREDIS 2.0 (available 2027) upgrade plan:
LIBS and LIA-QMS (20 ps)
autoresonant ion-trap MS
ionisation chamber for T detection
better pumps
in situ ex situ
NEW
Metallographic cross-sections for layer thickness and structure, melting depth, crater depth
in situ LIBS

## Slide 3: Bulk-W Lamellae incl. potential W fuzz
Plan: Metallography for layer thickness and structure, W fuzz thickness and structure, melting depth of LID, crater depth of LIA/LIBS
inner wall facing marking
Poloidal gap surface
End
Plan: On full W lamella measure with LID-QMS and LIBS/LIA-QMS the full poloidal and radial profiles on all 4 plasma-wetted surfaces. Until now max. 3 radial measurements on the sides: cut lamella samples: TDS analysis for temperature dependence
Poloidal gap surface
X
X
plasma side
End
End
End
End
End
End
Retention mainly by co-deposition
Poloidal gap surface
X
Top surface = Plasma facing
Oral at PSI conference 21.5.2026 .
Ref: M. Zlobinski et al., PSI 2026: https://plan.events.mpg.de/event/187/contributions/2571/

## Slide 4: Metallography on bulk-W lamellae
W lamella cuts incl. molten laser spots were cut, polished, etched (to see the W grains) for optical microscopy of cross-section. SEM images of top surface done.
Panorama image with complete laser spot done. Plan: Repeat for new samples to be received incl. LIBS craters and LID-QMS spots
cutting done:
spot1 2
spot 1 2
3 4
5 6