## Slide 1: Introduction to SP F
Andrei Goriaev
LPP-ERM/KMS
WP PWIE SP F lick-off meeting

## Slide 2: PWIE SP F in 2026 - 2027
SP F: Wall conditioning and boronization physics
  SP F1: Boronization physics and fuel retention
    Boronization physics studies in ASDEX-Upgrade, WEST and laboratory devices
    Fuel retention studies for boronization development support in TOMAS
  SP F2: Wall conditioning plasma and diagnostics
    Wall conditioning plasma studies and diagnostic development in TOMAS
    In-situ diagnostics development for wall conditioning studies in TOMAS and linear plasma devices PSI-2 and BiGym

## Slide 3: SP F1: Boronization physics and fuel retention
Exposure of samples to non-uniform (half diborane injection points) boronizations in WEST and analysis of the characterization results
Exposure of witness samples on Laser-Blow-Off (LBO) manipulator during AUG glow discharge boronization (GDB) and characterization of boron (B) and deuterium (D) retention using ion beam analysis (IBA)
Analysis of long-term silicon (Si) samples by ion beam analysis (IBA) to determine the campaign-integrated spatial distribution of boron content and deuterium retention behavior for samples from experimental campaign 2025
Comparison of laboratory B and B-D layers with coatings generated in boronizations in fusion experiments
Boronization physics studies in ASDEX-Upgrade, WEST and laboratory devices
CEA
MPG
MPG
FZJ

## Slide 4: SP F1: Boronization physics and fuel retention
Exposure of hydrogen and deuterium doped boron-coated samples in TOMAS wall conditioning plasmas supporting boronization studies for ITER and W7-X
Production of hydrogen-dopped boron-coatings on W substrate in laboratory devices and supporting coating analysis for TOMAS and PSI-2 exposure experiments
Production of B:W:N:O layers with doped deuterium via ion implantation, followed by pre-characterization and post-mortem analysis after exposure in TOMAS wall conditioning plasmas
Fuel retention studies for boronization development support in TOMAS
LPP-ERM/KMS
FZJ
VR

## Slide 5: SP F2: Wall conditioning plasma and diagnostics
Exploration of optimal breakdown conditions and magnetic configurations for Electron Cyclotron Wall Conditioning scenarios for JT-60SA and ITER
Characterization and analysis of H and D mixed wall conditioning plasmas in TOMAS utilizing the improved data analysis methods for TOMAS plasma diagnostics
Study of the combined glow + microwave discharges and ICWC wall conditioning scenarios in TOMAS
Development of a thermal desorption probe for TOMAS wall conditions characterization
Adaptation of the multichannel broadband spectrometer for characterization of TOMAS wall conditioning plasmas
Wall conditioning plasma studies and diagnostic development in TOMAS
LPP-ERM/KMS
LPP-ERM/KMS
KIPT
KIPT
FZJ

## Slide 6: SP F2: Wall conditioning plasma and diagnostics
Production and characterization of boron-coated W samples with different boron thickness and deuterium concentration for LIBS studies in PSI-2
Commissioning of LIBS on BiGyM and first tests with boron-coated samples
Implementation of in-situ laser-based diagnostics on TOMAS
Further optimisation of LID-QMS in PSI-2 regarding sensitivity
In-situ diagnostics development for wall conditioning studies in TOMAS and linear plasma devices PSI-2 and BiGym
IAP
ENEA
FZJ
FZJ

## Slide 7: Structure of subproject meetings on 2026
PWIE SP F kick-off meeting 2026
  When: 23 June
  Where: On-line
  Format: 2 – 3 slides per task, 5 minutes (talk) + 3 minutes (Q&A)
  Aim: describe the planned work + any progress already achieved
PWIE SP F monitoring meeting 2026
  When: end of October
  Where: On-line
  Format: 2 – 3 slides per task, 5 minutes (talk) + 3 minutes (Q&A)
  Aim: show achieved progress + delayed or incomplete work
PWIE Report meeting 2026
  When: 16 - 19 November
  Where: Aix-en-Provence, France
  Format: 1 review talk of subproject leader + 2 – 3 highlight talks (per subproject)
  Aim: report on tasks assigned in 2026