## Slide 1
Jun 23, 2026 I Huace Wu
Implementation of in-situ laser-based diagnostics on TOMAS
WP PWIE SP F kick-off meeting

## Slide 2: 3D view
Two candidate optical ports for laser diagnostics
The ECRH magnetron will be removed
Two candidate optical ports for laser diagnostics
Sample chamber
Design of in-situ laser-based diagnostics

## Slide 3
The TOMAS sample chamber has been modified.
The center of sample holder can now be positioned at the vessel midplane.
Midplane
Two ports can be used to test direct laser ablation of samples.
Recent Vacuum Manipulator Modification

## Slide 4
LID-QMS laser parameters:
pulsed Nd:YAG laser (1064 nm)
Pulse duration: 0.1-20 ms
Peak power: up to 40 kW at 2.5 ms pulse duration
Pulse energy: up to 100 J for pulse durations above 2.5 ms
Repetition rate: up to 1 kHz, limited to a maximum average power of 500 W
1. The LID-QMS laser and optical fiber are ready for integration.
2. The laser beam quality meets current operating requirements.
3. The optical design for coupling the system to TOMAS has been verified.
ms-LID-QMS Set up (will be used for TOMAS)

## Slide 5
ps-LIBS Set up (will be used for TOMAS)
1. ps-laser has successfully passed the acceptance test and is ready for integration.
2. Its output energy and stability meet the requirements for LIBS measurements.
3. Beam-delivery layout and laser-safety system are being finalized.
Nucl. Mater. Energy (41) 2024, 101812 and (45) 2025,102018

## Slide 6
Preliminary Laboratory Demonstration of LID-QMS
1. A preliminary LID-QMS experiment was successfully completed in the laboratory.
2. LID-QMS was successfully demonstrated on thin boron layers deposited on tungsten substrates.
3. A desorption fraction above 90% was achieved at HFF >25 𝑀𝑊/𝑚².
D content ，D/B ratio
ITER-grade tungsten
Notes: We have also completed a preliminary laboratory demonstration of LID-QMS. In these experiments, amorphous boron–deuterium layers were prepared by magnetron sputtering. The layers were deposited on ITER-grade tungsten substrates. The samples had a deuterium areal density of approximately 10^17 𝑎𝑡oms/𝑐𝑚². The D/B atomic ratio was about 10 at.%.
For the investigated conditions, the desorption fraction exceeded 90 percent when the parameter HFF(Heat Flux Factor) was above approximately 25 megawatt square-root-second per square meter. This result provides a useful experimental reference point for defining the initial LID-QMS operating parameters in the future TOMAS experiments.

## Slide 7
Conclusion & Outlook
The TOMAS vacuum manipulator is being modified, with two candidate optical ports reserved for in-situ laser diagnostics.
The laser systems for both LIBS and LID-QMS are ready for integration.
LID-QMS has been successfully demonstrated on thin boron layers on tungsten substrates. Operating conditions for achieving more than 90% desorption have been identified.
Select the final optical port and confirm the available line of sight.
Finalize the optical paths and interface designs for LIBS and LID-QMS.
Complete installation, alignment, safety integration, and commissioning on TOMAS.