## Slide 1: SP B meeting on reference samples
Antti Hakola
On behalf of the SP B team and task holders
Results and needs for additional samples, 03 July, 2026

## Slide 2: Sample exposures in MAGNUM-PSI/UPP and PSI-2
MAGNUM-PSI/UPP
Task descriptions (actual ones – different from what is written in IMS):
  ”Expose B reference layers to MAGNUM-PSI/UPP plasmas for studying their sputtering yields as functions of temperature and ion energy and identifying the role of chemical erosion (DIFFER)” (2026)
  “Expose W/B reference layers to MAGNUM-PSI/UPP plasmas for studying the formation and erosion characteristics of thick B+W-based re-deposits (DIFFER)” (2027)
PSI conference: reports on chemical erosion of B-based layers and stability of thick B layers  Plans for late 2026? Needs for additional samples outside of DIFFER?
Erosion of 2D/3D W structures  status and plans?
NB! 9 WEST boronization samples (B/W, Au/B/SS, and Au/B/W) available for exposures in MAGNUM-PSI/UPP
PSI-2
Task description:
  ”Expose W/B reference layers to PSI-2 plasmas for investigating the role of sample composition on erosion and re-deposition yields including chemical erosion (FZJ)” (2026)
PSI conference and recent articles: reports on chemical erosion of B-based layers (spectroscopy) and removal of fuel/isotopic exchange in B layers
How about exposure of W samples into various plasmas (incl. Ar, Ne)? Also layers simulating re-deposits
Plans for late 2026? Needs for additional samples outside of FZJ?

## Slide 3: Sample exposures in GyM and laboratory conditions
GyM
Task descriptions:
  ” Expose W/B reference layers to GyM/BiGyM plasmas for determining the impact of sample composition on erosion yields (ENEA)” (2026)
  “Expose W/B reference layers to GyM/BiGyM plasmas for determining the role of layer thickness and structure (incl. porosity) in their sputtering as well as the formation of deposits (ENEA)” (2027)
PSI conference: reports on erosion characteristics of compact and porous B layers  Plans for late 2026? Needs for additional samples outside of ENEA?
From KoM minutes: FIB cross sectioning for B samples before exposure  action on Andrea
Lab investigations
Task description:
  “Assess the erosion characteristics of W and B reference layers upon exposure to different ion beams under laboratory conditions – focus on temperature dependence of sputtering (ÖAW)” (2026)
PSI conference and recent articles: sputter yield from mixed B+W layers and sputtering from W samples with different crystal structures and roughnesses  plans for late 2026? Needs for additional samples?

## Slide 4: Sample needs and analyses on toroidal devices
WEST
Most work connected with analysis of boronization samples and pieces cut from monoblock tiles  any needs for counterpart investigations using reference samples?
From KoM minutes: Rodrigo also put forward an idea for oxidization studies on B samples  action on Antti to establish synergies between VR and IST with similar ideas proposed
Samples from the first non-uniform boronization (Au-coated) can be provided for further measurements if needed
AUG
Concentrate on the analysis of (i) samples from melting experiments, (ii) marker samples from 2025 erosion experiment, and (iii) reference samples exposed during the recent boronization
Do we need any additional helping hands or other samples to complement ongoing experiments?
W7-X
From KoM minutes: (i) organize a larger gathering involving all key contributors, also labs analysing dust samples, to understand properly the outcomes, e.g., thick deposits and dependence of deposits on the B-field direction (CP, Antti) and (ii) CP requested thick (~a few microns) B layers for erosion studies on W7-X in the autumn
Any other needs for samples or requirements for analyses?

## Slide 5: Reference boron layers: status and needs
The round-robin exercise started in 2024-2025 is practically completed: the last remaining samples (by T. Vuoriheimo/Uni Helsinki) are ready and waiting for their shipment during the summer  are we satisfied with the results so far (incl. several PSI contributions, journal papers, overview manuscript by Antti,…)?
Plans put forward in the KoM:
  Uni Helsinki samples: send a subset of deposited layers to Raman measurements (Cedric)
  IAP samples: New ideas include (i) study the impact of the coating parameters/coating method on the properties of the B layers (structure, D retention/release,…) – use simple B+D layers; (ii) formation of B-W alloys – collaboration between IAP and IST (Bobi, Rodrigo); (iii) isotope exchange studies – complementary to Tomi’s work (Bobi, Tomi)
  ENEA samples: Compact thick B layers for permeation studies by Vinko (JSI); role of porosity in erosion and retention characteristics of the layers
  Plasma-exposed samples: study the role of D in the B layers (IBA, TDS) and perform XPS analyses for them (JSI)
Do we have other ideas in mind on what to produce, characterize and distribute to the partner labs?

## Slide 6: Reference W layers and LIBS samples: status and needs
So far only few ideas identified, including
  Varying the structure and crystallinity of the W layers for erosion studies  IAP, ENEA
  Continue producing standard W layers for cross-comparison experiments on linear plasma devices
Other ideas? Especially from the LIBS community?
Note that in the PMP we have the following activities identified
“…determining the role of layer thickness and structure (incl. porosity) in their sputtering as well as the formation of deposits”
“… investigating differences between bulk materials and layers resembling re-deposited material on sputtering characteristics”
“… the effective sputtering yields for samples with varying 2D/3D microstructure…”
“focus on temperature and structure dependence of sputtering”
Alternatively we may consider re-scoping the tasks to put more emphasis on B+W mixed layers!?