## Slide 1: SP B.1: Physics of erosion and deposition (ÖAW)
Plans for 2026
Task: Assess the erosion characteristics of W and B reference layers upon exposure to different ion beams under laboratory conditions – focus on temperature dependence of sputtering
Temperature dependence of sputter yield for 2 keV D2 found for the W:B = 1:1 sample
Planned for August: Conduct 2 keV Ar & 2 keV D2 irradiation on W:B = 4:1 and W:B = 1:4
No additional samples needed
Plans for 2027
Task: focus on structure dependence of sputtering
Idea: Irradiate rough WB compounds
Open question: can anyone produce rough WB layers on a Quartz Crystal Microbalance?