## Slide 1
Infrared Reflections Modeling
at WEST, ASDEX-U and W7-X
MH. Aumeunier1, J.Gerardin1, C. Talatizi1, R. Mitteau1, P. Drewelow2, Y. Gao2, M.Jakubowski2, A.Herrmman3, M.Faitsch3, M. Ben Yaala4, L. Marot4
EUROfusion Meeting on Image Processing and Artificial Intelligence, 25.02-26.02 2020 Greifswald
1 CEA Cadarache, 13108 Saint Paul-Lez-Durance, France
2 Max-Planck-Institut für Plasmaphysiks, 17491 Greifswald
3 Max-Planck-Institut für Plasmaphysiks, D-85748 Garching
4Department of Physics, University of Basel, Klingelbergstrasse 82, 4056 Basel, Switzerland

## Slide 2: The issue of IR measurement
The analysis of thermography measurement is difficult (often qualitative) and can lead to false interpretation
The quantitative thermography is not a direct problem. Achievement of the desired precision requires a perfect understanding of all “sources” phenomena (surrounding environment) up to the transfer function of instrument
This is not a real hot pipe
BB 100°C
R.Magritte « The Treachery of Images»
Simulated IR image
SPEOS CAAV5 © CEA
SPEOS CAAV5 © CEA

## Slide 3: IR Synthetic Diagnostic for helping image analysis
Reflection ?
Hot Target ?
Different levels of analysis
Qualitative purposes:
  Discriminate reflections from hot target
  Identify the origin of reflections (primary hot sources)
Quantitative analysis
  (3) Recover true surface temperature solving the emissivity inaccuracy & reflection contribution
WEST experimental image
Aim: predict & understand the impact of low and variable emissivity and reflections on PFCs surface temperature measurement
IR synthetic diagnostic applied to Tore Supra, JET, ITER devices
for improving IR image interpretation & anticipating measure accuracy
 Currently benchmarked with WEST, ASDEX-U, W7-x experiments

## Slide 4: A “digital twin” approach
IR synthetic diagnostic: an end-to-end simulation aiming to model all physical phenomenon involved in the IR measurement chain: from source to optical response of instrument
ITER Wide Angle Viewing Sytem
Synthetic IR images
Light propagation in 3D model based on Monte Carlo Ray Tracing (MCRT) code
(ANSYS-SPEOS CAAV5) getting all radiations of thermal scene
IR Source Modeling
Modeling of plasma heat loads deposited on PFCs (main IR source)
Modeling of resulting 3D temperature field
Materials Thermal-radiative Modeling
Emissivity model
Reflectivity Model
Optics Modeling
Camera model
Optical Transfer Function
1
2
3

## Slide 5: Prediction of true surface temperature on WEST lower divertor
Pulse Configuration (#53694)
2/3
1/3
Ptot=3,75 MW injected (assuming 40% conducted)
lq = 5mm; Ratio inner-outer : 0.33/0.67
3D surface T° computed from fast thermal reduced model (Modal Identification Method) including 3d heat diffusion learnt from Ansys calculation
3D deposited heat flux on divertor computed from field line ray tracing code based on optical approximation (parallel transport only)
3D Heat Flux
Wetted area
3D surface temperature
Magnetic Equilibrium at 3.05s
PFCFLUX output
MIM output

## Slide 6: Modeling of materials thermal-radiative properties
2 physical models to describe how photon is emitted and reflected …
Emissivity Model
Reflectivity Model
Bidirectional Reflectivity Distribution Function (BRDF)
(λ,θi,θo φi, φ o ,T)
Spectral Directional Emissivity
ελ'(λ,θo,T)
Directional hemispherical reflectance

## Slide 7: WEST Thermal scene Modeling
Mainly metallic materials with W-coating
2 reflectance models considered:
  Diffuse reflectance (or Lambertian reflectance)
  Highly specular reflectance roughly fitting with W-sample measurement in laboratory
Reflectivity follows a gauss distribution with increasing intensity at higher incident angle
Quasi-specular reflectance of W sample with specular lobe of small angular width: from 3° to 6° wrt roughness
Isotropic BDRF ( same behavior at φR=0° or 90°)
Measure of Bidirectional Reflectance W-samples in VIS & NIR at ambient T° (Basel University)

## Slide 8: Specular Reflectance models on WEST wall surface fits roughly with experimental images… in accordance with BRDF measure
Experimental IR Image
Simulated IR image
Case with high specular surface
simulated from W-sample measurement
Case with all diffuse surface
Brightness T° Map
Brightness T° Map
Brightness T° Map
WEST Pulse #55210

## Slide 9: Simulation helps to discriminate reflection features from thermal events
Reflection
Reflection from Q4 & Q5 low divertor
Reflection
Reflection from FCI outboard
Hot spot
Reflection from FCI outboard
Experimental IR Image
#Pulse 55210 @ 7s(Ip=500 kA, 4.4MW LH + 0.7MW FCI)
Simulated IR Image
Strike Point Splitting (not modeled)
ANSYS SPEOS CAA © CEA
ANSYS SPEOS CAA © CEA
Hot pipes
Hot pipes
Brightness T° Map
Brightness T° Map
Reflections
Reflections from FCI outbord
Reflection from Q3 low divertor
Reflection

## Slide 10: IR synthetic diagnostics helps to understand unexpected light pattern on WEST PFU fillet
WEST experimental IR image (zoom of equatorial camera in Q2A)
WEST synthetic image
Fillet
WEST PFU (W-coating)
Issue : Unexpected light pattern along the fillet of WEST PFU (trailing edge) observed on several IR cameras
IR modeling proves that light pattern on PFU fillet is
NOT a thermal event
NOT a reflection feature
DUE TO an unpredicted and variable thermo-radiative properties of WEST PFU… and especially due to the angular-dependent emissivity model which can change with the surface state (between PFU fillet vs top face)

## Slide 11: ASDEX-U Thermal Scene Modeling
Materials Properties Assumptions
Closed divertor geometry similar to ITER divertor more favourable to reflections (between targets facing each others)
ITER divertor (iter.org)
Projection mapping of experimental image on 3d geometry to establish the 3D temperature field of divertor used as input of photonic simulation
2D experimental image
(outer divertor target)
Recovered 3D T° distribution on one bulk tile
3D T° Field used as input of photonic model
3D Temperature Field
Fully metallic device

## Slide 12: ASDEX-U first results (ongoing work)
Experimental Image
Simulated Image
(high specular reflectance materials)
Reflection Map
= Reflected Flux / Total Flux
Outer target
Main reflections reproduced on dome, on lower divertor (colder area)
Thermal modeling used as input of MCRT is still a work in progress (strike point fitting, tiles misalignment)
Under investigation: light pattern along the fillet of inner divertor (a change of emission model as observed in WEST or real deposited heat flux, both ?)
Real hot target ?
Lower divertor
Lower divertor
Inner target
2
Reflections from outer target (primary reflections)
1
1
Reflections from outer target (secondary reflections)
2
Reflections from outer target
3
3
4
Reflections from inner target
4
#Pulse 32858 , MWIR camera (sector 9)

## Slide 13: W7-X Thermal Scene Modeling
Materials Properties Assumptions (OP1.2)
Major components in carbon graphite characterized by lambertian emission (ɛ~0.8) and diffuse reflectance
Stainless steel for outer wall shield and vacuum vessel characterized by low Lambertian emission (ɛ~0.3) and high specular reflectance
3D Temperature Field (used as input of MCRT)
Surface heat loads assessed on divertor island for a standard plasma scenario from field line ray tracing code [Y.Gao & al., Nuclear Fusion, 59 (6), 066007 (2019)]
Resulting surface T° computed from 1D thermal model (semi-infinite wall)
Uniform temperature assumed for the remaining in-vessel components

## Slide 14: W7-X first results (ongoing work)
Experimental Image (20180724_018_AEF20)
Simulated Image (with reflections)
W/m2/sr
ANSYS-SPEOS 2019 © CEA
Simulated Image (free-reflections)
Reflection Map = Reflected Flux / Total Flux
Reflections coming from lower H-target
Reflections
Identification of main reflection patterns and their origin
  >50% of reflected flux on CFC lower V-target (of which 50% coming from lower H target) causing a temperature error of 140% on the coldest target at 50°C (120°C measured)
  ~75 % of reflected flux on SS outer shield at 50°C (of which 50% coming from lower H target) causing a temperature error of 100%
  ~30-40% of reflected flux on CFC lower baffle at 50°C (of which 25% coming from upper H-target ) causing a temperature error of 30% (15°C)
Next steps:
  Adjustment of thermal radiative properties and camera model (e.g. distortions modeling)
  Application to camera used for OP2
Lower H-target
Lower baffle
Outer Shield
Heat flux patterns
Heat flux patterns

## Slide 15: Conclusions
IR synthetic diagnostic is a confident and useful tool to improve our understanding of IR images
BUT parameters used as input need to be used with caution and consolidated, especially thermal-radiative properties of materials
 Tricky task since multi-parametric model and with some parameters which impact the results in the same way (e.g. emissivity value & angular distribution of materials)
IR synthetic diagnostic application
  Currently used for helping IR interpretation at WEST, ASDEX-U and W7-X: discriminating reflections features to real thermal events, understanding & finding the origin of unexpected light pattern  consolidate the PFCs monitoring in all reflective & radiative environment
  To be used for quantitative measurement (thesis under going): development of inverse method based on radiometry model to retrieve the true surface t° by solving reflections contribution and inaccurate emissivity, in case of all diffuse surface (first results in ISFNT paper 2019, C.Talatizi)
  Outlook: Synthetic data base to be used in learning phase for pattern recognition algorithm ?