## Slide 1
Inferring component thermal parameters from the data stream coming from the infrared viewing diagnostic
February 25th, 2020
Raphael MITTEAU

## Slide 2: What kind of thermal parameters can be inferred from the temperature time trace ?
Can relevant thermal parameters of a hot spot be inferred (= deducted) from the temperature history ?
  Material health (good, bad, armour delamination)
  Presence / absence of co-deposit
  Component being well cooled or thermally insulated
All these information's are relevant for decision-making toward wall monitoring
Measures available from diagnostic systems :
Surface temperature (time evolution) of a given spot. Including some assumptions regarding emissivity, reflectivity etc…
Total power Ptot (time evolution)… but usually not the local power density qdeposited

## Slide 3: 4 thermal behaviours, all up to 1000°C
4 thermal behaviours, all calibrated on a prescribed temperature rise of 950°C (from 50 °C to 1000 °C)
All do corresponds to simulated thermal models of possible plasma facing components
The power deposition lasts 10 seconds, from 5 to 15 seconds
The heat flux density is unknown
0
500
1000
0
500
1000
0
500
1000
500
1000
0
10
20
30
40
Temperature (°C)
Time (s)
Power on
off
Feed forward modelling

## Slide 4: Qualitative human expertise
0
500
1000
0
500
1000
0
500
1000
500
1000
0
10
20
30
40
Temperature (°C)
Time (s)
Heating and cooling are quasi-symmetrical
Fast response to Heaviside power steps : low capacity material – Look likes a co-deposited layer
Poor up-down symmetry. Slow return to base temperature : visible effect of radiation cooling
Poor up-down symmetry. Slow ramp-up plus very slow return to base temperature
 thermal capacity being filled, radiation cooling
Heating and cooling ramps are quasi-symmetrical
+ good match to exponential behaviour
Probably a well cooled component

## Slide 5: Unveiling local power density
While identical max temp 1000°C, quite different power densities
Temperature : a poor indication of actual heat load
0
500
1000
0
500
1000
0
500
1000
500
1000
0
10
20
30
40
Temperature (°C)
Time (s)
1.7 MW/m²
3.9 MW/m²
0.5 MW/m²
8.9 MW/m²

## Slide 6: Unveiling thermal model
0
500
1000
0
500
1000
0
500
1000
500
1000
0
10
20
30
40
Temperature (°C)
Same as above with addition of low adherence deposit
W macrobloc with top heat load and blackbody cooling
10 mm
Thick plate with local heating
1 mm
Thin plate with uniform heating
1.7 MW/m²
3.9 MW/m²
0.5 MW/m²
8.9 MW/m²

## Slide 7: Provisional conclusions & Statement of work
The temperature itself is of little use for knowing component status, the local heat flux density being unknown
Valuable knowledge about component status is present in the thermal dynamics of a hot spot
Numerical algorithms to be developed, to reveal that hidden data
Historical method : search the 'thermal time constant' (t)
Expected  = 0.7 second
Measured = 0.3 second
Difference attributed to thin deposited layer

## Slide 8: Estimating the thermal time constant of PFCs
The usual method : hunt for power time evolution with abrupt change and long enough plateaux before and after the change
At WEST, less than 10% of the plasma discharges are like this
Power
Time
Needed : a method allowing to estimate t on most plasma discharges
  Ramped power
  No power plateau
Power time profile for a typical selection of WEST plasma discharges of C3B btw #53800 et #53950

## Slide 9: Temperature history identification with Proportional control law
Example with tup = 1 second and tdown = 0.2 second
Order(i)
action(i+1) = G x (Ri – Oi)
Process
Result(i)
Non-Heaviside function
8 seconds heating

## Slide 10: Proportional Control – real power time history
Simple time history
Unsteady time history
Power time profile (normalised to 1)
Calculated Temperature, using tau_up = 2 seconds and tau_down = 5 seconds
Power time profile (normalised to 1)
Calculated Temperature, using tau_up = 2 seconds and tau_down = 5 seconds

## Slide 11: Optimisation toward best fit by comparison to temperature history
Define cost function Temperature
Minimisation algorithm
Power
Measured
Temperature
Calculated
Temperature
Script output :
tup = 0.8 s
tdown = 0.5 s
Zone "pipe" - 53827
Time (s)
Temperature or power, normalised to 1 (.)

## Slide 12: Stability of the identification technique
Same hot spot, another discharge
Power
Measured Temperature
Calculated Temperature
10-20% accuracy
Zone "pipe" - 53816

## Slide 13: Large use on C3 campaign
Results ( next slides )
Strengths / weaknesses ( next slides )

## Slide 14: 3 hot spots: div_bas (=inertiel), pipe (= cooled), electrode (=codeposit)
Algorithm stability (no crash  good)
Some difference btw tau_up and tau_down
Visible fast & slow components
More steadiness needed  discussed next slide
Scale [0 – 14] seconds
Scale [ 0 – 2] secondes

## Slide 15: Normalisation
Requires normalised signals = "min-max normalised"
Power shall be between 0 and 1
Temperature shall be btw 0 and 1
UA
Power x 10
Temperature
Time
Zone "pipe" 53826
200°C
0°C
10 MW
0
100°C
5 MW
20s
0
10s
1.0
0.8
0.
20s
0
10s
0.6
0.4
0.2
Time
Min – max normalisation to be improved toward more stable estimates

## Slide 16: Issue 1 : temperature drift
Power
Temperature
Final temperature plateau hotter than initial
Correction – or no correction ?
Sometimes meaningfull – sometime not.
Possible correction of the temperature time profile with affine law btw t_begin and t_end – doable, but shall seek/keep justification
t_begin
t_end
Probable cause : Photonic background increase – or progressive increase of an inertial component coinciding cartesian reflexion

## Slide 17: Issue 2 – Non proportional plateaus Power Temperature
Zone "pipe" for #53897
Ratio T_stable / P_stable changes
Possible effect of rad power, power deposition mechanism ….
This variation perturbs temperature reconstruction from power time trace
Maybe work shall be done for each discharge phase separately – phase 1, phase 2 , phase 3
Ratio T / P = 1 (par définition, plateau max de la normalisation)
Ratio T / P = 0.5
T / P = 0.8

## Slide 18: Conclusion
A algorithm based on proportional control rule is efficient for estimating the thermal time constant, even for plasma discharges having a power-time profile having no plateau
Very basic algorithm, can be implemented in any language (matlab, excel, python, C, whatever)
Consolidation work still to be done (exception handling, etc…)
More work shall be done toward increasing robustness, in presence of signal perturbations (parasitic signal, non-proportional plateaus)
Quality data signal helps getting good (= stable) estimates